## Slide 1: R&D Experience for KamLAND 3M liter Liquid Scintillator Detector
F. Suekane
RCNS, Tohoku Univ.
suekane@awa.tohoku.ac.jp
Frontiers of Liquid Scintillator Technology
FroST16@ FermiLab. USA

## Slide 2
Motivation of this talk
The KamLAND Detector uses 3000m3 of
oil (1200m3 of LS+1800m3 of Buffer Oil).
The detector has successfully produced
important physics results.
The detector was constructed 15 years ago
but is still the largest homogeneous LS
detector in the world.
It may be useful to show our experience of
the detector R&D for future large scale LS
experiment.
The following is a simplified R&D story of
the complicated actual tries and errors.

## Slide 3
Major Results from the KL detector
Discovery of Reactor
Neutrino Oscillation
q12 & Dm212 measurement
GeoNeutrino
Measurement
Awarded
Breakthrough
Prize

## Slide 4: An Early History of KamLAND
Idea (A.Suzuki) ~1993
Project Approval 1997
Detector Construction 1998~2001
Start Data Taking 01/2002
1st reactor paper (deficit) 12/2002 (PRL 90:021802)
2nd reactor paper (spectrum distortion) 06/2004 (PRL 94:081801)
Geo neutrino paper 07/2005 (Nature 436:499-503)
1997
1998
2001
1995
Neutrino man
Evolution of the Detector Design

## Slide 5
(1) Very Large & Uniform
Detector possible
 High Quality & Quantity Data
(2) High Light Output(>Cherenkov)
 Good Energy Resolution &
Low Energy threshold
(3) Abundant Protons
 Good for Low Energy ne
Detection
(4) Fast Pulse
 Good Timing & Position
Reconstruction
(5) Intrinsically Low U/Th/K
 Very Low Backgrounds
(6) price ~ a few K US$ /ton
 Low Cost
Why Liquid Scintillator?
The signal is delayed
coincidence with
n capture on H

## Slide 6
KamLAND Detector
... subjects of this talk
(1800m3)

## Slide 7
(1) Limited time, money, manpower and expertise of LS
(2) The LS can not be replaced after filling (no reservoir tanks).
(= Like a satellite, we can not fix problems once launched. )
(3) The detector size is very much larger than lab. test experiments.
(4) The required radio purity level was below the sensitivities of
laboratory measurements.
⇩
(1,2) Use only proven technologies. Make LS as simple as possible.
(1)  Robust design ( fine design based on sofisticated tests and
simulations) . Purpose of test experiments was to judge the tested
quality was OK or not. Not to evaluate the quality in detail nor to
make thorough investigations.
(2,3)  Do final check by 1-dimentional real length (6.5m) test
experiment to confirm the real scale performances.
(4)  Prepared the last resort (E>3MeV was safe) .
Do measures to reduce U/Th/K as much as possible.
Our Conditions and R&D Strategies

## Slide 8
I. Liquid Scintillator R&D
Tohoku-RCNS-2002-01
1. Introduction
2. Overview
3. Outline of R&D
4. Light Output
5. Transparency
6. Direct Light Yield Measurement
7. n/g, a/g Pulse Shape Discrimination
8. a Quenching
9. Oxygen Quenching
10. Studies with 1/14 scale LS System
11. Material Selection
Radio Purity
12. Preparation of LS and Initial
Performance in the detector
ArXive physics/0404071
"An Overview of the KamLAND
1 Kiloton Liquid Scintillator"
&
References:
Contents
.... and recollection of my memories.

## Slide 9
* Energy Resolution
* Light Output > 40% anthracene
* Light Attenuation Length >10m
* Radio Purity( U/Th/40K) <10-14/10-14/10-15g/g
* Quench Factor for 7.7MeVα >10
*Safety
Flash point >50℃
* Price a few US$/liter
* Oil companies have capacity to supply the large amount
of high quality oils within half year of filling period
Requirements for KamLAND LS

## Slide 10
KamLAND Liquid Scintillator (No hidden ingredients)
Pseudcumene

## Slide 11
Choice of the Aromatic Liquid
At that time,
* Xylene and Pseudocumen (PC) were commonly used in liquid
scintillators.
* PXE was less common.
* Linear Alkylbenzene(LAB) was not discovered yet by M.C..
 Thinking of our conditions, PC was almost unique candidate
because ...
* PC has higher flashpoint and more moderate and less toxic
compared with Benzen-Toluene-Xylen family
* PC was widely used for large scale LS detectors, such as
MACRO, Chooz, PaloVerde, and Borexino was planning to use it.
* Transparency of pure PC was measured to be very good.
* Large amount of high quality PC was produced in Japan by
COSMO oil company and it was not necessary to carry by ship.
(We were afraid of contamination from shipping tank wall. )

## Slide 12
 Our LS did not need to have as high light output as solar
neutrino detectors. Therefore, we diluted the PC with paraffin oil
(PO) to obtain,
* higher flashpoint (for safety),
* less toxicity, odor, reactivity (for safety),
* more H/C (more ne events) ,
* more transparency.
 There are 2 kinds of paraffin oil
Normal -Paraffin
(unique molecular structure)
Iso-Paraffin (or Mineral Oil)
(various molecular structures )
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H-C-C-C-C-C-C-C-C-C-C-C-C-H
etc.
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
C
H
H
H
H
C
H
H
H
H-C-C-C-C-C-C-C-C-C-C-C-C-H
Dilution of PC with Paraffin Oil

## Slide 13
Normal-Paraffin vs Iso-Paraffin (Mineral oil)
NP  Dodecane (N12K, Nikko Oil Company),
IP  Paraol-250(Showa Shell)
We picked up candidate products from NP and IP based on
high flashpoint and good availability in Japan.

## Slide 14
For >20%PC, the increase rate of the light output becomes slow.
Flashpoint became reasonably higher.
 Determined to PC:PO=20:80 volume %
Determination PC : PO Dilution Ratio
Light Output
Flash Point
Then we measured transparency of the oils. Since the KL detector
size is ~10m, we needed to measure the attenuation length of L>10m
N12
P250

## Slide 15
Noise of
Laser flash
Signal (IL)
(L=2.75m)
Signal (IS)
(L=1.0m)
IS
IL
* Long path length (1.75m)
* Remove laser noise
* Cancel laser instability
* Cancel PMT instability
* 0-calibration with air
 Measurement of L>10m
possible
1.75m
Attenuation Length
Attenuation Length (L>10m) Measurement

## Slide 16
Oil tubes
Integration
Spheres
End of an oil tube.
( UV transparent acrylic window)
N2 Dye Laser
Optical fibers

## Slide 17
Attenuation Length
N12K vs P250
Light output (PC20%+PO80%)
N12K was more transparent
N12K gave slightly higher light output
Additional good features of NP
* Distillation temperature window is narrow ( intrinsically pure)
* H/C ratio and density etc. are accurately known
(Less systematic error of n flux measurement, safe filling, etc.)
 We chose N12K to dilute PC
P250
N12K

## Slide 18
Radio Purity Measurements of Oils
It was necessary to measure many samples.
Measurement Methods: ICP-MS (Inductively Coupled Plasma Mass-Spectrometry) ;
Sensitivity ~10-13 g/g
Requirements: U/Th/40K <10-14/10-14/10-15 g/g
Reactor neutrino oscillation measurement
at E>3MeV was guaranteed from these
results.
However, E<3MeV was not guaranteed.
We could only hope, after careful treatments
and water extraction, the actual
contaminations would satisfy the
requirements.
 In the end the contamination turned out
to be very low. 
Sample U(g/g) Th(g/g) 40K(g/g)

## Slide 19
* 1st Flour
PC+PPO was most widely used in
large LS detectors. The emission
spectrum matches to the Q.E.
spectrum of our PMT.
 We decided PPO was the first
candidate.
Flours
* 2nd- ary wave length shifter:
2nd- ary wave length shifter, such as bis-MSB shifts the wavelength beyond the PMT highest Q.E. region.
A simulation showed light yield would be reduced with bis-MSB.
 We decided not to use 2ndary flour.
* Antioxidants:
We decided not to use antioxidants such as BHT because the LS would
be kept in completely dark and cold environment, and LS will be bubbled
by N2 before filling and kept in N2 gas.

## Slide 20
Choice of PPO Manufacturer
PPO samples from 5 different
manufacturers were tested and we
found the quality very much depend
on the manufacturers and even production
batches.
(1) Light absorption is a very good indicator of contaminations.
15g/L (10 times of LS) of PPO was dissolved in N12 and light absorption
was measured. Dissolution power of N12 is poorer than BTX and
contaminations more likely come out as sediments.
Manufacturer of the PPO was selected by
(1) Light absorption and sediments when dissolved in N12,
(2) Radio Purity, (3) Capacity of production (1.8ton) (4) Price,
(2) Radio purity measurements
 next page
good
example
L=10cm

## Slide 21
Since PPO was the "dirtiest"
material in the LS, we made
many U/Th/K measurements
with various conditions.
Sample U(g/g) Th(g/g) 40K(g/g) Method and date
Some samples did not
satisfy our requirements.
We asked extra purification to
manufactures.
Finally Packard PPO with
extra purification was selected.
(Another company produced very
good PPO but did not have capacity)
(2) Radio purity measurement.
Choice of PPO Manufacturer

## Slide 22
Real Path Length (6.5m) Direct Light Yield Measurement
* The 5" PMT has the same
photocathode as the KL PMT.
0.1~0.2 p.e./signal  photon counting
Absolute p.e. yield/MeV can be
measured after passing through 6.4m.
LS in black-anodized
aluminum tube (V=105 liter).
5"PMT
In order to determine the PPO concentration and measure the actual
number of p.e./MeV in the KL detector, full scale light yield
measurement was performed.
Cosmic ray
L=6.5m system

## Slide 23
5"PMT
(reference)
Cosmic-ray trigger counters
5"PMT
(photon counter)
Black Anodized Tubes(6.8m Long)

## Slide 24
From this study,
(1) Optimum PPO concentration=1.5g/liter for this size.
(2) Absolute light yield = 190 p.e./MeV
(3) Time structure of signal
(4) N12K base LS was found 30% more p.e. than P250 base LS.
(5) Long time stability
were measured.
degradation due to
self absorption
PPO concentration dependence of light yield
With these results, we finally select N12K and became confident
that the LS will work in the KamLAND detector.

## Slide 25
Long term stability measurement
The 6.5m system was used for the long term stability measurement
Since L is long, a slight changes of transparency as well as light output,
due to degradations of the LS affect the light yield much.

## Slide 26
Confirmation of delayed coincidence with 1/14 scale (380 liter)
test system (we did not have experience of delayed coincidence.)
 We learned how the delayed coincidence signal looks like.
Measured neutron absorption time, etc.
Dt (p-d)
Ep
Am-Be
Ed
BKG
Ep
Ed
This was our first
delayed coincidence
signal

## Slide 27
a quench factor (RQ)
Dissolved Rn in the
LS by bubbling
N2+Rn gas and
measured a quench
and a/g PSD.
U rich soil
214Bi
214Po(t=236ms)
210Pb
b(3.26MeV)
g(0.8MeV)
+a(6.9MeV)
Possible correlated
BKG
RQ
RQ
required
7700KeVa
 600KeV
(RQ~12)

## Slide 28: Buffer Oil Determination
1kton's of LS is contained in a thin
plastic balloon. It was necessary to
match the specific gravity of LS and
the buffer oil to avoid the pressure
caused by the density difference.
 Since P250 is heavy and we had
measured P250 has good properties,
we mixed N12 and P250 and tuned
the specific gravity of the buffer oil.
Specific Gravities: rN12=0.7526, rPC=0.8796, rP250=0.7958
B.O.=0.41 N12K + 0.59 P250

## Slide 29
 | Requirements | Expected from Lab. Tests | Achieved in real detector
Energy Resolution (1/sqrt(E(MeV)) | <10% | 7.3% (statistical only) | 7.5%
Attenuation Length | >10m | 10m @400nm | ~22m (effective length)
Light Output (anthracene) | > 40% | 50% | ~57%
Light Yield (pe/MeV) | 100 | >190 | ~300
Radio Purity(g/g) |  |  | 
U/Rn | < 10-14 | < 2x10-13 | 3.5 x 10-18
Th | < 10-14 | < 2x10-13 | 5.1 x 10-17
40K | < 10-15 | <2x 10-14 | 2.7x 10-16
Initial Performances (Values may be different from current ones)
The Light yield was much more than expected due to light absorption &
reemission effect which could not be measured with small test systems.

## Slide 30
1.8 ton PPO
from Europe
1,000m3 P250
(80x12m3 tank truck)
1,800m3 N12
(150x12m3 tank truck)
240m3 PC
(120x0.2m3
s.s. drums)
The LS was blended on site by us.
We cleaned inside the lorry tanks

## Slide 31
II. R&D of 1200 m3 Balloon
Real Size
Prototype Balloon

## Slide 32
Reference: Achievement Report by Prof. A.Suzuki (2004)
II. R&D of 1200 m3 Balloon

## Slide 33
Design Requirements for balloon
(1) Size: 13mf (slightly teardrop shape) (V=1,200m3)
(2) Strength: 1cm head pressure +Dr (0.3%)
(3) Oil tolerance: Compatible with LS and BO
(4) Transparency: >90% for l=400nm
(5) Radio purity: <0.1Hz /m2 g(E>1MeV)
(= <1Hz @ fiducial (r<5.5m) in LS)
(6) Gas permeability: rRn(in)/rRn(out) <10-4
(7) Oil leakage: <20m3/year
(8) Lifetime >5 years

## Slide 34
44 panels
Film and Net structure
The central part of the balloon is
made of 44 lens-shaped films.
Kevlar braid ropes surround
the balloon and hang and fix the
position

## Slide 35
Film
Film: 5-layers 135mm thick (Nylon(ON)+EVOH(XL)) films
Multilayer film:
Pros. * Design freedom, * Avoid pin-hole
Cons. * Tests are needed for glue of lamination
* Dust contamination between the films
135mm
XL(15mm)/ON(25mm)/ON/ON/XL
EVOH
H
H
H
H
-C-C-
n
H
H
H
-C-C-
m
OH
-

## Slide 36
 |  | EVOH | Nylon | Polyethylene
Parameter | unit | EF-XL (Kuraray) | ON | LDPE
Tensile Strength | kg/mm2 | 21 | 20 | 2
Young modulus | kg/mm2 | 360 | 170 | 15
Gas Parmiability (N2) | cc m/m2/day/atm | 0.001 | 0.2 | 4~8
Melting Temp. | deg C | 181 | 220 | ~110
Oil Compatibility | hrs (JIS Z 1515) | infinite | infinite | 20
Transparency | l=420nm, 0.1mmt | 92% | 80% | 90%
Hygroscopic | % | 2.8 | 4.0 | 0.2
Microwave absorption |  | Yes | No | No
Molecular Structure |  | [CH2CH-OH] | [CO-(CH2)5-NH] | [CH2CH2]
* As strong as Nylon.
* However, the max. thickness = 15mm  multi layer film
* Better transparency than Nylon,
* Good oil compatibility.
* Very good gas barrier (Rn protection)
* RF welding possible
* Good hygroscopicity  antistatic  prevent dust collection
Our Magic Film : Ethylene Vinyl Alcohol (EVOH)
H
H
H
H
-C-C-
n
H
H
H
-C-C-
m
OH
-

## Slide 37
 |  | EVOH | Nylon | Polyethylene
Parameter | unit | EF-XL (Kuraray) | ON | LDPE
Tensile Strength | kg/mm2 | 21 | 20 | 2
Young modulus | kg/mm2 | 360 | 170 | 15
Gas Parmiability (N2) | cc m/m2/day/atm | 0.001 | 0.2 | 4~8
Melting Temp. | deg C | 181 | 220 | ~110
Oil Compatibility | hrs (JIS Z 1515) | infinite | infinite | 20
Transparency | l=420nm, 0.1mmt | 92% | 80% | 90%
Hygroscopic | % | 2.8 | 4.0 | 0.2
Microwave absorption |  | Yes | No | No
Molecular Structure |  | [CH2CH-OH] | [CO-(CH2)5-NH] | [CH2CH2]
Item | Unit | EF-XL | ON | LDPE
 |  | EVOH | Nylon | Polyethylen
tensile strength | kg/mm2 | 21 | 20 | 2
Young's modulus | kg/mm2 | 360 | 170 | 15
hygroscopicity | % | 2.8 | 4.0 | 0.2
gas permeability | cc/m2/day/atm (O2) | 0.3 | 50 | 2700
Oil Compatibility | hrs (JIS 2 1515) | Infinite | Infinite | 20
melting temp. | deg C | 181 | 220 | ~110
transparency | l=420nm, t=0.1mm | 92 | 80 | 90
RF welding |  | Yes | No | No
EVOH
H
H
H
H
-C-C-
n
H
H
H
-C-C-
m
OH
-
Our Magic Film : Ethylene Vinyl Alcohol (EVOH)

## Slide 38
U in PMT glass  Rn
 Balloon film  LS
Rn
Good Gas barrier property of EVOH
 Prevent for Rn intrusion to the LS region
O2 permeability
N2 permeability
EVOH
Nylon
PVC
PE/FEP

## Slide 39
How to join the films.
The -OH part of EVOH absorbs micro wave and heated from inside.
Sandwich another EVOH film at joining part and apply RF.
The 3 EVOH film layers melt to one.
metal
rod
Pressure
Metal table
RF
EVOH
* Heated from inside
 The metal rod does not damage the surface of the film
* The melting temperature of EVOH is lower than Nylon
 does not damage Nylon layer.
* Visual inspection of joining part possible.

## Slide 40
Strength tests for film material and welding part
Pulling
Creeping
repeating load/unload
Tearing
Compatibility with LS/BO
Transparency
Radioactive contamination
Rn barrier (by Stanford Univ. )
:
:
Tests of Films

## Slide 41
A lot of lot of tests

## Slide 42
Radio contamination measurements
Final film
ICP-MS
Flame A. A.

## Slide 43
# | Diameter (scale) | Film configuration | Main Test Subject
1 | 90cm (1/14) | CN/ON/XL/CN | Strength test
2 | 90cm(1/14) | CN/ON/XL/CN | Used in the test bench.
3 | 65cm(1/20) | XL/ON5/XL | Used in the test bench. Took delayed coin. signal.
4 | 90cm(1/14) | XL 15mmt | Study of LS filling method
5 | 65cm(1/20) | XL/ON5/XL | Strength Test
6 | 65cm(1/20) | XL/ON5/XL | Long term strength test
7 | 3.25m(1/4) | XL/ON5/XL | ¼ scale. Water-water strength test
8 | 3.25m(1/4) | XL/ON5/XL | ¼ scale. Water-water strength test
9 | 13m(1/1) | XL/ON5/XL | Full scale. Comprehensive practice in real KL tank.
10 | 13m (Real) | XL/ON5/XL | Final balloon
9 test balloons were made before real one

## Slide 44
Test balloons

## Slide 45
KamLAND Balloon Under Fabrication
 Then Installation and LS filling followed.

## Slide 46: The First Result 2002.12
2416 citations (as of 20/Mar./2016)
Front
Page
of PRL

## Slide 47
Conclusions
* R&D for KamLAND detector was successfully completed and
a good neutrino detector was realized. It has been in operation
for 15 years and has led several important physics results.
* When we started R&D for the KamLAND detector, we did not
know LS technology well. We owe many people for their advices
and helps.
Although this talk showed only a small part of the whole R&D
stories, I hope this could be any repay to the next large LS
detectors.