## Slide 1: 46: Encapsulated Sulfur Targets
Ntombizonke Kheswa
(iThemba LABS)

## Slide 2
Low abundance of 36S (0.01%).
Enriched 36S material is very expensive ($190/mg) while having an enrichment of less than 90%.
Elemental sulphur targets sublime rapidly in vacuum when subjected to beam bombardment.
46:Enriched Sulphur targets for light ion beam experiments

## Slide 3
Ag2S, thickness 20 μg/cm2, A. S. Kachan et al., Izv. Akad. Nauk RAS, Ser.Fiz. 72, 430 (2008)
CdS S. Piskor et al., Nucl. Phys. A414 (1984) 219
GeS L.M. Solinet al., Sov. J. Nucl. Phys. 29 (1979) 143
C implanted foils 26μg/cm2 carbon, 2-3 μg/cm2 36S W.von Oertzen, et al., Z.Phys. A353, 373 (1996) 30μg/cm2 carbon, 10 μg/cm2 36S(96%) L.K. Fifield and N.A. Orr, Nucl. Instr. Meth. A288 (1990) 360
H2S gas target (100 μg/cm2 Ti foils), G. Eckle et al., Nuclear Physics A491 (1989) 205-226
S (264 μg/cm2 ) sandwiched between C + Formvar (30 + 5 μg/cm), A. Hogenbirk et al., Nuclear Physics A516 (1990) 205-254
Enriched Sulphur targets for light ion beam experiments

## Slide 4
Light ions with low energy loss p, d, t, a at 100 Mev/u
Minimal use of enriched material: “what I buy is what I use”
Reduced loss of sulphur material using Mylar sandwich (C10H8O4)
Spread of heat deposition using a swivelling mechanism
Target for energetic light ion beam experiments

## Slide 5
Target Production
Two Mylar (0.5 µm thickness) foils are “adhered” together by applying heat using a temperature controlled soldering iron and conducting rod (copper)
Mylar foils are stuck together and encapsulating 1 mg of sulfur material with a surface area of approximately 1 cm2
The target frame is made of two identical rings allowing 4 M2.5 screws to clamp the mylar foil in between.
Sulfur
Welding tool
Heat supply
Target
Mylar

## Slide 6: Targets

## Slide 7
Ion Beam Analysis
Two motors displace the target to expose the sulphur material evenly
A surface barrier detector placed at 135 degrees with respect to the beam axis.
3MeV proton beam between 1-10nA.

## Slide 8: Target in action

## Slide 9
RBS spectrum
C, O from Mylar. Highest energy contributor is Sulphur
C
O
S

## Slide 10
Typical thickness
Starting with 1mg/cm2 of Sulphur material, RBS indicates about
0.5mg/cm2 in between the foils (consistently observed on 3 different targets)
Material may be lost at the welding stage
High roughness ~2mg/cm2 FWHM (powder directly deposited on foils)
C | H | O | S | Total mg/cm2
85 | 5 | 120 | 450 | 660

## Slide 11
Scaler on Ep > 2.5 MeV
Arrows indicate when the target is swivelling, measurements taken when high sulphur spots are found (4 hours @ 6nA, 3MeV protons)

## Slide 12
Conclusions
Roughness was expected to reduce with beam exposure, but it keeps pretty high
Heat treatment after welding could be applied to melt sulphur in between the foils
Effective method to produce targets with extremely small amount of material (1mg → 0.5mg/cm2) and good tenure to radiation

## Slide 13: THANK YOU FOR THE ATTENTION