## Slide 1
Manufacturing and characterization of targets in IFIN-HH: developing an interdisciplinary body of knowledge
INTDS, 2018
Andreea MITU
Horia Hulubei National Institute for Physics and Nuclear Engineering
(IFIN-HH)

## Slide 2
INTDS, 2018
1/81
Outlines:
Target laboratory in IFIN-HH
Laboratory development
Specific examples and particularities
Target preparation and characterization
Nuclear forensics laboratory: developing an interdisciplinary collaboration
Conclusions and perspectives

## Slide 3
2/81
My current status
INTDS, 2018

## Slide 4
INTDS, 2018
3/81
Outlines:
Target laboratory in IFIN-HH
Laboratory development
Specific examples and particularities
Target preparation and characterization
Nuclear forensics laboratory: developing an interdisciplinary collaboration
Conclusions and perspectives

## Slide 5
INTDS, 2018
4/81
Where?
Horia Hulubei National Institute for Physics
and Nuclear Engineering
IFIN-HH
Bucharest-Magurele, Romania

## Slide 6
5/81
General information
Brief History
1949: Institute of Physics of the Romanian Academy
1956: Institute of Atomic Physics (IFA)
1977: Central Institute of Physics (ICEFIZ)
IFIN (nuclear),
IFTAR (radiation equipment),  IFTM (materials),
CFPS (earth),
IGSS (space),
1990: ICEFIZ became IFA
1996: IFIN-HH
￼
Horia Hulubei (1896-1972)
Founder and First Director
of the Institute
Contribution to the study of quantum diffusion of X-rays
(Ph.D. Thesis, Paris, 1933)
Supervisor: Jean Perrin (Nobel Prize)
Chairman: Marie Curie (Nobel Prize)
INTDS, 2018

## Slide 7
6/81
Research Areas
￼
Basic Physics Research
Nuclear Physics and astrophysics
Particle physics and field theory
Atomic physics and condensed matter physics
Mathematical physics and information physics
Life and environmental protection
Applied Physics Research
Advanced detection systems
Nuclear safety, radiation protection and radioactive products
Radioecology and nuclear biomedicine
Nuclear techniques and applications
Advanced communication systems
INTDS, 2018

## Slide 8
7/81
Research Departments
￼
Theoretical physics
Nuclear physics
Tandem Accelerators
Hadronic Physics
Elementary Particles Physics
Computational Physics and Informational Technologies
Life and Environmental Sciences
Radioisotopes and Radiation Metrology
Applied Nuclear Physics
Multipurpose Irradiation Facility Centre
Nuclear Training Centre
Reactor Decommissioning
Radioactive Waste Management
Protection and Prevention Compartment
The Centre for Technology Transfer and Marketing
Details on: http://www.nipne.ro
INTDS, 2018

## Slide 9
8/81
Extreme Light Infrastructure (ELI-NP)
￼
Details on: http://www.eli-np.ro
ELI-NP facility will consist of two components:
A very high intensity laser system, with two 10 PW laser arms;
A very intense brilliant γ beam (1013 γ/s), which is obtained by incoherent Compton back scattering of a laser light of a very brilliant, intense, classical electron beam (Ee up to 720 MeV) produced by a warm LINAC.
Under construction!
INTDS, 2018

## Slide 10
INTDS, 2018
9/81
Experimental Infrastructure in IFIN-HH
9 MV Tandem
ROSPHERE gamma detectors array
3MV Tandetron
1MV Accelerator Mass Spectrometry
19 MeV Proton Cyclotron for production of radioisotopes
Gamma-ray Irradiator

## Slide 11
INTDS, 2018
10/81
9MV TANDEM ACCELERATOR
25 positions on 5 rings (37◦ ,70◦, 90◦, 110◦, 143◦ )
2 configurations envisaged: - 15 50% HPGe detectors with BGO shields and 10 to 20 LaBr3(Ce)
scintilators
- 25 50% HPGe detectors
- ROmanian array for γ-SPectroscopy in HEavy ion Reactions

## Slide 12
INTDS, 2018
11/81
Types of experiments performed at 9MV tandem accelerator
Recoil Distance Doppler Shift method (RDDS)
Target support
Stopper support
Micrometer
Sliding Bearings
inchworm
Piezocrystal
L=814 mm
PLUNGER reaction chamber (Cologne design)

## Slide 13
INTDS, 2018
12/81
Types of experiments performed at 9MV tandem accelerator
Tape Station used for gamma-ray spectroscopy:
 Kapton tape transport station in closed loop
 Flexible time cycle control using in-house electronics
 3x HPGe clovers (Eff ~ 1%) w/ BGO suppression
 Angular correlation table
 Digital data acquisition system
Target requirements
thin (<2 mg/cm2)
self-supported targets that allow the recoil products to scatter onto the kapton tape

## Slide 14
INTDS, 2018
Types of experiments performed at 9MV tandem accelerator
γ,n,p
α
projectile
ejectile
target
I. Activation
g
g
HPGe
detector
target
Counting setup in Bucharest, IFIN-HH, Romania
              2 HPGe detectors (relative efficiency of 55 % and 100%)
              Passive lead shielding
              Close detection geometry
              -> the summing corrections were performed using the Monte Carlo simulation code GESPECOR
Pb walls and Cu and Al plates on the inside
The activation technique consists in bombarding the target with α-particles to produce radioactive nuclei followed by the measurement of their specific activities once the irradiation has stopped.
II. Counting
13/81

## Slide 15
INTDS, 2018
No matter the type of experiment one wishes to perform, a good target is needed!
13/81

## Slide 16
INTDS, 2018
The target preparation laboratory in IFIN-HH
TARGETS FOR NUCLEAR STRUCTURE EXPERIMENTS:
thin films, self-supported or deposited on various backings, the material to be deposited is isotopically enriched
14/81

## Slide 17
INTDS, 2018
Equipment for target preparation
Vacuum chamber
- stainless steel
- cylindrical
- 45 cm diameter
- 53 cm high
used for creating self-supported,
backed or sandwiched targets by:
  - thermal evaporation
  electron-gun evaporation
  sputtering deposition methods
HIGH VACUUM DEPOSITION SYSTEM produced by
Intercovamex Company
15/81

## Slide 18
INTDS, 2018
Thermal evaporation process
Electron gun process
Sputtering process
Evaporation methods
16/81

## Slide 19
INTDS, 2018
Outlines:
Target laboratory in IFIN-HH
Laboratory development
Specific examples and particularities
Target preparation and characterization
Nuclear forensics laboratory: developing an interdisciplinary collaboration
Conclusions and perspectives
17/81

## Slide 20
INTDS, 2018
e-beam evaporation - Mantis Deposition System
Description…..
https://www.mantisdeposition.com/uhv-components
18/81

## Slide 21
INTDS, 2018
The control system for e-beam
Control of each pocket
Monitoring all parameters
19/81

## Slide 22
INTDS, 2018
20/81
Rolling equipment
This is an extremely efficient method for self-supported metallic foil production using small amounts of starting material. The rolling method allows preparation of metallic foil with thicknesses ranging from several hundreds of µg/cm2 to hundreds of mg/cm2.

## Slide 23
INTDS, 2018
Manual press vs. Hydraulic press
21/81

## Slide 24
INTDS, 2018
Outlines:
Target laboratory in IFIN-HH
Laboratory development
Specific examples and particularities
Target preparation and characterization
Nuclear forensics laboratory: developing an interdisciplinary collaboration
Conclusions and perspectives
22/81

## Slide 25
INTDS, 2018
How to choose the preparation method?
target characteristics (thickness, surface, shape)
material cost and availability (metallic form, compound)
availability of the method in the target preparation laboratory
method effectiveness
avoiding contamination of the target
23/81

## Slide 26
INTDS, 2018
Target characteristics
TARGET
thickness
thickness uniformity
identification of impurities
surface roughness
surface morphology
24/81

## Slide 27
Target preparation methods
Mechanical reshaping and powder processing
Physical
Chemical
Rolling
Material preparation (melting, conversion into metallic form)
Powder processing (tablet pressing, sedimentation)
Vacuum deposition (resistive heating, electron gun, sputtering)
Electrodeposition
Molecular plating
Classification
INTDS, 2018
25/81

## Slide 28
INTDS, 2018
Target characterization
Alpha particle energy loss
PIXE (Particle Induced X-Ray Emission)
PIGE (Particle Induced Gamma-Ray Emission)
RBS (Rutherford Back Scattering)
AFM (Atomic Force Microscopy)
SEM/EDX (Scanning Electron Microscopy/ Energy dispersive X-Ray)
XRD (X-ray Diffraction)
26/81

## Slide 29
INTDS, 2018
Targets
SrF2
SrCO3
57Fe
24Mg
64Ni
Rh
58Ni
70Zn
68Zn
LiF2
196Pt
194Pt
Os
W
106Cd
27/81
INTDS WEBSITE

## Slide 30
Database
Argonne National Laboratory, 2018
Network
Database
Strong
Community
28/81

## Slide 31
INTDS, 2018
Outlines:
Target laboratory in IFIN-HH
Laboratory development
Specific examples and particularities
Target preparation and characterization
Nuclear forensics laboratory: developing an interdisciplinary collaboration
Conclusions and perspectives
29/81

## Slide 32
INTDS, 2018
30/81
Preparation and characterization of thick osmium targets
Strontium targets for nuclear astrophysics experiments
Decontamination of 64Ni targets
Specific examples and particularities

## Slide 33
INTDS, 2018
Preparation and characterization of thick osmium targets
preparation and characterization of Os targets for nuclear astrophysics experiments with alpha particles
Al backing
α beam
Os target
γ
p
n
Os layer
31/81

## Slide 34
INTDS, 2018
Required characteristics:
Os
target
very smooth
without specks or wrinkles
constant thickness
32/81

## Slide 35
INTDS, 2018
Physical properties
high density
(22.5g/cm3)
toxic
brittle
hard
refractory
high vaporization temperature
(5012 °C)
76Os
Because of its hardness, brittleness, low vapor and very high melting point (3033 °C, the fourth highest of all elements, after only C, W, and Re), solid osmium is difficult to machine, form or work.
33/81

## Slide 36
INTDS, 2018
Target preparation method
PULSED LASER DEPOSITION ( PLD )
Developed in collaboration with INFLPR
National Institute for Laser, Plasma and Radiation Physics
(Bucharest-Magurele, Romania)
34/81

## Slide 37
INTDS, 2018
PULSED LASER DEPOSITION (PLD)
vacuum chamber
35/81

## Slide 38
INTDS, 2018
The advantages of PLD method
- It allows deposition of chemical elements, compounds and some polymers;
- It allows obtaining thin layers of better quality compared to other methods:
high density
thickness uniformity on the defined surface
controllable thickness
high purity
durability
36/81

## Slide 39
INTDS, 2018
Os targets
Nd:YAG Laser: 1064 nm (IR range)
Os [2000nm] / Al [20um]
Os [100nm] / glass (test)
37/81

## Slide 40
INTDS, 2018
Target characterization
-morphology, composition, structure and thickness determination-
XRD (X-Ray Diffraction)
RBS (Rutherford Back Scattering)
AFM (Atomic Force Microscopy)
SEM/EDX (Scanning Electron Microscopy/ Energy Dispersive X-ray Spectroscopy)
38/81

## Slide 41
INTDS, 2018
Morphological features
Os/glass
Rq=1.38 nm
Long deposition (30 h)
Rq=0.31 nm
glass
Rq=35.6 nm
Al
Rq=44.06 nm
Os/Al
Os/Al
Rq=36.33 nm
Short deposition (5 h)
Backing
AFM
topography images
39/81

## Slide 42
INTDS, 2018
SEM and EDX Os/Al mapping micrographs
Al
Mag=25.00KX
Al
Os/Al
40/81

## Slide 43
INTDS, 2018
41/81
XRD spectra

## Slide 44
INTDS, 2018
RBS spectra of Os deposited on Al,
measured by the RBS fixed detector at 165°
The thickness is: 98.6 nm, corresponding to 0.222 mg/cm2
It implies - the use of a rather simple scattering geometry
- the use of a beam composed of light nuclei
- a particle detector placed at backwards angles
The thickness is: 2240 nm, corresponding to 5.05 mg/cm2
42/81

## Slide 45
INTDS, 2018
Experimental results
Os stable isotopes:
184Os 0.02 %
186Os 1.59 %
187Os 1.96 %
188Os 13.24 %
189Os 16.15 %
190Os 26.26 %
192Os 40.78 %
Example of one of the reaction of interest:
43/81

## Slide 46
INTDS, 2018
Strontium targets for nuclear astrophysics experiments
The isotopes produced on natural strontium targets by α irradiation
0.56 % 84Sr
9.86 % 86Sr
7.00 % 87Sr
82.58 % 88Sr
Proposed experiment
86Sr
87Sr
88Sr
88Zr
89Zr
90Y
87Y
91Y
(α,p)
(α,n)
(α,p)
(α,p)
90Zr
91Zr
92Zr
84Sr
(α,γ)
44/81

## Slide 47
INTDS, 2018
Ideal target
45/81

## Slide 49
Can we use it?
NO!

## Slide 50
INTDS, 2018
Trouble…
Metallic Sr targets exhibit a significant chemical activity and oxidize very fast in regular environment (air)!
48/81

## Slide 51
INTDS, 2018
Solutions?
This is a major constraint for measuring absolute cross-sections for the alpha particle activation of Sr isotopes.
49/81

## Slide 52
SrF2
SrCO3
INTDS, 2018
Strontium compounds
overcome this constraint by using targets consisting of strontium compounds which are not reactive in air!
Goal of the present study:
50/81

## Slide 53
INTDS, 2018
Targets
84Sr
86Sr
87Sr
88Sr
SrCO3
SrF2
51/81

## Slide 54
INTDS, 2018
Preparation of Sr targets
1. Pressing powder
2. Heating pellet
3. Evaporation of the Sr compound on Al backing
52/81

## Slide 55
INTDS, 2018
Vaporization temperature
~1500°C
~3000°C
SrF2
SrCO3
53/81

## Slide 56
INTDS, 2018
Target characterization
XRD (X-Ray Diffraction)
SEM (Scanning Electron Microscopy)
EDX (Energy Dispersive X-ray)
Nuclear activation measurements
54/81

## Slide 57
INTDS, 2018
X-ray diffraction
XRD patterns of Al substrate, SrF2 powder and SrF2/ Al target
XRD patterns of Al substrate, SrCO3 powder and SrCO3/ Al target
SrF2
SrCO3
55/81

## Slide 58
INTDS, 2018
SEM micrographs
B
4μm
SrF2
Al backing
SrCO3
SEM micrographs of:
SrF2/ Al
SrCO3/ Al
Al backing
56/81

## Slide 59
INTDS, 2018
EDX analyses
Copper contamination!
57/81

## Slide 60
INTDS, 2018
Nuclear activation spectra
87Sr(α,p)90Y
84Sr(α,p)87Y
86Sr(α,n)89Zr
86Sr(α,n)89Zr
84Sr(α,p)87Y
SrF2
SrCO3
58/81

## Slide 62
INTDS, 2018
Decontamination of 64Ni targets
AIM and IMPORTANCE of the experiment
- shape coexistence in 66Ni
T. Otsuka , private communication
64Ni(18O,16O)66Ni 39 MeV ROSPHERE array
60/81

## Slide 63
68%
4%
1%
26%
~1%
INTDS, 2018
61/81
Target used in the experiment

## Slide 64
INTDS, 2018
Targets required for the proposed experiment
2 thick
targets
3-4 thin
targets
5 mg/cm2
1 mg/cm2
To achieve all these targets I started
from 100 mg of 64Ni powder
62/81

## Slide 65
INTDS, 2018
Preparation of 64Ni foils
1. Pressing powder
2. Heating pellet
3. Rolling process
63/81

## Slide 66
INTDS, 2018
Reaction Kinematics below Coulomb barrier
Before
After
16O
18O
64Ni
66Ni
γ
HPGe detectors
ROSPHERE
+2n
64/81

## Slide 67
INTDS, 2018
Fusion-evaporation
cross-section calculation
Contaminants from 18O on 16O
18O + 64Ni @ 39 MeV
1425
1760
66Ni
65/81

## Slide 68
INTDS, 2018
How to improve the experimental
results?
Removing oxygen
66/81

## Slide 69
INTDS, 2018
How to remove the oxygen?
O
2H
H2O
Which is the first formula that we learn in chemistry?
67/81

## Slide 70
INTDS, 2018
Hydrogen oven
68/81

## Slide 71
INTDS, 2018
The thermal treatment for the 64Ni target
a- heating to 6000C (60min)
b- stationary at 6000C (30min)
c- heating to 6450C (60min)
d- stationary at 6450C (15min)
e- heating to 6500C (60min)
f- stationary at 6500C(120min)
g- cooling process to 250C (625min)
69/81

## Slide 72
INTDS, 2018
Comparison between before (top) and after (bottom)
the “target treatment”
The peak at 1425 keV has been used as normalization the two spectra
70/81

## Slide 73
INTDS, 2018
18O + 64Ni @ 39 MeV
(gg – total projection)
71/81

## Slide 75
Concluding remarks
Argonne National Laboratory, 2018
2
3
improvements
process efectiveness
1
73/81

## Slide 76
INTDS, 2018
Outlines:
Target laboratory in IFIN-HH
Laboratory development
Specific examples and particularities
Target preparation and characterization
Nuclear forensics laboratory: developing an interdisciplinary collaboration
Conclusions and perspectives
74/81

## Slide 77
The first nuclear forensics laboratory of Romania
The aim of this project:
Loss-of-Control Point
National Nuclear Forensic Library
Age, Isotopic Composition, Physical Form, Chemical Composition, Microstructure, Impurities, Dimensions, Surface roughness, etc.
Materials that contain uranium, plutonium and their descents
INTDS, 2018
75/81

## Slide 78
Why?
Over 630 nuclear trafficking incidents were recorded in the Black Sea states between 1991 and 2012
“In a strange turn of history, the threat of global nuclear war has gone down, but the risk of a nuclear attack has gone up.”
© B. Obama
INTDS, 2018
76/81

## Slide 79
INTDS, 2018
Unknown nuclear material
CHEMICAL CHARACTERISTICS
PHYSICAL CHARACTERISTICS
NULCEAR MATERIAL IDENTIFICATION
(U, Pu, MOX and their daughter products)
ELEMENTAL
COMPOSITION
ISOTOPIC
COMPOSITION
-weight, sizes and geometry -24h
-microstructure, morphology (aprox. 0.5μm) -24h
-microstructure, morphology (≤ 1nm) -1 week
-the exact chemical composition of the material -1 week
-metallic impurities, other elements -1 week
-type of material and isotopic composition -24h
-age determination -2months
77/81

## Slide 80
Tuning the first Romanian nuclear forensics lab
to Euroatlantic standards
Physical characteristics and macroscopic parameters:
Precise analytical balance
3D scanner
Optical microscope
High-resolution scanning electron microscope (SEM), equipped with energy dispersive X-ray detector (EDX)
X-ray diffractometer (XRD)
Chemical and isotopic composition:
Particle induced X-ray emission (PIXE)
Particle induced γ-ray emission (PIGE)
AMS (Accelerator Mass Spectrometry)
Gamma-ray Spectrometry
INTDS, 2018
78/81

## Slide 81
INTDS, 2018
Outlines:
Target laboratory in IFIN-HH
Laboratory development
Specific examples and particularities
Target preparation and characterization
Nuclear forensics laboratory: developing an interdisciplinary collaboration
Conclusions and perspectives
79/81

## Slide 82
Conclusions and perspectives
Thin films preparation for various types of nuclear physics experiments with accelerators
Production of targets by pulsed laser deposition
Target quality - characterization in terms of thickness, uniformity, purity in collaboration with several departments of our Institute
ACHIEVEMENTS:
Developing a database
LOOKING FORWARD:
INTDS, 2018
80/81

## Slide 83
THANK YOU FOR YOUR ATTENTION!
INTDS, 2018
81/81