## Slide 1: Long Quadrupole Giorgio Ambrosio Fermilab
BNL - FNAL - LBNL - SLAC
Long Quadrupole Task Leaders:
Fred Nobrega (FNAL) – Coils
Jesse Schmalzle (BNL) – Coils
Paolo Ferracin (LBNL) – Structure
Helene Felice (LBNL) – Instrumentation and QP
Guram Chlachidize (FNAL) – Test preparation and test
Notes: 1

## Slide 2: LARP R&D plan†
“S”: Shell-based support structure
“C”: Collar-based support structure
Length
† P.Wanderer, et al., "Overview of LARP Magnet R&D," Applied Superconductivity, IEEE Trans. on , vol.19, no.3, pp.1208-1211, June 2009
Completed
In progress
1st test
5/2010

## Slide 3: Long Quadrupole†
Main Features:
Aperture: 90 mm
magnet length: 3.7 m
Target:
Gradient: 200+ T/m
Goal:
Demonstrate Nb3Sn magnet scale up:
  Long shell-type coils
  Long shell-based structure (bladder & keys)
  LQS01 was tested in Nov-Dec 2009
  LQS01b test in progress
† LQ Design Report available online at:
https://plone4.fnal.gov/P1/USLARP/MagnetRD/longquad/LQ_DR.pdf
LQS01 SSL | 4.3 K
Current | 13.9 kA
Gradient | 242 T/m
Peak Field | 12.4 T
Stored Energy | 473 kJ/m

## Slide 4: LQ Structure†
LQS is based on TQS (1m model)
and LRS (4m racetrack)
  Segmented shell (4)
TQS Modifications:
  Added masters
  Added tie-rods for yoke & pad laminations
  Added alignment features for the structure
  Rods closer to coils
  Rods made of SS
† P. Ferracin et al. “Assembly and Loading of LQS01, a Shell-Based 3.7 m Long Quadrupole Magnet for LARP” to be published in IEEE Trans. on Applied Superconductivity.
Aluminum shell
TQS
LQS

## Slide 5: LQ Coils†
Fabrication technology:
  From 2-in-1 (TQ coils) to single coil fixtures (LQ)
  Mica during heat treatment
  Bridge between lead-end saddle and pole
Coil design:
  LQ coils = long TQ02 coils with gaps to accommodate different CTE during HT
Cross-section of TQ/LQ coil
LQ Coil Fabrication:
5 practice coils (Cu and Nb3Sn)
coils #6-#9  LQS01
coils #10-#13  LQS02
Note: coils #6-#9 had 3 severe discrepancies
† G. Ambrosio et al. “Final Development and Test Preparation of the First 3.7 m Long Nb3Sn Quadrupole by LARP” to be published in IEEE Trans. on Applied Superconductivity.

## Slide 6: LQS01 Load & Cooldown
Pre-load
  Target stress on shell
  Target stress on roads
  Lower stress on coils ID
Cooldown
  Shell: close to target stress
  Rods: close to target stress
  Coil ID: ~ ½ target stress
Azimuthal stress (MPa) in the coil poles during cool-down:
values measured (colored markers)
and computed (black markers) from a 3D finite element model

## Slide 7: Coil-Pad Mismatch
FEM model with azimuthally oversized coils (120 mm)
  bending due to coil-pad mismatch
  Lower stress in the pole
    Consistent w measurement
  Higher stress on midplane
    Risk of damage above 200 T/m
Verified during disassembly
  Tested with pressure sensitive paper
Contact points
Contact points

## Slide 8: LQS01 Quench History
Slow start
  First quenches at high ramp rate (200 A/s)
    Trying to avoid QPS trips due to voltage spikes
  Slow training at 4.5K
    Due to low pre-load on pole turns
Faster training at 3 K
  Reached 200 T/m
Stopped training
  to avoid coil damage before reassembly
200 T/m
200 A/s
Test report available online at:
https://plone4.fnal.gov/P1/USLARP/MagnetRD/longquad/report/TD-10-001_LQS01_test_summary.pdf
After the initial
training at 4.5 K
After the training
at 3.0 K
At the end of test
200 T/m

## Slide 9: Voltage Spikes
Large voltage spikes
  Due to flux jumps
    Seen in TQ magnets using RRP 54/61
  Larger than in TQs
  Variable quench detection threshold
  Variable ramp-rate during training
    200 A/s  3 kA
    50 A/s  5 kA
    20 A/s  9 kA
    10 A/s  quench
Maximum Voltage Spike amplitude at 4.5 K with 50 A/s ramp rate
RRP 54/61
by OST
Will be eliminated or significantly reduced by using RRP 108/127
RRP 108/127
by OST

## Slide 10: Magnetic Measurement
Magnetic measurement at 4.5K:
  Harmonics:
    Some are a few units different w.r.t. computed
    Similar to short models (TQ) †
    A few harmonics, slightly worse, may have been affected by assembly
  Dynamic effects
    No decay and snapback
In progress on LQS01b
Geometrical harmonics at 100 and 179 T/m field gradient.
Results are presented at 22.5 mm reference radius, which corresponds to the official radius adopted for LHC (17 mm) corrected for the increase in the magnet aperture from 70 to 90 mm.
An 81.8 cm long tangential probe was used.
# | 100 T/m (5.3 kA) |  | 179 T/m (10 kA) | 
 | Computed | Measured | Computed | Measured
b_3 |  | 2.29 |  | 2.61
b_4 |  | 6.73 |  | 6.93
b_5 |  | 0.17 |  | -0.08
b_6 | 9.8 | 9.89 | 6.1 | 7.47
b_7 |  | -0.06 |  | -0.11
b_8 |  | -0.98 |  | -0.38
b_9 |  | 0.19 |  | 0.13
b_10 | -0.04 | 0.35 | -0.02 | -0.47
a_3 |  | 2.28 |  | 2.28
a_4 |  | 1.94 |  | 2.11
a_5 |  | -0.51 |  | -0.65
a_6 |  | -0.12 |  | -0.29
a_7 |  | 0.29 |  | 0.14
a_8 |  | 0.08 |  | 0.06
a_9 |  | -1.09 |  | -0.16
a_10 |  | 0.37 |  | 0.12
† G. Velev, et al., “Field Quality Measurements and Analysis of the LARP Technology Quafrupole Models”, IEEE Trans. On Applied Supercond. , vol.18, no.2, pp.184-187, June 2008

## Slide 11: Coils after Test
Some “bubbles” on coils inner layer
  Coil-insulation separation
Possible causes:
  Superfluid helium and heat during quench
    Seen in TQ coils
  Heat from heaters on inner layer
    Only in LQ coils
Plans:
  Strengthen insulation or
  Change heater location

## Slide 12: LQS01b Loading
New shims give correct ratio between strain in the shell and strain in the coils (same coils of LQS01)
   More uniform prestress
Higher preload based on short models (TQS03 a/b/c)
   Peak load: 190 MPa +/- 30
LQS01b
12

## Slide 13: Strain Gauges: LQS01b vs. LQS01a
LQS01a: Most gauges unloading at 11.2 kA
LQS01b: No unloading at 12.8 kA

## Slide 14
G = 200 T/m
G = 220 T/m

## Slide 15
LQS01b: 220 T/m
in 4 quenches

## Slide 16: LQS01b Quench Location
Quench # 3:
Coil8_B2_B3
Quench # 9:
Coil 6_B2_B3
9
6
7
8
Most quenches are in Inner Layer pole turn, with a few exceptions
The location keeps changing
 Still training

## Slide 17: LQS01b Preliminary Observ.
LQS01b reached the best performance of all TQS02 series (made with same conductor)!!!
  With the first four LQ-production coils; three of which had “severe” discrepancies
   We know how to make and fix long Nb3Sn coils
  Al-shell-based structure is providing support (up to 225 T/m and 91% of ssl) with no signs of limitation
   Segmented shell structure can be used for long Nb3Sn magnets with shell-type coils
  Quench protection keeps hot-spot temperature below 260 K
   We have tools (computation & instrumentation) for protecting long Nb3Sn magnets above 2.2K

## Slide 18: Insulation Development
The cable insulation in LQS01 and LQS02 coils is an S2-glass sleeve
    Same insulation used in TQ and LR coils
    The application to long coils requires days of labor and is not suited for a production
Development of new insulation for Long Nb3Sn Coils and test in LQS03 coils:
  Plan A: E-glass tape (tested in TQ coils)
    Qualification in progress
  Plan B: S2-glass braided on the cable (NEWT)
    Qualification in progress
  Plan C: S2-glass braided on the cable (other vendors)
  Plan D: use the sleeve for LQS03 coils and continue develop.

## Slide 19: LQ GOALS
Next LQ models goals:
  Reproduce short-model performances (gradient and training):
    LQS01b/LQS02  TQS02 gradient at 4.5K (~220 T/m)
    LQS03  TQS03 gradient at 1.9K (~240 T/m)
  Demonstrate reproducibility & memory; 4m keys & bladders; uncontrolled cooldown:
    LQS02 , LQS02b
  Demonstrate conductor with reduced voltage-spikes &
  cable insulation suited for production:
    LQS03, LQS03b
Need still some R&D:
  Reliable solution for protection heaters on inner layer at 1.9K

## Slide 20: LQ Schedule
LQS01b test
LQS02a test
LQS02b test
108/127 coils
LQ test turn around time: ~ 7 months
LQ test time: 2 months

## Slide 21: Extra

## Slide 22: LQS01 Assembly
LQS01 assembled and pre-loaded
Strain gauge readings:
on the structure (shell & rods) are on target
on the coils are lower than expected with large scattering
  Seen also in TQS models; possibly caused by coil/pads mismatch
G. Ambrosio - Long Quadrupole
LARP CM14 - FNAL, Apr. 26-28, 2010
Comparison of measurements and targets
293 K | sy (MPa) | sz (MPa)
Shell measured | +33 ±8 | +3 ±7
Shell target | +34 | +6
Pole measured | -12 ±11 | +14 ±17
Pole target | -49 | -14
Rod measured | n/a | +60 ± 3
Rod target | n/a | +63

## Slide 23: LQS01 Cooldown
Azimuthal stress (MPa) in the coil poles during cool-down:
values measured (colored markers)
and computed (black markers) from a 3D finite element model
Delta stress on the pole lower than expected
Stress on the shell close to expected value
  Stress distribution in the coil different from the computed one
Azimuthal stress (MPa) in the coil shell:
values measured (colored markers)
and computed (black markers) from a 3D finite element model

## Slide 24: FEM Analysis
FEM model with azimuthally oversized coils
  bending due to coil-pad mismatch
  Lower stress in the pole
    Consistent w measurement
  Higher stress on midplane
    Risk of damage above 200 T/m
Less stress
More stress

## Slide 25: LQS01 Disassembly
Test with pressure-sensitive paper confirmed coil-pads mismatch
Contact points
Contact points

## Slide 26: Quench Location
All quenches in pole turns
  Except high ramp-rate quenches
  No preferred location
All coils participating
  Largest number in coil 07
    Smallest Ic margin

## Slide 27: LQS01b Pre-load
Target pre-load at cold:
  Pole: 160 ± 30 MPa
    Same as TQS03b
  Inner layer: 193 ± 30 MPa
    Lower than TQS03c
  Outer layer: 186 ± 30 MPa
    Lower than TQS03c
Delta based on sensitivity analysis
  Coil mid-plane variation: ± 50 mm
  Shell inner-radius variation: ± 65 mm
LQS01b
TQS03c