## Slide 1: RaDIATE
1st Annual Collaboration Meeting May 19 2014
Cost-effective Irradiations Discussion
Radiation Damage In Accelerator Target Environments

## Slide 2: How to afford material irradiations?
High energy protons
  Best match for RaDIATE parameter space
  Allows for miniature mechanical testing
  Needs to run in a non-parasitic mode on existing program or experiment
  Expensive
Low energy ions
  High dose rate
  Little to no residual activity
  Can allow for in-situ measurements
  No gas production
  Several “scaling” issues
  Less expensive,

## Slide 3: Issues with Low Energy Irradiations
Shallow depth of penetration (< 10 microns)
  Studies have typically been TEM, nano-indenter
  New work with micro-mechanics
Non-uniform DPA accumulation with depth
  Protons have more uniform profile
Dose rate effects
  Damage effects not equal for rastered vs continuous beam
No gas production
  Implant H, He with concurrent beams?
Ion “poisoning”
  Beam ions stop in material being studied
  Self-ions can be used, but still more interstitials than “normal”

## Slide 4: In-Between Case?
Proton irradiation in the 10 – 30 MeV range
  Gas production
  Depth of penetration
  More uniform damage profile with depth
  Protons “poison” sample with higher H “production”
  Dose rate is only remaining large issue
Will result in highly active samples!
Limitations in current mean small transverse irradiation area (<< 1 mm2)
Less expensive than high energy proton beam, but still expensive (> 1 k$ per hour)

## Slide 5: Need short term path and long term path
Within next 2 years?
  Low energy irradiations
    Use existing facilities at universities and Labs
    Develop higher current proton irradiation facilities (FETS?)
    Contribute to “scaling” studies (needs high energy validation)
  High energy irradiations
    Use existing facilities for “in-between” beam (10-30 MeV)
    Use as non-parasitic as possible irradiation volumes for higher energies (BLIP, NuMI)?
    Contribute to “scaling” studies as validation (needs careful planning)
  Develop solutions for the long term

## Slide 6: Need short term path and long term path
> 2 years?
  Low energy irradiations
    Continue to use existing facilities at universities and Labs
    Start to use FETS for larger (transverse) samples at high damage accumulation
    Capitalize on “scaling” studies to design more application relevant experiments
  High energy irradiations
    Continue to use existing facilities for “in-between” beam (10-30 MeV)
    Develop high current facility for “in-between” beam (energy upgrade for FETS?)
    Develop additional non-parasitic irradiation volumes for higher energies (SNS-FMITS)?
  Will need both high energy and low energy solutions

## Slide 7: Costs to “user” depends on context?
“Commercial” model-
  Where a user reimburses the facility for beam-time, often paying full overheads
  When Fermilab irradiates at BLIP (BNL) we follow this model (although overheads were kept to a minimum)
    Cost is near 60 k$ per week (~0.17 DPA per week for Ti)
  Even when doing low energy irradiations, the cost can be relatively high (~1,000 $/hr at BNL 1 uA Tandem)
“Academic” model-
  Where a student has a proposal for an experiment, and the facility does not charge for beam-time
  Obviously less expensive!
How to use the academic model?

## Slide 8: Discuss!
What facilities are available for now?
What are possibilities for non-parasitic irradiation volumes?
What about PIE?
  What activity level can available labs currently handle?
How do we utilize the “academic” model?
  Do we need to partner with universities?

## Slide 9: RaDIATE
10 keV protons into Beryllium (simulated with SRIM 2008 and artistically rendered with Graphic Converter by P. Hurh)
Radiation Damage In Accelerator Target Environments