## Slide 1: Novel Aluminum-based High-Q Cold RF Resonators for ADMX
Katsuya Yonehara
ADMX RF resonator workshop at LLNL
24-28th August, 2015

## Slide 2: Attractive metal, high-purity Aluminum
Improved aluminum refining techniques now provide high-quality, cost effective high-purity aluminum samples
High-purity aluminum shows extremely low electric resistivity at low temperatures in strong magnetic fields
High energy physics opportunities now at hand motivate a targeted R&D program to fabricate and evaluate resonating cavities using very high purity aluminum at low temperatures in strong magnetic fields
  Axion detector resonator

## Slide 3: DC electric resistivity of Aluminum and Copper
• Resistivity of 5N-Al is one order of magnitude smaller than 5N-Cu
• 6N7-Al is available as a commercial product that shows two orders of magnitude lower resistivity than 5N-Cu
• Al cost about half from the same
purity Cu
5N = 99.999 %
6N7 = 99.99997 %
Al ingot purified through
ultra-high vacuum melting
H. Hoshikawa et al., “Refining Technology and Low Temperature
Properties for High Purity Aluminum”, R&D report, Sumitomo Kagaku
Vol. 2013.

## Slide 4: DC electric resistivity of Al and Cu in strong magnetic fields
• Resistivity of copper increases quadratic as a function of external magnetic field strength
• It is called magneto-resistivity
• Magneto-resistivity of aluminum is saturated in a strong magnetic field
H. Hoshikawa et al., “Refining Technology and Low Temperature
Properties for High Purity Aluminum”, R&D report, Sumitomo Kagaku
Vol. 2013.

## Slide 5: AC electric resistivity of Al and Cu
• This is only experimental result I found
• 1/t (∝ resistivity in Drude theory) of Cu significantly increases (take a part from the DC measurement) at low temperature which shows an anomalous skin effect
• While 1/t is a constant (close to the DC measurement) in Al conductor
D. Movshovitz et al., Phys. Rev. B41, 10503, 1990

## Slide 6: Electron conductivity model
• Most characteristics of metal is represented
by Fermi surface (k-space)
• Cu has one conductive electron while Al has
three
• Since the Fermi surface of Cu is close to
a sphere some properties can be estimated
analytically
Example: surface resistivity of Cu conductor
Assume DC resistivity = 6.6 nW

## Slide 7: Theoretical investigation of conductivity in Aluminum
Meshed second-zone Fermi surface
Meshed second- and third-zone Fermi surface in computer simulation
• Electron conductivity of Al is more complicate
• Relaxation rate due to an electron-phonon interaction
Scattering amp
Density function
Relaxation rate in second
zone Fermi surface
Relaxation rate in third
zone Fermi surface
• Model shows qualitative agreement with experiment
D.P. Love et al., Phys. Rev. B26, 5577, 1982

## Slide 8: Thermal conductivity of Aluminum and Copper
• 6N-Al shows the highest thermal conductivity
• Kink point at 1.2 K is because Al becomes superconducting
• Thermal conductivity of copper will be worse in stronger magnetic fields according to the Wiedemann-Franz law
A.L. Woodcraft, Cryogenics 45(9) 626-636, 2005

## Slide 9: High-Q cold RF resonator for ADMX
The present ADMX resonator is made of copper. It operates at 100 mK in an 8-Tesla solenoid field with resonant frequencies 0.5-2 GHz. Because the magneto-resistivity and the anomalous skin effect are prominent in the copper resonator, the available Q-factor is <105.
If the AC resistivity of high-purity aluminum in strong magnetic fields is kept as low as previous measurements imply, the Q-factor could be an order of magnitude higher than the copper resonator, resulting in an order of magnitude reduction in the integration time required to detect the axion signal.

## Slide 10: Proposed 3-yrs project for studying of material properties of high-purity aluminum
DC electric resistivity and thermal conductivity test
AC electric resistivity test
Prototype High-Q cold RF resonator
Time table (3 year plan)
Dark blue: Preparation
Orange: Cold test
Light blue: Contingency

## Slide 11: DC electric resistivity and thermal conductivity tests
DC electric resistivity measurements are required to check the sample quality and to use
the result for theoretical investigations of electron conductivity compared with the AC result
Teslatron
(0-14 Tesla)
Inserts for DC resistivity test
(300 – 1.9 Kelvin)
Instruments
(nano-voltmeter,
low jitter current source,
temperature sensor)
High-field cold facility in Technical Division at Fermilab

## Slide 12: AC electric resistivity
SCM-1
(0-20 Tesla
300-0.01 Kelvin)
• Preliminary AC electric resistivity measurement will be done in Teslatron at Fermilab
• In order to meet the ADMX operation parameter, other AC electric resistivity measurement will be carried out at the National High Magnetic Field Lab in Florida
• A compact resonator will be made
• Above pictures are a superconducting 1.86 GHz Coplanar Waveguide Resonator
• Size of resonator part is only a few mm

## Slide 13: Make prototype cold RF resonator
Make a prototype resonator in which the resonant frequency can be 2 GHz – 20 GHz
Demonstrate feasibility of a large volume high-Q resonator
  Develop surface treatment technologies including with metallic coat, SRF surface polishing, and annealing processes
Test will be done at NHMFL and/or Mucool Test Area
Radial size of pillbox cavity

## Slide 14: Require systematic investigation of surface condition
• Surface condition is particularly important to reduce the
surface resistivity (when the mfp of electron is longer than
surface roughness)
Randomly scattered from surface
Conductor surface
Incident electron
• Control roughness
- Make smooth by annealing at 773 K (melting point of Al 993 K)
- Electro-polishing, chemical rinsing, etc
• Thickness

## Slide 15: Two possible ways to fabricate Al-based resonator
Use a thin aluminum sheet and form a resonator shape
Make a thin aluminum film by vacuum deposition

## Slide 16: Fabricate Al-base RF resonator by using SRF technique
Conceive manufacturing as for SRF cavities, i.e. using deep-drawing to produce half cells
Tune half cell by trimming equator
Join half cells by EBW
Or, since high purity aluminum is soft (like gold) we can apply metal spinning formation
→ Advantage for seamless shape

## Slide 17: Vacuum Deposition Thin Film Coatings Facility at Lab 7
Thin Film Coating Facility in Particle Physics Department in Lab 7 at Fermilab
Available thickness will be limited

## Slide 18: Possible applications by using high-purity Al resonators
Accelerator cavity
  High Secondary Emission Yield (SEY) induces a multipactoring in the resonator
  It sucks up a huge RF power
  Multipactoring may prevent by a thin-film-coating or putting buffer gas in the resonator
Stabilizer for SC magnet
Substrate for SRF
Quantum electric circuit

## Slide 19: Summary
Propose high-purity aluminum resonator
  High-purity aluminum has excellent property, particularly at low temperatures in strong magnetic fields
    May be the best material for the axion detector resonator
  There are many uncertainties to design for the resonator
  Propose 3-yr project to find out material properties of high-purity aluminum
Look for more collaborators