## Slide 1: Superconducting Microresonators and Detectors
Jonas Zmuidzinas
Caltech

## Slide 2: 2001: CPW Microresonators
Mazin et al 2001, Proc. LTD Workshop, AIP

## Slide 3: 2004: CPW Microresonators and Qubits

## Slide 4: Resonator geometries
Readout
line
Coplanar
Waveguide
(CPW)
Transmission-
Line resonator
Lumped-element
resonator

## Slide 5: Equivalent Circuits

## Slide 6: Single-channel analog readout
Resonator frequency, Q monitored at ~100 kHz sampling rate
Readout point

## Slide 7: Current distribution in CPW

## Slide 8: Conformal mapping
Matlab package: Schwarz-Christoffel toolbox
See J. Gao PhD thesis, Caltech, 2008

## Slide 9: Electrical Conductivity
scattering
time
Current density
Ohm’s law – definition of s
Conductivity
Superconductor:
Newton’s
2nd law

## Slide 10: Two-fluid model
``superconducting electrons’’:
``normal electrons’’:
Superconducting + normal:

## Slide 11
``BCS theory’’
1972 Nobel prize
e-
e-
``superconducting electrons’’ =
electron pairs

## Slide 12: Surface impedance vs frequency (Mattis-Bardeen calculation)
gap frequency:
onset of pair breaking
kinetic inductance
inductor
resistor
Rs determined by nqp(T, Po)

## Slide 13: Pair breaking by photons
Pair breaking occurs when:
Pair breaking does not occur at microwave frequencies
Pair breaking does occur at infrared/visible frequencies

## Slide 14: Kinetic Inductance Detectors
Inductor (L) + capacitor (C) = RF resonator
TiN inductor is also the optical absorber
High resistivity: rTiN ~ 500 rAl (at 10 K)
High absorption efficiency
TiN absorber used in Herschel/PACS bolometers
Resonator frequency shifts down as submm radiation is applied
1 mm
Variable-temperature blackbody
in
out
Cardiff ``LEKID’’ pixel
TiN film (gold) on Si substrate (green)
MKID = Microwave Kinetic Inductance Detector

## Slide 15: Kinetic inductance per unit length
KI per unit length
Cases where t > leff
Need current distribution
Use EM simulation, e.g. Sonnet

## Slide 16: Surface quality factor

## Slide 17: CPW vs. microstrip lines
microstrip
CPW
Crystalline dielectric (e.g., silicon substrate)
or deposited amorphous dielectric (e.g., SiO2)
Kinetic inductance fraction: a ~ 2 l / h

## Slide 18: Early 2000: first resonator tests
A. Vayonakis

## Slide 19: 2001: CPW Microresonators
Mazin et al 2001, Proc. LTD Workshop, AIP

## Slide 20: 1999: mm-wave loss in superconducting microstrip
Loss: 0.5% per wavelength
Credit: A. Vayonakis
(11.4 mm long)

## Slide 21: 2010: BICEP2 Focal Plane
Focal plane: 2 x 2 mosaic of tiles
1 tile: 8 x 8 array of dual-polarization pixels
Each 8 x 8 mm2 pixel contains :
  Dual-pol phased-array slot antenna
  Bandpass filter + TES bolometer (2 ea)

## Slide 22: 2005: Loss due to TLS in amorphous dielectrics

## Slide 23: 2008: TLS surface layer for CPW resonators
Gao et al. 2008

## Slide 24: Resonator noise
Day et al 2003; Gao et al 2007, 2008; Zmuidzinas 2012

## Slide 25: 2008: Capacitor (TLS) Noise
Gao et al 2007;
Noroozian et al 2010
Kumar et al 2008
Gao et al 2007

## Slide 26: 2014: Resonator noise & dephasing

## Slide 27
Heike Kamerlingh Onnes
University of Leiden
1908: liquid helium
1911: superconductivity
1913: Nobel prize
(1963)
Electrical resistance (W)
Temperature (K)
1911: Discovery of superconductivity

## Slide 28
Andrews et al 1946

## Slide 29: SCUBA 2 with 10,000 pixels 42x30 = 1280 pixels per tile
Voltage-biased TES: Irwin 1995
SQUID TDM mux: Chervenak et al 1999

## Slide 30: 1999: In search of a better detector
Individually, TES and SQUIDs are elegant, but…
TES bolometers are complex
SQUID multiplexers are very complex
  Superconducting ICs with ~12 lithography layers
TES x SQUID mux = very x (complex)2
  Expensive
TES & SQUID not integrated
  Each TES needs superconducting connection to SQUID mux
  Labor-intensive, or complex (e.g. bump bonding)
Is there an easier way ??

## Slide 31
1999 – 2013: MKID
(Microwave Kinetic Inductance Detector)

## Slide 32: Pair-breaking and recombination
Submm photons (hn > 2D) break superconducting Cooper electron pairs into individual electrons or ``quasiparticles’’
  Photon energy is not converted to heat immediately as in a bolometer
  Quasiparticles rapidly relax to gap edge via phonon emission
Barends et al 2010
Quasiparticles subsequently recombine on timescale tqp ~ 10-100 ms by emitting a 2D phonon into the substrate
  tqp plays role of bolometer thermal time constant
Kinetic inductance depends on Cooper pair density
AC resistance depends on quasiparticle density

## Slide 33: Frequency multiplexing

## Slide 34: Frequency multiplexing (18 x 24 = 432 pixels)
RF In
RF Out
(to cryo amp)
Fabrication - Rick Leduc at JPL

## Slide 35: Frequency multiplexing (18 x 24 = 432 pixels)
Fabrication - Rick Leduc at JPL
RF In
RF Out
(to cryo amp)

## Slide 36: Frequency sweep
Low readout frequency (200 MHz) enabled by use of TiN (large rn  large Lk)
Resonator frequencies span 185-250 MHz (65 MHz bandwidth or 0.43 octaves)
415/432 resonators deeper than 6 dB (96% yield)
160 kHz average spacing

## Slide 37: Resonator Q sets mux density
High Qr  low collision probability
  Do not rely on precise placement of resonator frequencies (sf)
  Collision probability independent of sf for high mux density
Need Qr ~ 105 to multiplex 500-1000 pixels/octave
Previous slide: 432 pixels / 0.43 octave = 994 pixels/octave @ 96% yield
pixels/octave

## Slide 38: MAKO: a prototype camera (Swenson et al, SPIE Proc., 2012)

## Slide 39: MAKO goes to the CSO
CSO: a 10.4m Leighton dish on Mauna Kea, HI

## Slide 40
MAKO goes to the CSO
G34.3
SgB2

## Slide 41: Multichannel Digital Readout
FPGA implements digital channelizer for readout tone separation
Microwave (GHz) readout requires up/down frequency conversion
RF readout (< 500 MHz) allows ``direct drive’’ with ADC/DAC
  Reduces readout bandwidth, complexity, and cost
  Converters are typically 12-bit, 500 MSPS (ADC < $200 ea)
  Use frequency readout since
Microwave readout
RF readout
L. Swenson, LTD-15 2013

## Slide 42: Readout Electronics
Use fast DAC to generate multifrequency readout signal, send to cryostat
Digitize returning signal (200-500 MSPS)
Perform FFT in real time (FPGA/GPU)
Select FFT channels corresponding to readout carriers
Stream to disk
ROACH 2 + custom ADC, DAC
1U server + GPU + PCIe ADC/DAC

## Slide 43: Readout Electronics
10 MHz rubidium standard & 1 PPS Signal (from GPS antenna)
Amp Bias
Roach Clock (500 MSPS)
ROACH
10 MHz standard, Clock, and Amp bias can be shared by multiple ROACH readouts
1 ROACH can handle 2 readout lines, up to 4000 detectors
MAKO/ROACH firmware developed by Ryan Monroe, CIT/JPL

## Slide 44: KID/MKID projects
INSTITUTIONS | PROJECT | DESCRIPTION
MPIfR Bonn, SRON, TU Delft | A-MKID | 20 kpixel submm camera for APEX (R. Gusten)
IRAM, Neel Institute, Cardiff | NIKA2 | 5 kpixel mm camera for IRAM 30m (A. Monfardini)
UCSB, JPL | ARCONS | 2 kpixel optical camera for Palomar (B. Mazin)
Penn, NIST | BLAST upgrade | 1000 pixel, dual-pol focal plane for balloon-borne far-IR polarimetry. PI: M. Devlin
Cardiff, SRON, TU Delft, Neel Institute Grenoble, Centro de Astrobiologia (Spain), AimValley, QMC Instruments | spaceKIDS http://www.spacekids.eu/ | EU FP7 project. Development of MKID arrays for space applications. PI: Matt Griffin
Argonne National Lab | http://www.aps.anl.gov | Detectors for use with ALS synchrotron
Fermilab | http://www.fnal.gov | 100 kpixel optical MKID camera for Dark Energy
NAOJ, U. Tokyo, U. Tsukuba, U. Saitama | http://atc.mtk.nao.ac.jp | CMB polarimetry: GroundBIRD, LITEBIRD
Columbia U. | SKIP http://arxiv.org/abs/1308.0235 | Balloon-borne CMB polarimetry. PI: A. Miller
Penn, JPL | ICarIS | Balloon-borne far-IR spectroscopy. PI: J. Aguirre

## Slide 45: TiN MKIDs for energy-resolved single photon imaging
B. Mazin
UCSB

## Slide 46: ARCONS MKIDs
2024 (44x46) pixel array
222 micron pixel pitch
2 feedlines
2 MHz resonator spacing
~92% resonator yield
~70% “good” pixel yield
  Frequency collisions dominate yield!
  More uniform TiN (multilayer, ALD, new materials) should significantly improve yield
110 mK operating temp.
Mazin et al. 2012, Optics Express, 20, 2

## Slide 47: 10 kpix DARKNESS Array
Funded to build 3 10-20 kpix instruments
DARKNESS for Palomar (NSF): 2016A
MEC for Subaru (Japan): 2016B
PICTURE-C Balloon (NASA): 2019
This is the highest pixel count LTD array ever made.

## Slide 48: Flex cables
NbTi flex cables using G3PO connectors for high density, low head load cables. Blind-mate with LNF 4-8 GHz HEMTs.
Copper G3PO flex cables for 300 K to 4K

## Slide 49: Resonator Design
We use a square microlens array to improve effective fill factor to ~92%

## Slide 50: Layout Details
Multiple feedlines require good ground planes
  Don’t use high KI materials for ground planes or feedlines!
  You must have crossovers!
Getting heat of the chip is a big concern
  Use gold bond pads and gold wire bonds
Long, narrow feedlines are a yield problem
  Carefully design and debug the fab process
Notes: Note: Present a non-proprietary technical presentation on the technology selected to be of interest by the audience (Heliophysics and Astrophysics). Keep in mind your total presentation should be no more than 20 minutes allowing an additional 10 minutes for Q&A.
Suggested talking points:
  Understanding of alignment with NASA mission(s)
  Commercialization or government infusion plans/goals
  Compare your technology to others in the marketplace or currently under development
  Business alliances/partnerships and/or synergy with NASA, Industry, academia, and other government agencies.

## Slide 51
THz Superconducting Imaging Array (TeSIA) Developed for DATE5 Telescope
DATE5: 5m THz telescope
wavelength: 350/200um
instruments:
SIS/HEB receivers & TeSIA
TeSIA:
wavelength: 350um
detector: 32x32 MKIDs/TES
NEP: 1e-16W/Hz0.5

## Slide 52
NIKA selected science result: first polarised light
NIKA2 is ready for installation
Bi-layer LEKIDs for < 100 GHz
I, Q, U maps of the Crab Nebula at 150 GHz
A. Catalano et al., arXiv:1504.00281, A&A, in press
NEP  10-17 W/Hz0.5
Arrays and
beams-map

## Slide 53
Credit: J. Baselmans, SRON

## Slide 54
4 x 880 = 3520 pixels @ 350 GHz
4 x 5400 = 21600 pixels @ 850 GHz
Total = 25120 pixels
Credit: J. Baselmans, SRON

## Slide 55
Credit: J. Baselmans, SRON

## Slide 56
Hubmayr et al. 2014

## Slide 57: Horn-coupled KIDs for CMB polarization McKarrick et al., Rev. Sci. Instrum. 2014, submitted
seven modules = 2317 single-polarization detectors
Prototype 150 GHz Module
Credit: B. Johnson, Columbia U.

## Slide 58: LITEBIRD: a Proposed CMB Satellite
2780 MKIDs
55 – 330 GHz

## Slide 59
Credit: J. Baselmans, SRON

## Slide 60: Photon Noise
NIST detectors
Hubmayr, et al.
SRON
A-MKID detectors

## Slide 61: Photon bunching
Superspec, Hailey-Dunsheath, et al.
150 GHz, Columbia, Flanigan, et al.

## Slide 62: Quasiparticle Production Efficiency
Absorption efficiency vs frequency
Conversion efficiency of photon energy to quasiparticles
SRON/Cambridge
SRON/Cambridge, deVisser, et al.

## Slide 63: Microwave generation of quasiparticles
P. De Visser
PhD thesis
TU Delft
2014

## Slide 64: Nonequilibrium superconductivity:
Calculations:
S. Withington & D. Goldie
U. Cambridge

## Slide 65: Nonlinear Kinetic Inductance of TiN and NbTiN
P. K. Day et al 2011

## Slide 66: TiN/NbTiN “fiber” paramp (Eom et al., Nature Physics, 2012)

## Slide 67: Credits
Pete Barry
Matt Bradford
Goutam Chattopadhyay
Saptarshi Chaudhuri
Peter Day
Ran Duan
Darren Dowell
Byeong Ho Eom
Jiansong Gao
Sunil Golwala
Matt Hollister
Warren Holmes
Attila Kovacs
Rick Leduc
James Lamb
Nuria Llombart
Phil Mausokopf
Ben Mazin
Chris McKenney
David Moore
Ryan Monroe
Tony Mroczkowski
Omid Noroozian
Hien Nguyen
Steve Padin
Keith Schwab
Erik Shirokoff
Loren Swenson
Rebecca Wernis
Emma Wollman
David Woody

## Slide 68: Bibliography
Zmuidzinas J. “Superconducting Microresonators: Physics and Applications”, Annu. Rev. Condensed Matter Phys. 2012 3:169-214 (2012)
Barends R., et al. “Quasiparticle Relaxation in Optically Excited High-Q Superconducting Resonators”, Phys. Rev. Lett. 100:257002 (2008)
Doyle S, et al. “Lumped element Kinetic Inductance Detectors”, J. Low Temp. Phys. 151 530-36 (2008)
Noroozian O, et al., “Crosstalk Reduction for Superconducting Microwave Resonator Arrays”, IEEE Trans. Microwave Theory Tech. 60 1235-1243 (2012)
Swenson L., et al. “Operation of a titanium nitride superconducting microresonator detector in the nonlinear regime”, J. Appl Phys. 113 104501 (2013)
McKenney C, et al. “Design considerations for a background limited 350 micron pixel array using lumped element superconducting microresonators”, Proc. SPIE 8452 84520S (2012)
Swenson L, et al. “MAKO: A pathfinder instrument for on-sky demonstration of low cost 350 micron imaging arrays”, Proc. SPIE 8452 (2012)
Swenson L, et al. “The Status of MAKO”, Proceedings of LTD-15 (2013)
McKenney C, et al. “Lumped element kinetic inductance detectors: Pixel design for large scale far infrared arrays”, Proceedings of LTD-15 (2013)

## Slide 69: More details…