## Slide 1: Fabrication of Interlayer Glass for Long Coils
Steve Krave
19 August 2015

## Slide 2: Method
Current coils use single length ~12” wide of 2-layer S2 glass with holes cut for pins and holes.
Laser only cuts 3.70m in one pass
  Worked well for LHQ
2 cuts work OK, but alignment by eyeball
Twice as much potential for error (switching programs, warping fabric, more handling of insulation etc…)

## Slide 3
No Slits (Ideal)
1 slit (QXFP1b, LHQ, QXFS)
T Slit, 2 section
Angle slit 1 section (QXFP1)
Not to scale

## Slide 4: Proposal: Fabricate interlayer insulation in 2 pieces
Pros
  Allows more efficient use of glass (3 pieces per width instead of 2)
  Allows more consistent product
    Less technician dependent
  Reduces handling
  Easier to cure (7’ section fits well on 8’ mandrel) 16’ available for longer lengths
  Significantly faster
  Significantly more efficient
Cons
Seam in middle of coil

## Slide 5: Resources Required
 | Full Length | Half Length | Units
Setup | 20 | 10 | minutes
multiples | 1 | 3 | 
Sheets | 1 | 2 | 
piece multiplier | 1 | 1.5 | 
Cut Time | 14 | 42 | minutes
Shift and align | 10 |  | minutes
Cut 2nd half | 14 |  | minutes
reset | 10 | 5 | minutes
set time | 71 | 63.5 | minutes
Total time per set | 71 | 42.3 | minutes
efficiency | 0.81 | 0.9 | 
alignment efficiency | 0.9 | 1 | 
overall part efficiency | 0.73 | 0.9 | 
efficiency adjusted | 97.39 | 47.04 | Minutes
For 90 sets | 146.09 | 70.56 | Hours
Glass Required | 624.7 | 337.3 | meters