## Slide 1: HRMT24 BeGrid Experiment Preliminary Results
Kavin Ammigan
Proton Accelerators for Science and Innovation Workshop
11-13 November, 2015

## Slide 2: Collaborating Institutions
P. Hurh
R. Zwaska
B. Hartsell
K. Ammigan
R. Losito
M. Calviani
M. Butcher
M. Guinchard
S. Roberts
V. Kuksenko
C. Densham
A. Atherton
M. Fitton
J. O’Dell
T. Davenne
P. Loveridge
O. Caretta
G. Burton
CERN HiRadMat team and support groups: A. Fabich, A. Bouvard, V. Clerc, L. Lacny, G. Vorraro, T. Lefevre, et al.

## Slide 3: Motivation and Objectives
Investigate the use of beryllium as windows and targets for future high intensity particle accelerator facilities
Help successfully design and operate these components
Experiment objectives
Explore the onset of failure modes in beryllium under controlled conditions of highly localized strain rates and temperatures
Identify thermal shock limits of different beryllium grades
Validate highly non-linear numerical models with experimental measurements

## Slide 4: CERN’s HiRadMat Facility
‘single-shot’ experiments with 1016 POT/year limit

## Slide 5: Experimental Set-up
Experiment chamber
BPKG/BTV assembly
HiRadMat mobile table
Rad-hard camera
HEPA filter
Optical path
Mirrors
beam
Vertical lift tower

## Slide 6: Test Matrix
Thin disc samples
Cylindrical ‘slugs’ samples
Specimen types
Gafchromic foils

## Slide 7: Numerical Simulations
Beam σ = 0.3 mm chosen to push beryllium to just below its melting point (1290 ◦C)
Peak ΔT for max. intensity pulse ~ 1050 ◦C
Thermal shock expected due to large temperature gradient in material

## Slide 8: Instrumentation list
Physical measurements (slugs)
  Circumferential strain
  Temperature
  Radial displacement and velocity (LDV)
LDV spot
Temperature sensor
Strain gauge
Camera for online visual monitoring
Beam alignment
  Rad-hard camera for foil imaging
  BPKG/BTV

## Slide 9: Experiment Installation
BA-7 installation (08/24 – 08/31)
Experiment box assembly
Array/beam position alignment
Optical path mock-up
  HD camera and LDV
DAQ system checks
TNC installation (09/01 – 09/04)
Transport table from BA-7 to TNC
Final connections
  BPKG/BTV calibration
  Vacuum pump connections
  Finalize optical path alignment
Beam time (09/17 – 09/18)

## Slide 10: Experimental Beam Parameters
No wire scans on Pulses 8 – 11. Emittance estimated by averaging emittances of Pulses 4-7
Average bunch intensity: 1.3 x 1011 ppb
σx : 0.268 – 0.306 mm
σy : 0.202 – 0.307 mm
Total protons on target: 1.8 x 1014

## Slide 11: Beam Spot Position
Pulse 11: shift in BPKG baseline observed (need confirmation of data)
x-position: -0.47 to -0.07 mm
y-position: -0.02 to 0.12 mm

## Slide 12: Preliminary Results
Array 3 slugs
24 bunches
3.196 x 1012 POT
No residual plastic strain upon cool-down

## Slide 13: Preliminary Results
Array 2.1 slugs
36 bunches
4.722 x 1012 POT
Some residual plastic strain

## Slide 14: Preliminary Results
Array 4 slugs
216 bunches
2.792 x 1013 POT
Significant residual plastic strain

## Slide 15: Next steps
Test rig disassembly
Be contamination check (filter inspection)
Disassemble experimental box
Pack individual array boxes accordingly based on gamma spectroscopy results
Ship to Oxford University for PIE
Post-experiment pictures
Post-irradiation activities
Thin disc specimen PIE
  Microstructural analyses
Benchmark numerical simulations and material strength models with experimental measurements

## Slide 16: Post-Irradiation Examination
EDX spectroscopy
EBSD
Profilometry
FIB
PIE of thin disc specimens at University of Oxford
Elemental analysis of the different Be grades
Measurement of out-of-plane deformation
Localized deformation and crack analysis
3D analysis of crack morphology

## Slide 17: Conclusions
Completed experiment successfully and safely
  No unforeseen or catastrophic events
  However…
    Large variations in beam sigma on target
    Array 4 did not receive the desired high intensity pulse
    Noisy LDV data due to faint signal from Be slug surface
    Gafchromic films exposed quicker than expected
      Offline analysis needed
Bulk of results will come from PIE work planned for next year
  Insight on thermal shock response of the different Be grades
  Findings will drive possible follow-up experiment (BeGrid2)