## Slide 1
Radiation Effects in Beryllium: recent results from the NuMI beam window material
Slava Kuksenko1 C. Densham2, P. Hurh3, S. Roberts1
1 University of Oxford, UK
2 Rutherford Appleton Laboratory, UK
3 Fermi National Accelerator Laboratory, USA
Many thanks to
Steven Van Boxel, Alex Cackett and Chris Hardie (CCFE)
K. Ammigan and B. Hartsell (FNAL)
PASI workshop. 12 November 2015, Fermi National Accelerator Laboratory

## Slide 2
Beryllium
is extensively used as a material of neutrino targets parts, for example – beam window
is a promising candidate for future high-power neutrino sources
Application | Operating conditions |  |  |  |  | Proton beam parameters
 | Avg. T (°C) | Peak T (°C) | Total DPA | Gas production (appm/DPA) |  | 
 |  |  |  | He | H | 
Beam window (vacuum to air) | 200 | 300 | ~ 0.23/yr | >2000 | >2000 | 700 kW; 120 GeV; ~1 Hz; σrms = 1.3 mm
Target | 375 | 450 | ~ 0.23/yr | >2000 | >2000 | 700 kW; 120 GeV; ~1 Hz; σrms = 1.3 mm
For example, the expected working conditions for some parts of the Long-Baseline Neutrino Facility (LBNF)
Environment: elevated temperature + radiation + pulsing loads
Compressive fracture or yield strength as a function of fluence (E > 1 MeV) for beryllium specimens irradiated at 75-125°C.
D.S. Gelles rt ul. /Journal of Nuclear Materials 212-2I5 (1994) 29-3X
Examples form n-irradiation - reduction induced embrittlement - irradiation induced hardening
What can we expect?

## Slide 3
Investigation of the as-received Be
Investigation of the proton Be window (NuMI)
Ion irradiation experiments
Thermal shock experiments
Experimental investigation

## Slide 4
 | Max impurities, appm
Al | 170
C | 450
Fe | 130
Mg | 810
O | 2900
Si | 130
N | 195
Be | balance
PF-60
Method of manufacture: vacuum hot pressing and cross-rolling
Beryllium is of industrial purity
Materials
50 µm
PF-60 (VHP), rectangular sample. 5mm× 5mm 1mm
50 µm
PF-60, cross-rolled disk sample
Ø15mm x 0.75mm
Industrial beryllium is a non-homogeneous material.
“White contrast particles” on SEM images (in the SE2 detector) decorate GB-s

## Slide 5
60 µm
60 µm
60 µm
PF-60, VHP rectangular sample
5mm× 5mm 1mm
PF-60, cross-rolled disk sample
Ø15mm x 0.75mm
Average diameter – 25 ± 14 µm
Average diameter – 9 ± 4 µm
2 different states of the PF-60 are investigated: (a) VHP and (b) cross-rolled
2 grades are very different grain size
PF-60: Microstructure in the as-received state: VHP vs Cross-rolled

## Slide 6
60 µm
60 µm
PF-60, rectangular sample
5mm× 5mm 1mm
PF-60, disk sample
Ø15mm x 0.75mm
No texture (macroscopically – isotropic)
Strong (0001) texture
PF-60: Microstructure in the as-received state: VHP vs Cross-rolled

## Slide 7
PF-60, disk sample
Ø15mm x 0.75mm
50 µm
Oxygen
Aluminium
Silicon
Iron
Industrial beryllium is an impure alloy: relatively pure grains and strongly “alloyed” GB
Oxygen
Aluminium
Silicon
Iron
20 µm
SEM
PF-60, rectangular sample
5mm× 5mm 1mm
SEM
PF-60: Microstructure in the as-received state: impurities distribution

## Slide 8
Preparation of samples for fine scale investigations
FIB lift out
APT sample
FIB lift-out
investigation of localized microstructure and properties
minimize activity of samples
minimize toxicity of samples
TEM sample
Culham Materials
Research Facility

## Slide 9
Industrial beryllium: GB – decorated by BeO(+Si) and Fe segregation

## Slide 10
Be
Fe
Ni
O
Small quantity of Fe, Cu, Ni and C are homogeneously distributed inside Be grains
, nm
, nm
PF-60 | Max impurities, appm | Impurities in Beryllium matrix (APT), appm
C | 450 | 15±10
Fe | 130 | 50±10
Ni | 31 | 25±10
Cu | 14 | 15±10
O | 2900 | ?
Al | 170 | Not detected (ND)
Mg | 810 | ND
Si | 130 | ND
N | 195 | ND
Preparation of samples for fine scale investigations

## Slide 11
Fe
Fe segregates to dislocation lines
No evidence of other elements segregations
Possible consequences:
Cottrell-type solute pinning?
Yield Point ?
Isosurface CFe=500 appm

## Slide 12
Microstructural response:
creation of transmutation products;
creation and agglomeration of point defects;
segregation (precipitation) or depletion on point defect sinks
What can we expect during irradiation?
Possible irradiation effects:
reduction induced embrittlement
irradiation induced hardening
swelling
reduction of thermal conductivity

## Slide 13
300 kW NuMI beam window
(MARS calculations of Brian Hartsell, Fermilab)
120GeV proton beam
about 3×1013 protons per pulse, 0.5 Hz
1.57×1021 protons during its lifetime
1.1mm beam sigmas, X and Y
T ≈ 50ºC
NuMI beam window experiments
Dosimetry film, 5 days of exposure
19 mm
Large difference of dpa and transmutants production is likely to produce non-homogeneous changes across the surface of Be window.
dpa

## Slide 14
Surface contamination:
Ni - comes from plating?
Ca, S, Cl, C – drips of drainage water?
O
Oxide layer thickness is about 75 nm

## Slide 15
0 dpa
0.3 dpa
9Be++
9Be+
(9Be+H) +
12C+
16O+
(16O+H)+
9Be+
9Be++
7Li+
6Li+
New peaks on mass-spectrum – transmutation products

## Slide 16
PF-60 | Max impurities, appm | Impurities in Beryllium matrix (APT), appm | Impurities in Beryllium matrix after p-irradiation 0.33 dpa (APT), appm
C | 450 | 15±10 | 245+50 (if we consider the natural abundance)
Fe | 130 | 50±10 | 50±10
Ni | 31 | 25±10 | 22±10
Cu | 14 | 15±10 | 15±10
O | 2900 | ? | ?
Al | 170 | ND* | Lithium: 420 appm
Mg | 810 | ND | Others: ~ 2400 appm
Si | 130 | ND | 
N | 195 | ND | 
Li is not soluble in Be. Will it segregate?

## Slide 17
~ 400 appm of Li
~ 460 appm of Li
Good agreement between the MARS model and APT data on Lithium production
Irradiated
As-received
Be9 +
Be9 ++
Be9 ++
Be9 +
Li7 +
Li6 +

## Slide 18
After irradiation inside grains:
Transmutant Li is homogeneously distributed
Impurities (Fe, Ni, Cu, C) are still homogeneously distributed
…but the temperature was low (50ºC), and the behaviour can be different under new working conditions (>200ºC). Ion implantation/annealing experiments are needed
Li
Be9 ++
Be9 +
Li7 +
Li6 +

## Slide 19
Radiation embrittlement?
NuMI beam window experiments
Irradiated
As-received
Irradiated

## Slide 20
FIB preparation for EBSD analysis

## Slide 21
~ 0.29dpa
~ 0.27dpa
~ 0.44dpa
EBSD

## Slide 22
Transition form transgranular fracture to grain boundary/mixed mode fracture
Non-irradiated beryllium – transgranular cleavage
Grain-boundary fracture is observed after high temperature irradiation (>500°C) due to GB decoration by He bubbles.
Grain-boundary fracture at low T the is dominated by strengthening of the matrix accompanied by losses in ductility
~ 0.29dpa
~ 0.44dpa

## Slide 23
1 µm
~ 0.45dpa
NuMI beam window experiments: TEM

## Slide 24
~ 0.45dpa
Some grains of beryllium are strongly deformed and full of dislocation and SGB:
cross-rolling?
Deformation during post-irradiation handling?

## Slide 25
“black dots” are visible for certain “gb” contrast conditions;
they remind contrast from defect clusters after neutron irradiation, thus, they may be irradiation damage;
We didn’t find void/bubbles – where are He and H?
~ 0.45dpa

## Slide 26
Swelling?
High swelling at low T?
But we have “only” about 2000 appm of He
We cannot confirm this now after our first TEM experiments.
… but we have investigated only few surface grains
Irr. Be, TEM, BF, He bubbles, Tirr.=413 °С, F = 6.5×1021 сm−2 (Е > 1 MeV) (Klimenkov et al. JNM 2013)

## Slide 27
Interesting behaviour of single located BeO – Al and Si shell. Al-Si eutectic is a low melting point phase
RIS is often observed, for example, in steels,
… but, we have no confirmation that this is radiation induced effect.
~ 0.45dpa

## Slide 28
Transgranular fracture
GB/mixed fracture?
Transmutant Li can be one of the reasons of properties degradation under proton irradiation
But detailed TEM and He/H transmutants distribution analysis is needed
Micromechanical tests should be made

## Slide 29
Beryllium is highly non-homogeneous at macroscale and highly anisotropic material.
Industrial beryllium is an impure alloy: relatively pure grains and strongly “alloyed” GB
Impurities strongly create GB precipitates and segregations, segregate to BeO and dislocations
Beryllium matrix has some quantity of homogeneously distributed carbon, iron, nickel and cupper
Proton irradiation cause Li production, which is homogeneously distributed (T=50°C)
Signs of irradiator induced embrittlement and change in fracture mode (from intra- to inter-granular) under high energy proton irradiation
Conclusions
20 µm

## Slide 30
The scattering makes sense… but the anisotropy is impressive
EBSD map
Nanoindentation
PLANS
Repeat at higher T up to 500˚C
Repeat after ion irradiation
Compare with the NuMI beam window

## Slide 31
0.3mm
Beam Thickness 2um
Stress (Pa)
Strain
Fe 6%Cr
Chris Hardie University of Oxford
Why use micro-cantilever testing?
PLANS
D. Armstrong/ University of Oxford

## Slide 32
MIAMI irradiation – try to mimic the irradiation effects with ions
Focus: - 461 nm
Focus: +461 nm
Size: up to 1…2 nm
ND ~ 5·1023…1·1024 m-3
PLANS
Ions: He+
Beam energy: ~ 18keV
Mean He/dpa = 4000
1.5 dpa

## Slide 33
Surrey Ion Beam Centre, UK
(collaboration with Prof. R.Gwilliam)
APT sample
Pt
Pre-tip
Ions: He+
Maximum beam energy: 2 MeV => 7.5µm implantation depth (SRIM)
Dose: up to 1 dpa
Temperature: 50ºC and 200ºC
TEM sample
8 × 8 µm3
He implantation experiments
Micromechanical
tests
~ 300 appm(He)/dpa

## Slide 34
0 dpa
He irradiation, 6000 appm of He, 1.5 dpa
0 dpa
He implantation, 1.5 dpa

## Slide 35: Thank you for your attention!