## Slide 1: Horizontal Testing During LCLS-II Production
D. Gonnella, J. Ozelis
October 29, 2015

## Slide 2: Outline
Goals/scope/reasons for HTS testing
Test rate
System performance parameter measurement
Test procedures/configuration options
Or in other words – Why, What, How.
As we propose – subject to discussion!

## Slide 3: Goals for HTS testing
Has two primary goals distinct from vertical test (cavity qualification) and CM test (cryomodule qualification for linac):
  Are the processes, procedures, tooling, and staffing yielding the required performance of the combined SYSTEM when assembled from qualified individual components
  Are the vendor-supplied components conforming (or still conforming) to required performance specifications when used/operated under conditions similar to those encountered during cryomodule operation (and which cannot be duplicated “on the bench”).
Evaluates reproducibility and effectiveness of preparation and assembly procedures and processes
Provides QA/QC of vendor supplied components in a manner not available from “bench tests”

## Slide 4: Goals for HTS testing
Limited evaluation of cavity and it’s auxiliary systems under CM-like operational conditions
  Coupler operation
    heating, multipacting, vacuum level, Qext range & nominal setting
  HOM
    temperatures and notch filter setting/fundamental rejection
  Tuner
    range, hysteresis, dead-zone, freq offset
  Cavity performance
    FE onset/levels, operating gradient (admin limited), meet Q0 spec @ E spec

## Slide 5: Goals for HTS testing
We should remain cognizant of the costs associated with HTS testing (manpower, M&S, schedule impact) and limit testing to
  information that can not be obtained any other way (bench tests, CM tests, VTS)
  information that is needed (not just “interesting”) to meet testing objectives

## Slide 6: Goals for HTS testing
An established HTS test program also provides two other ancillary benefits, that can contribute to risk-mitigation strategies:
  A ready means for investigating performance issues that arise from early CM testing, that require an iterative approach or evaluation in a CM-like environment of design/component changes during production
  Use of HTFs at partner labs can provide a means for long-term stability or lifetimes tests of crucial systems (tuner, LLRF, FPC) that can not be evaluated by other means.
  For now, long term-testing for lifetime/stability studies of systems (tuners, LLRF, FPC, etc.) are not in the scope of this discussion as far as deciding upon a common set of data/parameters to measure, as resources for that are not in the baseline.
    Discussion of the viability and necessity for long-term studies should nevertheless take place.

## Slide 7: HTS Test Rate – As Baselined
Nominally 1 cavity per 2 cryomodules (16 production CMs)
  1 in 16 cavities/8 of 128 cavities
  1 month per test (3 weeks minimum?)
    One cavity per CM initially ?
Test duration of 8 months
  Could be extended to more closely align w/CM production rate
Consider “front loading” the P6 schedule/plan with HTS tests to better evaluate consistency of assembly procedures & processes, and component fit-up in early stage of vendor’s production run
  Eliminate HTS testing of cavities in the last 4-6 CMs.
    Maintain overall # of HTS tests
    More confidence in vendors and assembly staff/procedures in latter stages of production

## Slide 8: HTS Parameter Measurements
This is a suggested list based on test goals outlined previously.
  Does not include activities like calibration, instr checkout etc. - lets assume each lab will perform tests based on local “best practices” and established procedures
Pre-test parameters
  Cavity vacuum
  Coupler vacuum
  Cavity passband frequencies (use tuner to set to f0)
  Cavity HOM notch frequencies
  Coupler Qext’s (FPC (base and range?), antenna, HOM 1&2)

## Slide 9: HTS Parameter Measurements
Gradient-based parameters
  Maximum gradient reached (limited to admin limit of ??)
    Nature of limit (quench, thermal BD, RF limit, admin)
  Forward power at Eop, Emax
  FE onset gradient
  FE (radiation) level at Eop, Emax
    Initial and final values of the above if FE processing performed
  HOM emitted power at Eop, Emax
Q0
  Q0 at Eop
  Q0 elsewhere?
  Heat load off resonance (FPC contribution to Q0) ?

## Slide 10: HTS Parameter Measurements
Tuner parameters
  Range
  Hysteresis/dead zone
  Resolution (PZT & stepper)
  Tuner motor temperature ?
Thermal Parameters (depends upon instrumentation !)
  FPC temperature at Eop after ~6hrs
  HOM temperatures at Eop after ~6hrs

## Slide 11: HTS – Procedures, Options, Open Questions
Active pumping of cavity?
Active pumping of coupler?
Warm coupler conditioning?
Cavity fast cooldown – need to define parameters for successful cooldown
  Now we use DT (top-bottom), flux measurements
    No instrumentation in production?
    Have to use J-T valve settings, supply pressure, beampipe flux etc.
  what if cooldown not successful (what does that mean?), warmup & re-cool? (this only affects Q0 measurement)
FE – what level (@ Eop, Emax) indicates failure?
  When is processing pursued, how long? What limits on RF/gradient/duty cycle?

## Slide 12: HTS – Procedures, Options, Open Questions
Global magnetic shielding instead of individual (cavity) shielding ?
  Less of a chance of damaging local shielding if not used
    Must ensure adequacy of HTS global shield so no effect on Q0
  Plan to install shielding into HTS between pCM cavity testing and production
    Will need to verify effectiveness before eliminating local shields
Eliminate tuner ?
  Simplifies test prep, tuner needs to be removed before string assembly
  Negates one of the primary motivations for performing HTS testing during production

## Slide 13: HTS – Procedures, Options, Open Questions
Dependence of Q0 on time cold
  Observe increase in Q0 over time as end groups, support rails, etc. get colder.
  Since HTS testing is limited in time, expect Q0s will be better in CM after a few months spent @ 2K, compared to the HTS result
    Not yet quantified (pCM test is an opportunity)
  Does this imply we can/should accept a lower Q0 spec for HTS (might help improve acceptance rate)? Or is there some Q0 degradation in CM from HTS?
Q0 vs T
  Difficult (time consuming) to perform, and probably not relevant

## Slide 14: HTS – Acceptance Criteria
Some cavities will not meet required specifications for all parameters. We need to know what constitutes “failure”, and when re-work will be needed.
  Failure to meet Eop
  Failure to meet Q0 spec @ Eop
  FE too high – what is “too high”? Just effect on Q0, or effective DC, cavity fratricide?
  Failure to meet tuner range spec/cavity frequency range spec
  FPC Qext initial setting/adjustment range out of spec
  HOM Qext too low, or improper tuning
  Coupler or HOM thermal performance/thermal strapping
    What is “spec”? Temp limit? Or effect on Q0/low Q0? Will this be instrumentation dependent? Can failure be clearly attributed to the dressed cavity and e.g., not on details of thermal strapping in the HTS cryostat? Do we make allowance for 80K vs 40K shield?

## Slide 15: HTS – Documentation
HTS test documentation (results, data, procedures) will be managed by Vector @ FNAL (Pansophy @ JLab?)
  In keeping with standard practice, travelers will be used to record data, test conditions, observations, etc. and track testing activity. This includes using the NCR/Deviation functionality
  Travelers should undergo a review/approval process to ensure relevant and appropriate data are being compiled (compliance with recommendations arising from this workshop).
    Content of the test traveler should be (nearly) identical for both facilities (FNAL/JLab)
  Testing (and test prep) procedures will be controlled documents linked to the travelers. These are facility specific. Review/approval by subject matter experts to assure “best practices”.

## Slide 16: HTS – Instrumentation
Deployment of identical instrumentation, while preferable, is neither necessary nor perhaps practical.
  Existing facilities may already have sufficient and capable instrumentation that is well-understood
  Focus on making sure instrumentation matches measurement needs (type and accuracy/sensitivity/reliability)
“Final” instrumentation requirements can only be ascertained once a “final” list of measurements/parameters is developed and accepted.