## Slide 1: MICE Spectrometer Solenoid Repair

## Slide 2: MICE Spectrometer Solenoids
These magnets have had a long history and I will make NO attempt to review it in any detail here.
  Steve and Soren will fill in some of the details
Both magnets met the full specification at the vendor and were fully mapped.
  Cryogenic operation was very good. Both magnets had significant cooling headroom (SS2 more than SS1)
SS2 (in upstream position of the beam line – SSU) has reached full operating current at RAL, but full training (soak, solenoid mode) has not been completed.
SS1 (in downstream position – SSD) had a lead failure during training.
What is the optimal path forward?

## Slide 3: Reminder: Basic design
5 2-stage CCs
1 single-stage CC
5 Coils
Max current ~300A
High inductance 10-40H
M2
M1
E2
C
E1

## Slide 4: Power system

## Slide 5: Power delivery system
2 Vacuum feedthroughs bring power into vacuum space
  One for ECE, one for M1 and M2
Copper leads to HTS
  IL/A = 3.6 X 106 A/m
HTS:
  HTS-110 500A (M1, M2, C) and 250A E1 and E2
LTS:
  Vacuum feedthrough: Proprietary Wang design based on SSC superconductor
  Inside He space: Cu stabilized conductor

## Slide 6: Training SSD
SSD has been a bit problematic at RAL
  Some vacuum issues
  Lost voltage tap on LTS lead of M2 coil
In the training run of September 13th, 2015 all was going very well.
  Implementation of additional QP for the M2 lead had not yet been done, so a decision was made to ramp only M1 and ECE
  A quench occurred at ~ 260A in ECE (much higher than expected, next slide).
QP system performed as expected, nothing outwardly unusual except for the large current.

## Slide 7: Training history

## Slide 8: Lead failure
However, upon entering the hall the odor of burnt FR4/G10 was extremely strong. Strongest at He relief valve
After a great deal of analysis, it has now been determined that (see diagram on next slide):
  One leg of M1 dead short to ground. This is LTSA lead.
  LTSB lead not connected to coil (open), but connected to LTSA with ~ 2.4KOhm resistance.
  M2 coil OK.
  No damage seen anywhere else.
    However, M2 coil has 1.3 KOhm resistance to M1 (& ground)
  AC measurements show that QP on M1 not active indicating a break in the internal QP circuit. Most likely point is indicated in the figure on the next slide (x next to diodes) because there is another short to ground on this leg of the circuit.
  All other coils OK (including their QP circuit).

## Slide 9: M1 circuit after fault
Diagram of the M1 circuit. Resistance (four wire and two wire)
measurements revealed:
i) Lead A has hard short to ground,
ii) LTSB is shorted to LTSA through 2.4 kOhms and LTSB is not connected
to the M1 coil on the Lead B side.

## Slide 10: QP data – M1

## Slide 11: QP data – M1 Expanded V scale

## Slide 12: QP data – M1 Expanded V scale II

## Slide 13: Analysis
Quench initiated on ECE and initially proceeded normally
  There is no evidence that any LTS leads were involved initially
At ~ 20 sec, the internal QP for coil M1 failed
  The voltage on the coil increased rapidly and, it appears that an arc at the LTS power feed through (from vacuum to LHe volume) occurred which burned out the lead and effected M2 (the power leads for M1 and M2 utilize the same 4 pin feed through).
What caused the QP failure?

## Slide 14: Internal QP Original Wang configuration

## Slide 15: We have add previous issues

## Slide 17: LBNL re-design Picture of final configuration for SS2/SSU
Quench protection circuitry
Conductively cooled resistors

## Slide 18: SS1/SSD
This is a photo of the QP pack for SSD/SS1. What is not known at this time is
exactly how the terminations were made. Did Wang follow the procedures used on SSU/SS1?

## Slide 19: Normal Quench
These are data from a normal quench
  All coils ramping together to their design current
  NOTE: In this case, the quench occurred as the currents were ramping down
ECE initiated the quench (QP system detected and sent trigger to open contactors)
M2 followed, then M1
  As predicted.

## Slide 20: Quench delay M1 & M2

## Slide 21
Chart: Hot Spot Temperature
Chart: Hot Spot temperature
Compared the results with (case I)and without (case II) M2 powered.
Quenches were initiated in E2 in both cases.
The quench current in case I is 265A in all coils.
In case II, the quench currents in ECE and M1 are 260A and 250A, respectively.
Case I
Case II
Quench propagation analysis without M2 powered

## Slide 22: Quench delay
Time to Q for M1 increased by ~ 2X
However, overall scale in simulation does not agree with data
  There is a qualitative understanding
    LHe & gas not modeled exactly
    The thermal properties of the mandrel + insulation between coils and the bobbin are not precisely known
    The starting location of the quench will affect the heat propagation from the hot spot to the mandrel, this will cause time difference. The model is always set so that the innermost layer initiates the quench.
Given the above, there is qualitative agreement:
  The quench delay of M1 increased by ~2X, from 10 seconds to 20+ seconds.

## Slide 23: Moving Forward
Can obtain lattice to allow MICE Step IV running without SSD M1 coil. However, limits momentum scan
Harder when RF is added
  Impossible?
However, risk that a M2 lead will fail must be considered high at this point
  M2 has been powered at low current (5A) and all looked good.
Need guidance on how to proceed