## Slide 1: MICE Spectrometer Solenoid Design and Assembly

## Slide 2: Magnet Design Features
5 coils on a single mandrel
200L LHe volume in cold mass
5 ea 2-stage cryocoolers for recondensing helium vapor and cooling the shield
Vapor and return LHe pass thru the same cooler tubes at the top of the cold mass
8 ea HTS leads feed the 5 coils
60K thermal shield made from series 1100 Al

## Slide 3: Internal Design Details

## Slide 4: Internal Design Details

## Slide 5: Coil Winding Mandrel
- 6061-T6 aluminum mandrel
- Forged tube, machined profile

## Slide 6: Coil Winding
- Stycast epoxy wet coil winding
- Fiberglass cloth between layers

## Slide 7: Completed Coil Windings
- 1.65 mm x 1.0 mm superconductor
- 222 Nb-Ti filaments, ~4:1 Cu/SC ratio

## Slide 8: Banding and Axial Reinforcement
- Wound aluminum banding w/Stycast
- Welded aluminum axial stiffeners

## Slide 9: Completed Cold Mass
- Welded aluminum clamshell type cover
- ~200 liter cold mass interior volume

## Slide 10: Vacuum Side Coil Leads
- LTS leads heat sinked to cold mass body
- Commercial ceramic feedthroughs

## Slide 11: Cold Mass MLI Spacers & Heaters
- Spacers help prevent thermal shorts
- Heaters provide pressure regulation

## Slide 12: MLI Wrapped Cold Mass
- ~32 layers of aluminized Mylar MLI
- Interleaved joints, Mylar tape

## Slide 13: Cold Mass End Wrap Detail

## Slide 14: 60K Shield Assembly
- Series 1100 aluminum thermal shield
- Copper transition for cooler connection

## Slide 15: Nested Cold Mass/Shield
- Cold mass nested in shield before
installation in vacuum vessel

## Slide 16: Cold Mass Vent and Fill Lines
- Fill and vent lines intercepted at shield
- Thinned out walls limit conduction

## Slide 17: Shield Prep for MLI
- ~64 layers MLI on thermal shield
- Fiberglass cloth protects during welding

## Slide 18: Shield/Cold Mass Installation

## Slide 19: Cold Mass Alignment
- Cold mass alignment using portable CMM

## Slide 20: Cold Mass Support Bands
- Fiberglass bands for low heat leak
- Intermediate intercept at 60K shield

## Slide 21: Mounting of Cold Mass Suppts
- Support bands are pre-tensioned
during cold mass alignment

## Slide 22: 60K Support Band Intercepts

## Slide 23: Thermal Shield Support Band
- Low heat leak fiberglass bands
support weight of thermal shield

## Slide 24: Thermal Shield Bore MLI Wrap

## Slide 25: Shield End Plate Installation
- Shield end plates are welded to bore and outer tube
- Saw cuts in end plates minimize eddy currents

## Slide 26: Vacuum Vessel End Wall/Warm Bore

## Slide 27: Benchtop Cooler Tower Assembly
- Drop in arrangement simplifies cooler installation
- Some heat leak in thin walled sleeves

## Slide 28: Cooler Tower Install on Vessel

## Slide 29: Thermal Intercepts for Lower HTS Leads
- Thermal intercepts to cold mass provide
cooling for bottom end of HTS leads

## Slide 30: HTS Lead Installation
- HTS leads bolted and soldered at both ends
- Pre-installation tests ensure integrity

## Slide 31: Warm Lead Configuration
- Warm leads optimized to balance
heat leak and resistive heating
- Heat intercepted at 1st stage plate

## Slide 32: Upper HTS Lead Thermal Intercept
- Wang NMR designed double intercept
- Bypass leg provides current path

## Slide 33: Single Stage Cooler for HTS Leads
- Single stage cooler directly protects HTS leads
- 175 W of cooling power at 55K

## Slide 34: Warm Lead/Feedthru Assembly
- Ceramic feedthrus very fragile
- Technique developed for rapid replacement

## Slide 35: Power Feedthrus w/Copper Flags

## Slide 36: 1st Stage Cooler to Shield Connection
- Layered copper sheets connect coolers to shield
- Also shields cooler sleeves from direct radiation

## Slide 37: Completed Cooler Tower Assembly

## Slide 38: Completed Magnet

## Slide 39: Other Information
The two magnets shipped to RAL are virtually identical in design
SSU (1st magnet completed) performed better cryogenically than SSD
Wang NMR went thru several design iterations due to various performance deficiencies
LBNL and MICE collaborators took a lead role in the final design and assembly of the magnets