## Slide 1
Long QXF Mirror Fabrication
(MQXFPM1) Rodger Bossert HiLumi-LARP Collaboration Meeting May 18-20, 2016 SLAC

## Slide 2
QXF Mirror Design
Tests single LQXF coil in traditional Fermilab yoke with stainless steel weld-on skin.
Bolt on skin
Coil Protective Shell
Coil midplane shim
Yoke (EDM’d blocks)
Aluminum Side Clamp
Longitudinal side weld

## Slide 3
LQXF Mirror Design is derived from previous Mirrors built at Fermlab.
HFM Dipole Mirror
SQXF Mirror
LQXF Mirror
TQ mirror
HQ mirror

## Slide 4
Preload is adjusted by altering shims within the cross section.

## Slide 5
CMM Measurements Summary – Coil QXFP01a

## Slide 6
CMM measurements – Typical cross section
Average azimuthal size = -4 mils
Average radial size = -3.5 mils
One square =
100 um (4 mils)

## Slide 7: Coil Strain Gauges
Strain gauge system, standard for long mirror. There are two “stations”, located at approximately one third of the way from each end of the coil. Each station contains:
1 set of full bridges on inner titanium pole, one azimuthal bridge, one longitudinal bridge.
4 quarter bridges bonded to inside surface of inner coil, used during construction only.
Gauges bonded to coil

## Slide 8: End Preload Bolt Strain Gauges
Strain gauges bonded to end preload bolts.
Temperature Compensator
Location of temperature compensator
Location of end preload bolts
Short QXF mirror shown
End load the same as the short mirror. 2 preload bolts on each end, each applying 7 kN (1600 pounds) of force from the 50 mm thick end plate, for a total of 14 kN (3200 pounds) at each end.

## Slide 9: Shell (Skin) Strain Gauges
An array of gauges on the shell at 30 and 60 degrees from the midplane. One set of four gauges in each quadrant at each station.
Gauge at 30 degrees
Gauge at 60 degrees
Temperature Compensator

## Slide 10: Quench Antenna

## Slide 11
Assembly Steps – Planned and Actual
Press to 80 Mpa azimuthal stress in press without skin or clamps.
Actual – -74 MPa azimuthal
+171 µS longitudinal
Drive in side clamps, increasing azimuthal preload to 90 Mpa
Actual – -86 MPa
+170 µS longitudinal
Plan was to replicate the preload of the short QXF mirror.

## Slide 12
3. Remove press pressure, clamps deflect, azimuthal preload is 66 MPa.
Actual – -66 MPa azimuthal
+186 µS longitudinal
Install skin, return to press, press to azimuthal preload of 70 MPa.
Actual – -60 MPa azimuthal
+184 µS longitudinal
Weld skin and release press. Final average azimuthal coil preload of 80 MPa.
Actual – -98 MPa azimuthal
-98 µS longitudinal
Assembly Steps – Planned and Actual

## Slide 13
Coil Strain Gauge Summary
Operation | Pole Azimuthal |  | Pole Axial |  |  | Coil gauges near pole |  | Coil gauges near midplane | 
Units | MPa |  | µS |  |  | MPa |  | MPa | 
Station | 1 | 2 | 1 |  | 2 | 1 | 2 | 1 | 2
After Clamping | -61 | -70 | +255 | +116 |  | -50 | -44 | -70 | -52
After Welding | -90 | -106 | -98 | -99 |  | -87 | -83 | -129 | -116
(Station 1 is nearer the lead end and station 2 is nearer the return end. )
Note: Axial strain on MQXFPM1 is continually positive (tension) until after the welding is complete, and becomes negative after the press pressure is removed. This is typical of long mirrors. For example, the long LHQ mirror (LHQM01) axial strain readings averaged +208 uS during welding, but -125uS after releasing pressure.

## Slide 14
MQXFPM1 Fabrication Schedule

## Slide 15
MQXFPM1 Construction Pictures
Coil placed in lower yoke before end clamps

## Slide 16
During installation of upper yoke
MQXFPM1 Construction Pictures

## Slide 17
MQXFPM1 Construction Pictures
Ready to install side clamps
Side clamps installed
Side clamp installation

## Slide 18
MQXFPM1 Construction Pictures
Preparing to weld yoke

## Slide 19
MQXFPM1 Construction Pictures
End Plates welded, and installing End Preload Bolts

## Slide 20
Summary
Long mirror design is based on previous quadrupole and dipole mirrors.
MQXFPM1 is nearly complete, and should be shipped to BNL for testing in early June.
No significant manufacturing problems occurred.
Preload average at pole is 98 MPa, higher than the short QXF mirror.

## Slide 21
Backup Slides

## Slide 22
LQXF Mirror Magnetic Field at 19 kA

## Slide 23
HQ and TQ Mirror Magnetic Field (for reference)
HQM at 17 kA
TQM at 14 kA

## Slide 24
Titanium alloy
E(293K) = 130 GPa
E(4.2K) = 130 GPa
α= 1.74/(1000*293)
Steel
E(293K) = 213 GPa
E(4.2K) = 224 GPa
α= 1.97/(1000*293)
Insulation
E(293K) = 30 GPa (x)/30 GPa (y)
E(4.2K) = 30 GPa (x)/30 GPa (y)
αx= 7.06/(1000*293)
αy= 7.06/(1000*293)
Cable Composite
E(293K) = 52 GPa (r)/44 GPa (θ)
E(4.2K) = 52 GPa (r)/44 GPa (θ)
αr= 3.08/(1000*293)
αθ= 3.36/(1000*293)
St. Steel
E(293K) = 193 GPa
E(4.2K) = 210 GPa
α= 2.84/(1000*293)
AL Bronze
E(293K) = 110 GPa
E(4.2K) = 120 GPa
α= 3.12/(1000*293)
Steel
E(293K) = 213 GPa
E(4.2K) = 224 GPa
α= 1.97/(1000*293)
FEA Structural Model
St. Steel
E(293K) = 193 GPa
E(4.2K) = 210 GPa
α= 2.84/(1000*293)

## Slide 25
Radial Shim=0.1mm
Saz, Pa
300K

## Slide 26
4K
Saz, Pa
At quench current the azimuthal Lorentz force in the mirror is ~30% lower than in the quadrupole model => lower coil prestress needed.

## Slide 27
Radial Shim=0.1mm
Saz, Pa
4K 11.9T 18kA

## Slide 28: Coil Stress in TQ and HQ mirrors (for reference)
90 mm
120 mm
300 K
4 K
4 K, 14 kA, 17 kA
28