## Slide 1
Sam Posen
TD R&D Retreat
26 January 2016
Fermilab Nb3Sn SRF R&D Program

## Slide 2: Increasing Reach of SRF Accelerators
Consider these two regimes of SRF accelerators:
Gradient in state of the art Nb cavities limited by Hsh (quench near ultimate limit)
Low duty factor, high energy
High duty factor / CW
  ILC: 16,000 cavities in 31 km linac
  Cryoplants for large linacs cost ~$100 million and require MW of power
Image from Rei Hori, linearcollider.org
Image from D. Delikaris, Cryogenics at CERN, 2010
Large dynamic load
Cost optimum gradient is relatively low: Pdiss ~ Eacc2/Q0
An alternative SRF material with higher Hsh and higher Q0 than niobium could offer dramatic cost savings, increasing reach of SRF accelerators of these types and others
Notes: LDF1000

## Slide 3: Alternative SRF Materials
There are many superconductors
Need high Q0 (large Tc), high Hsh
Many other important factors to consider
  Fabrication over large, complex geometry
  Easy to clean (e.g. no reaction with water)
  ξ not too small (more on this later)
Nb3Sn meets these criteria well
Image from Wikipedia

## Slide 4: Accelerator R&D Subpanel Report
Recommendation 4. Direct appropriate investment in superconducting RF R&D in order to inform the selection of the acceleration technology for the multi-MW proton beam at Fermilab.
Recommendation 6. Increase funding for development of superconducting RF (SRF) technology with the goal to significantly reduce the cost of a ~1 TeV energy upgrade of the ILC. Strive to achieve 80 MV/m accelerating gradients with new SRF materials on the 10-year timescale.

## Slide 5: Coating Mechanism: Vapor Diffusion
Sn vapor arrives at surface
Sn diffusion
Ts = Sn source temperature
=~1200 C
By independently controlling Sn vapor abundance, it can balanced with Sn diffusion rate to achieve desired stoichiometry
Sn
Nb
Nb3Sn
Sn Vapor
Heater
Coating chamber in UHV furnace
Nb cavity substrate
Tf = furnace temperature
=~1100 C

## Slide 6: University of Wuppertal Nb3Sn Furnaces

## Slide 7: Cornell Nb3Sn Furnace

## Slide 8: Cornell Nb3Sn Furnace
Tungsten feet
Tin crucible
Tin source heater
Witness samples
Inner heat shields

## Slide 9: Nb3Sn Q0(T)
Large Tc ~ 18 K
  Very small RBCS(T) – RBCS(T) ~ e-1.76Tc /T
  High Q0 even at relatively high T
Higher temperature operation
  Simpler cryogenic plant
  Higher efficiency
Possibility of cryocooler operation!

## Slide 10: Single Cell 1.3 GHz cavities at Cornell – 4.2 K
T = 4.2 K
Approx.
Hpk = Hc1
of Nb3Sn
N-doped Nb
Rs 10x smaller

## Slide 11: Improved Cooldown – Flat Q0 !
2x1010 at 18 MV/m, 4.2 K!

## Slide 12: Cryogenic Power Requirements, 1 cell at 1.3 GHz
Eacc = 16 MV/m
With Continued R&D

## Slide 13: Pulsed Quench Field
Used high power RF (MW) from klystron with short pulses
Measure quench field as a function of temperature
Compare to predicted ultimate magnetic field limit Hsh(T)

## Slide 14: High Gradients – Klystron Measurements
Demonstrated close to Tc Nb3Sn follows the expected superheating field of the 18K superconductor.
When extrapolated to 2K this leads to surface magnetic fields of 300 mT
  Nb superheating field 200 mT.
These results suggest that a well prepared Nb3Sn cavity with optimal shape can reach 80-90 MV/m
Superheaing field
Heating at defect/or second phase behavior takes over
With Continued R&D
Posen, Valles, Liepe, Phys. Rev. Lett. 115, 047001 (2015)

## Slide 15: Low Tin Content Regions
Nb
Nb3Sn
2
1
Nb L
0.5 μm
2
1
Sn L
0.5 μm
A. Godeke, Supercond. Sci. Tech, 2006
Transition?
C. Becker et al., App. Phys. Lett., 106, 082602 (2015).

## Slide 16: Nb3Sn SRF R&D at Fermilab
Increase accelerating gradients Eacc
  Optimize coating process to eliminate low tin content regions
  Study fundamental field limits of Nb3Sn with high power RF
  Study influence of surface roughness
Increase quality factors Q0
  Study origins of residual surface resistance
  Reduce influence of thermocurrents
  Retain high Q0 to high fields
Parameters for new recipe
Coat 9-cell sample cavity, measure uniformity
Coat multi-cell cavities, RF test
Coat samples then measure SEM/EDX, PPMS
Coat 1-cell cavities, RF test w/ T-map
Feedback for coating parameters: Tc, microstructure, composition, uniformity, Rs, quench field….

## Slide 17: Nb3Sn SRF R&D at Fermilab
Why vapor diffusion?
  Proven high quality SRF results
  Micron-sized grains
  Favorable phase diagram
  Quite smooth surfaces
Sn Vapor
Heater
Coating chamber in UHV furnace
Nb cavity substrate
M. Hein et al.
Wuppertal University
20 GHz Samples on Sapphire with grain size ~450 nm
S. Posen et al., Cornell U.

## Slide 18: Nb3Sn SRF R&D at Fermilab
Why vapor diffusion?
  Proven high quality SRF results
  Micron-sized grains
  Favorable phase diagram
  Quite smooth surfaces
Sn Vapor
Heater
Coating chamber in UHV furnace
Nb cavity substrate
M. Hein et al.
Wuppertal University
20 GHz Samples on Sapphire with grain size ~450 nm
S. Posen et al., Cornell U.

## Slide 19: Nb3Sn SRF R&D at Fermilab
Why vapor diffusion?
  Proven high quality SRF results
  Micron-sized grains
  Favorable phase diagram
  Quite smooth surfaces
Sn Vapor
Heater
Coating chamber in UHV furnace
Nb cavity substrate
M. Hein et al.
Wuppertal University
20 GHz Samples on Sapphire with grain size ~450 nm
S. Posen et al., Cornell U.

## Slide 20: Fermilab Furnace

## Slide 21
Coating chamber (Nb)
Modified door

## Slide 22
Coating chamber (Nb)
Modified door

## Slide 23: 1.3 GHz 9-cell
Modified door
Cavity support (Nb)
Coating chamber (Nb)
Chamber support
Inner heat shields
Tin Source

## Slide 24: 650 MHz 5-cell

## Slide 25: Summary
Nb3Sn extremely promising alternative material for SRF
  High Q0 even at high temperatures (++cryogenic efficiency)
  Predicted ultimate gradient limit twice as high as Nb
R&D initiative supported by LDRD
  Advance state of the art, both Eacc and Q0
  Scale up to coating production-style 9-cell 1.3 GHz and 5-cell 650 MHz cavities for the first time