## Slide 1
Martina Martinello
New Perspective, Fermilab
14th July 2016
Effect of Interstitial Impurities on the Field Dependent Microwaves Surface Resistance of Niobium

## Slide 2: Outline
Introduction
BCS Surface Resistance
Trapped Flux Sensitivity
Q-factors vs Mean free path
Best Surface Treatment
Conclusions

## Slide 3: SRF Cavities Figure of Merits
Standard ILC cavity
Q-factor ():
High → lower power consumption
Accelerating field ():
Determine the energy transferred to charged particles
High → lower accelerator length
High Q at large gradient may reduce both capital and operational costs of accelerators
SRF Cavities Figure of Merits

## Slide 4: Experimental procedure
Large variety of 1.3 GHz single cavities with different surface treatments:
    standard Nb treatments: 120 C baking, electro-polishing (EP)
    different N-doping treatments
Surface resistance contributions analysis for each cavity
Mean free path determination for each cavity

## Slide 5: BCS Surface Resistance
RBCS defines by Mattis and Bardeen and based on the Bardeen-Cooper-Schrieffer theory of superconductivity:
Depends on material parameters:
Theoretical minimum of RBCS vs around

## Slide 6: Residual Resistance
Residual resistance is mainly due to defects, precipitates and so on…
Depends on both bulk and surface treatments
It is known that with 120C bake treatment it increases of about 2 nm

## Slide 7: Trapped Flux Surface Resistance
RFl defines the dissipation due to trapped flux during the SC transition:

## Slide 8: Mean Free Path Calculation
Measurements of frequency vs T close to Tc
The interpolation is done using Halbritter SRIMP code. The parameters of the interpolation are:
                London penetration depth: → fixed
                Critical temperature: → fixed
                Intrinsic coherent length: → fixed
                Mean free path (m.f.p.):
                Energy gap:
                Penetration depth at f0 :
                Residual resistance:

## Slide 9: Outline
Introduction
BCS Surface Resistance
Trapped Flux Sensitivity
Q-factors vs Mean free path
Best Surface Treatment
Conclusions

## Slide 10: BCS vs mfp
N-doping allows to tune the mean free path and reaching the theoretical minimum of RBCS vs mean free path
Different theoretical curves for standard Nb cavities and N-doped cavities
  → Mean free path is not the only parameter changing with N-doping
  → N-doped cavities may have larger than standard Nb cavities

## Slide 11: Outline
Introduction
BCS Surface Resistance
Trapped Flux Sensitivity
Q-factors vs Mean free path
Best Surface Treatment
Conclusions

## Slide 12: Trapped Flux Sensitivity
How much the cavity dissipated per amount of trapped flux:

## Slide 13: Sensitivity vs mean free path
2/6 N-doping

## Slide 14: Trapped Flux Sensitivity Field Dependence

## Slide 15: Outline
Introduction
BCS Surface Resistance
Trapped Flux Sensitivity
Q-factors vs Mean free path
Best Surface Treatment
Conclusions

## Slide 16: Q-factor vs mfp
Adding together all the contributions, it is possible to predict the Q-factor as function of mean free path for different amount of trapped flux

## Slide 17: Q-factor vs mfp
Adding together all the contributions, it is possible to predict the Q-factor as function of mean free path for different amount of trapped flux

## Slide 18: Q-factor vs mfp
Adding together all the contributions, it is possible to predict the Q-factor as function of mean free path for different amount of trapped flux

## Slide 19: Q-factor vs mfp
Adding together all the contributions, it is possible to predict the Q-factor as function of mean free path for different amount of trapped flux

## Slide 20: Outline
Introduction
BCS Surface Resistance
Trapped Flux Sensitivity
Q-factors vs Mean free path
Best Surface Treatment
Conclusions

## Slide 21: Q-factor vs Trapped Flux for different surface treatments
12
15

## Slide 22: Outline
Introduction
BCS Surface Resistance
Trapped Flux Sensitivity
Q-factors vs Mean free path
Best Surface Treatment
Conclusions

## Slide 23: Conclusions
N-doped cavities are closed to both minimum of BCS and maximum of sensitivity
Light N-doping allows lower sensitivity and still low BCS
The 2/6 N-doping recipe gives the highest Q-factor at 2 K and 16 MV/m as long as the trapped field is less than 10 mG
Further optimization still possible towards even lighter N-doping

## Slide 24: Thank you for your attention

## Slide 25: Back up Slides

## Slide 26: N-doping effect on mean free path
Nitrides
Interstitial nitrogen in Nb
N-doping modify the mean free path ( ppm of interstitial N)
Non-doped
Doped
Depth (mm)
LE-mSR measurements (Ba=25mT)
Atomic concentration (cm-3)
~15 nm - no screening
N-doped: mfp~40 nm
EP: mfp > 400 nm
120C bake: mfp~2-16 nm

## Slide 27: Insight on the Anti-Q-Slope
Fit of Rs vs T at different field levels using BCS theory (with SRIMP1):
With BCS theory we cannot discriminate which parameters is changing with the field:

## Slide 28: Flux Trapping during Cooldown
2
1.5
1
0.5
0
The amount of trapped magnetic flux depends on:
external magnetic field ()
flux expulsion ()
No trapped flux when:
      mG
      or
      @ the equator
@ equator:
Simulation with perfect diamagnetic () walls:
Magnetic flux fully expelled
Magnetic flux fully trapped