## Slide 1
Mechanical Analysis of Coil E2
Reported by P. Wanderer, BNL
Analysis by H. Witte and A. Marone, BNL
MICE-US meeting
March 25, 2016

## Slide 2: MICE Spectrometer

## Slide 3: Aims of Study
Understand training behaviour
Quenches triggered mostly by E2
  Mechanism?
After training spectrometer is ok
Thermal cycling requires re-training
Fix?

## Slide 4: Spectrometer Training
 | Margin
E2 | 0.7
SS | 0.78
E1 | 0.7

## Slide 5: Model
NbTi: Orthotropic material properties
  E1/2=100/50 GPa
  From:
    Mechanical properties of epoxy impregnated superconducting solenoids. DOI: 10.1109/20.511486
    Also: DOI:10.1016/0010-4361(78)90587-6
Al-6061T6
  Isotropic elastic
FEA model
  Contact elements between bobbin & coils (0.2 friction)
E2
E1
C
M1
M2
Good field region

## Slide 6: Model
Winding tension + Cooldown + EM force
Quasi-static
Transient

## Slide 7: E2 After Cooldown
Radius (m)
Aluminum mandrel shrinks more than NbTi solenoid
Axial shrinkage leads to coil being clamped in place
Partially detached axially
Radially detached from bobbin
x, y axes in meters
Axis in color: δr, m
E2 at room temp.

## Slide 8: Forces on E2
Solenoidal forces
  Axial compression
  Radial expansion
Additional axial force towards Centre Coil
  Fringe field effect from C
Coil shrinks longitudinally and is pressed against C coil
Bobbin acts as clamp

## Slide 9: Load Cycles (~during training)
0→25%
0→40%
0→60%
0→80%
0→100%
E2 at room temp.
x, y axes in m

## Slide 10: Radial Displacement
25%
40%
60%
80%
100%
E2
Non-zero slope of straight line indicates “training”
All slides:
Displacements have been amplified for better visibility.

## Slide 11: Radial Displacement
After Cooldown
After mechanical cycling
E2

## Slide 12: Warming Up + Cooldown
293K→4.2K, energization→293K
4.2K→energiz., 293K→4.2K
Radial displacement (amplified) vs axial position, before and after cycling (note two line colors).
Conclusion: cycle to 293K brings magnet to pre-training state.

## Slide 13: Comparison: E1
E1
Straight line has no slope.

## Slide 14: Preliminary Analysis of M.I.C.E. Solenoid Coils
Marone
March 23, 2016

## Slide 15: Model Run With/Without ½” Aluminum Outer Sleeve Pre-stress and Thermal Contraction
Coil bends in reverse direction about 75μm.
No sleeve
Conclusion: aluminum sleeve important

## Slide 16: Model Run With ½” Aluminum Outer Sleeve, With / Without magnetic forces
B=0
Δr ~75μm
B~4T
Δr ~ 300μm
Conclusion: cycling produces significant deflections, even with sleeve

## Slide 17: Comparison & Summary
Comparison of model inputs
  Remark: models still under development, will converge
Summary for E2
  Both models show significant deflections of the end flange due to thermal contraction
  Models established a mechanism for training, repeatable training and reset of training due to thermal cycle
  Mechanical changes are essential to eliminate this problem
 | friction | sleeve | Coil design | B | Thermal Contr. | other
Witte | Y | N | Wang | ~5.6T | Y | TBD
Marone | N | Y | Gupta | ~4.0T | Y | TBD

## Slide 18
BACKUP

## Slide 19: Two Cycles – Same Current
0%
25%
0%
25%
0%

## Slide 20: Steel Bobbin

## Slide 21: Summary
Understand training behavior
  Mandrel acts as clamp
Quenches triggered mostly by E2
  E2 is held weakly on one side
  Forces push E2 out of clamp
After training spectrometer is ok
  Same load does not seem to produce slippage
Thermal cycling requires re-training
  Room temperature: “reset”
Fix?