## Slide 1: Cable Development and Optimization
E. Barzi
Fermilab High Field Magnet Program Design Review
28-29 April 2016

## Slide 2: Outline
CHARGE: Is the cable selection appropriate for this application?
PRESENTATION CONTENT
Strand and Cable parameters for Outer Coil – Same as 11 T Dipole
Cable Development for Outer Coil – Same as 11 T Dipole
Strand and Cable parameters for Inner Coil
Cable Development for Inner Coil
15 T Dipole Short Sample Limits
Sensitivity of Ic and RRR to Heat Treatment Parameters
Summary of Strand Procurement and Cable Fabrication
Strand R&D with OST
Conclusions

## Slide 3: Strand and Cable Previous Landscape
Chart: B (T)
| 1997 | 2008
Record | 13.5 | 13.8
HFDA 2000-2005 | 4.5014 | 5.0274 | 6.4757 | 10.1 | 9.8 | 10.6
HFDM-LM 2002-2008 | 6.6821 | 9.99 | 6.0052 | 6.4435 | 11.4 | 10 | 9.9
HFDC 2003 | 5.7924
TQC 2006-2011 | 11 | 10.9548 | 11.2506 | 11.5 | 11.7 | 11.9
TQM-LQM 2008-2012 | 10.4 | 12.4 | 12.3 | 13.3 | 13.3
MBHSP 2012-2014 | 10.4 | 11.7 | 11.6
MBHSM | 12.52
HFD15 | 15 | 15 | 15 | 20
60 x 0.7 mm
(27-28) x 0.7 mm
40 x 0.7 mm
27 x 0.7 mm

## Slide 4: Strands and Cables for 11T Dipole Coil = 15T Outer Coil
Baseline strand
R&D strand
0.7 mm strand - to achieve required magnet transfer function of 11 T at 11.85 kA
40 strand cable – CERN cabling machine limit
Critical current degradation due to cabling < 10%
StSt core
Large aspect ratio - cable mechanical stability
  cable geometry, packing factor

## Slide 5: 11 T Dipole Cable Studies and Optimization
A mid-thickness spec of 1.25 mm meets the Ic degradation requirements also in the case of a cored cable.
The Ti doped wire preserved its current carrying capabilities up to large cable compaction factors, even without any prior annealing.
Maximum Ic degradation at 12 T was ~2% at ~89% cable compaction.

## Slide 6: Strand Parameters for Inner Coil

## Slide 7: Cables used in Studies for Inner Coil
  Effect of cable Packing Factor (PF) on Ic degradation and RRR
  Effect of pre-treating the wires before cabling
  Effect of magnetic field on RRR

## Slide 8: Results of Cable Studies for Inner Coil

## Slide 9: Results of Cable Studies for Inner Coil (cont.)
  Comparison of transport data with microscopy analysis of cable cross sections
  Magneto-resistivity effect

## Slide 10: Cables and Insulation Specs

## Slide 11: Magnet Short Sample Limit
Magnet short sample limit estimated based on extracted strand data:
  11.05 kA (Bap=15.25 T) at 4.5 K
  12.2 kA (Bap=16.65 T) at 1.9 K

## Slide 12: Sensitivity of Ic and RRR to Heat Treatment Parameters

## Slide 13: Nb3Sn Strand Procurement FY11-FY16
11 T program ~450 kg
15 T program will need ~500 kg (250 kg already procured)
Year | L, km | W, kg | D, mm | Design | Ternary type
2010 | 17.3 | 59 | 0.7 | 108/127 | Ta
2011 | 42.1 | 144 | 0.7 | 150/169, 108/127 | Ta
2012 | 40.6 | 138 | 0.7 | 108/127 | Ta, Ti
2013 | 53.3 | 182 | 0.7 | 108/127 | Ti
2014 | 17.7 | 120 | 1.0 | 150/169 | Ti
2016 | ~20 | ~135 | 1.0 | 150/169 | Ti

## Slide 14: Cable Production FY11-FY16
Coil ID | Cable N x D | Billets ID | Strand Type | Cable length | Cable geometry | Core width | Cable fabrication
MBH02, MBH03 | 40 x 0.7 mm | 12292, 12319, 12521-22, 13062-63, 13090 | 108/127 (Ta) | 414 m | 1.251±0.001 x 14.71±0.01 mm2, 15.0 deg | None | Jul. 2011, 2-pass w/intermediate anneal
MBH05, MBH07 | 40 x 0.7 mm | 13538, 13613 | 150/169 (Ta) | 120 m 230 m | 1.251±0.002 x 14.69±0.01 mm2, 15.0 deg | 11.0 mm | Sep. 2011, 2-pass w/intermediate anneal
MBH08 | 40 x 0.7 mm | 14144, 14145, 14194, 14195, 9772 | 108/127 (Ta), 114/127 | 138 m | 1.252±0.004 x 14.71±0.01 mm2, 14.0 deg | 11.7 mm | Nov. 2012 1-pass
MBH09 | 40 x 0.7 mm | 14144, 14145, 14194, 14195, 14700 | 108/127 (Ta) | 180 m | 1.249±0.002 x 14.70±0.01 mm2, 14.8 deg | 11.0 mm | Nov. 2012 1-pass
MBH10, MBH11 | 40 x 0.7 mm | 14144, 14145, 14194, 14195, 14700 | 108/127 (Ta) | 220 m | 1.245 x 14.72 mm2, 15.0 deg | 11.0 mm | Nov. 2012 2-pass w/intermediate anneal
Practice coils | 40 x 0.7 mm | 11444 | 132/169 (Ti) | 216 m | 1.251 x 14.73 mm2, 15.6 deg | 9.5 mm | Mar. 2013 1-pass
 | 40 x 0.7 mm | A101 | Hard Cu | 600 m | 1.250 x 14.71 mm2, 16.8 deg | 11.0 mm | Oct. 2013 1-pass
15 T Dipole Outer Layer | 40 x 0.7 mm | 15043, 15044, 15045, 15244, 15245, 15290 | 108/127 (Ti) | 374 m | 1.251±0.001 x 14.71±0.01 mm2, 16.8 deg | 11.0 mm | Oct. 2013 1-pass
15 T Dipole Inner Layer | 28 x 1 mm | 16638, 16639, 16640 | 150/169 (Ti) | 420 m | 1.803±0.002 x 14.79±0.02 mm2, 15.5 deg | 11.0 mm | Dec 2015 1-pass

## Slide 15: RRP Strand R&D (with OST)
Goal: increase Jc(15T) with an ultimate target of 2000 A/mm2 for a 169 stack strand at 1.0 mm (Ds~58 µm)
  Present subelement design - average Jc(15T)~1500 A/mm2
Approach: modifications to the subelement designs
Chemical optimization
  Produce a half height high-Jc subelement billet having Nb and Nb-Ti filaments with a Nb-Ta diffusion barrier
  Deliver ~45 kg of 1 mm wire
Local Area Ratio (LAR) optimization
  Produce two half height high-Jc subelement billets having Nb and Nb-Ti filaments with variable LAR from annulus to barrier
  Deliver ~90 kg of 1 mm wire
  0.8, 0.9, 1.0, 1.1 and 1.2 mm wire samples
Next: 1-1.2 mm RRP-217 stack design.

## Slide 16: Conclusions
SC wires and cables are key elements of the 15 T Dipole Demonstrator
Cables were designed and optimized based on the properties of present Nb3Sn wires
Sensitivities studies are being performed to allow for variations in temperature and time during coil heat treatment
Wire R&D continues with OST on layout and chemical optimizations to increase Jc, which is important for margin
SBIR are being submitted within a number of agencies to probe further Jc increases acting on the inherent flux pinning mechanisms