## Slide 1: SEY measurement and RFA simulations
Yichen Ji

## Slide 2: Table of content
SEY measurement and analysis
  Newest SEY result
  SEY vs time, beam intensity, integrated intensity
RFA related POSINST simulations
  SEY, intensity scan
  Analysis based on simulation result and RFA data
Future works

## Slide 3: TiN

## Slide 4: Stainless steel

## Slide 5: Intensity Hisory

## Slide 6: SEY over time
Chart: 
| 41527 | 41556 | 41580 | 41724 | 41772 | 42018 | 42066 | 42081 | 42115 | 42318 | 42403 | 42423
TiN | 2.0982 | 1.5617 | 1.3498 | 1.3246 | 1.8901 | 1.2699 | 1.253
SS | 2.2739 | 1.7937 | 1.6815 | 1.7816 | 1.4898 | 2.3062 | 1.7549 | 1.7488 | 1.5488 | 1.9677 | 1.6731 | 1.539
intensity | 16.8 | 24.4 | 26.6 | 26.6 | 24.2 | 24.2 | 24.9 | 30.5 | 34 | 23.7 | 33.7 | 37.9

## Slide 7: SEY over Beam Intensity
Chart: 
| 24.9 | 30.5 | 34 | 24.4 | 26.6 | 26.6 | 24.2 | 33.700000000000003 | 37.9
SS | 1.7549 | 1.7488 | 1.5488 | 1.7937 | 1.6815 | 1.7816 | 1.4898 | 1.6731 | 1.539
TiN | 1.5617 | 1.3498 | 1.3246 | 1.2699 | 1.253

## Slide 8: SEY over Integrated beam intensity
Chart: Integrated beam intensity e18
| 0 | 9.5042255609999984 | 16.875968678850661 | 16.875968678850661 | 36.577650965180752 | 0 | 15.567300067359209 | 23.251609892070281 | 43.440955883181097 | 0 | 38.382325938570503 | 51.227070998650802
TiN | 2.0982 | 1.5617 | 1.3498 | 1.3246 | 1.8901 | 1.2699 | 1.253
SS | 2.2739 | 1.7937 | 1.6815 | 1.7816 | 1.4898 | 2.3062 | 1.7549 | 1.7488 | 1.5488 | 1.9677 | 1.6731 | 1.539

## Slide 9: RFA related simulation
Chart: Beam Intensity e12 protons
| 34.44 | 35.42 | 36.409999999999997 | 37.39 | 38.380000000000003 | 39.36 | 40.340000000000003 | 41.33
1.2sey | 812000000 | 943000000 | 1180000000 | 1500000000 | 1990000000 | 2660000000 | 3800000000 | 5440000000
1.25sey | 1220000000 | 1680000000 | 2580000000 | 4640000000 | 11300000000 | 36900000000 | 154000000000 | 678000000000
1.3sey | 2670000000 | 6230000000 | 26200000000 | 245000000000 | 1880000000000 | 4640000000000 | 7490000000000 | 10300000000000
1.35sey | 128000000000 | 1260000000000 | 4630000000000 | 8120000000000 | 11800000000000 | 15300000000000 | 19200000000000 | 22700000000000
1.4sey | 4370000000000 | 8280000000000 | 12900000000000 | 17600000000000 | 22100000000000 | 26900000000000 | 31700000000000 | 35800000000000
1.45sey | 12300000000000 | 18000000000000 | 23700000000000 | 28400000000000 | 33300000000000 | 38600000000000 | 42400000000000 | 46400000000000
1.5sey | 24400000000000 | 29500000000000 | 34500000000000 | 39400000000000 | 43700000000000 | 48200000000000 | 52000000000000 | 57100000000000
1.55sey | 33800000000000 | 38900000000000 | 43700000000000 | 48100000000000 | 52700000000000 | 57400000000000 | 61600000000000 | 66100000000000
1.6sey | 42000000000000 | 46300000000000 | 51700000000000 | 56200000000000 | 60800000000000 | 65500000000000 | 69900000000000 | 74900000000000
1.65sey | 54200000000000 | 60700000000000 | 64700000000000 | 70400000000000 | 75400000000000 | 80800000000000 | 86500000000000 | 91800000000000
1.7sey | 60800000000000 | 65700000000000 | 71500000000000 | 77000000000000 | 82900000000000 | 88700000000000 | 94400000000000 | 99900000000000
1.75sey | 68200000000000 | 74200000000000 | 79700000000000 | 86100000000000 | 91300000000000 | 98000000000000 | 103000000000000 | 111000000000000

## Slide 10: RFA signal to bombardment rate fudge factor estimation
Based on RFA circuit
  1V~1.4e8#/s/cm2
  off by one order of magnitude
Turned on RFA amplifier on April 11th
  Factor of 8 change in fudge factor
Based on POSINST and Feb 23rd SEY measurement
  Before Apr 11th 1V~4.2e13#/s/cm2
  After Apr 11th 1V~5.3e12#/s/cm2
Rule of thumb: 1C/m2 causes a noticeable change in SEY
  6e14#/cm2
Estimate current SEY
  1.4

## Slide 11: Future work
More SEY measurement
  Conclude The TiN experiment
  Compare with the SEY estimation
More accurate RFA simulation
  Details such as bunch length, beam size, bunch structure, better SEY curve, Magnetic field and etc.
  SEY condition publications