## Slide 1: WG-1: Performance Frontier
Guilherme Dalla Lana Semione
X-Ray Physics and Nanoscience
DESY Nanolab
TESLA Technology Collaboration
21-24 February 2017
Facility for Rare Isotope Beams, East Lansing, MI, USA
“Nitrogen infusion” in Niobium model system

## Slide 2: Cooperating groups
DESY Nanolab (FS-NL)
Prof. Andreas Stierle
DESY Linear Accelerator Technologies (FLA)
Nicholas Walker
Prof. Brian Foster (Humboldt/Universität Hamburg)
DESY MHF-SL
Wolf-Dietrich Möller
Detlef Reschke
DESY Nanolab group
Manuel Abuín Herráez
Björn Arndt
Annika Böhme
Marcus Creutzburg
Dirk Franz
Simon Geile
Elin Grånäs
Thomas F. Keller
Konstantin Krausert
Satishkumar Kulkarni
Pirmin Lakner
Johannes Pfrommer
Henning Runge
Roman Shayduk
Arti Dangwal Pandey
Heshmat Noei
Vedran Vonk
Susanne Weigert
Prof. Dr. Andreas Stierle

## Slide 3: Motivation
Physical and chemical understanding of the role of nitrogen;
Determine changes in the niobium surface layer;
  Evolution of native oxide layers, nitrogen concentration and chemical state
Optmization of treatment procedures;
Nb
100nm
Wang et al. Phys. Rev. B 74, 235304
GIXRD
http://jacobs.physik.uni-saarland.de
XPS
http://www.mpip-mainz.mpg.de/62518/Scattering_methods
XRR

## Slide 4: Experimental method
X-Ray Reflectivity
Constructive interference
between layers
  Thickness (d)
  Layer density profile (ρe)
  Surface or interface roughness (σ)
  Independent of crystalline state
Electron density
profile

## Slide 5: Experimental procedure
  Heat up to 800°C, keep for 2 hours
    P0 = 3.6x10-9 mbar / P800 = 8.0x10-7 mbar
  Cooldown to 120°C (P120=2.10-8 mbar)
    Insert 25 mTorr (0.033 mbar) of N2 (99.999%)
    Keep for 23 hours
  Record successive XRR scans
Nb(100) single crystal: 10 mm wide
4 mm thick
In-situ tracking of the nitrogen infusion process:
X-rays
Cu Kα
Detector

## Slide 6: Results: XRR
RT
NbO
Nb
Nb2O5
NbO2
NbO
Nb
~4.7nm
~4.2nm
800°C/2h
Infusion
NbO
Nb
NbOxNy
~14nm
~1nm
In-situ infusion
Air-exposure
High Pressure Water Rinsing

## Slide 7: Results: XRR
Mo Kα
As-received crystal
Mo Kα
Cu Kα
Nb2O5
NbO2
NbO
Nb
800°C/1h - UHV
“Infusion”
Natural oxide layers suppressed
Protective layer - passivation
+ air exposure
~ 36 days
+ air exposure ~ 35 days
In-situ infusion
Air-exposure
High Pressure Water Rinsing
NbO
Nb
NbOxNy

## Slide 8: Results: SEM, FIB
Rough surface
Without precipitates
400 nm
3μm
3μm
Contrast change – irregular layer visible, 15 to 40 nm thick
32.53 nm
22.06 nm
In-situ infusion
Air-exposure
High Pressure Water Rinsing

## Slide 9: Results: XRR, SEM
Layer | σ (Å)
NbO | 20
Nb | 2.5
SEM
Before
After
Sample position
In-situ infusion
Air-exposure
High Pressure Water Rinsing
400 nm
500 nm
NbO
Nb
NbOxNy
~4.5nm
Notes: 670mm

## Slide 10: Conclusions
The infusion process creates an overlayer within the first hour of treatment. No significant changes are observed after longer N2 exposure.
The growth of the natural oxide layers in the surface due to air exposure is suppressed by the infusion process.
No precipitates were found, most notably absent is the β-Nb2N phase.
Passivation still remains after High Pressure Water Rinsing.

## Slide 11: Future Work
Reproduce the experiment, also with longer infusion time (48 hours)
  Different Single-crystal orientations;
  Large Grain samples;
XPS sputtering profile
  Composition of layers;
Diffuse Scattering X-Ray measurements
  Nitrogen concentration
  Trapping effects
O, N interstitials
NbOxNy
NbO
Nb
Bulk contribution
M. Delheusy, 2008

## Slide 12: Acknowledgements
Special thanks to:
Nicolay Krupka
Detlef Reschke
Axel Matheisen
Marc Wenskat
Alena Prudnikava
Arti Dangwal Pandey
Heshmat Noei
Vedran Vonk
Prof. Andreas Stierle

## Slide 13
Thank you!

## Slide 14
NbO
(022)
GIXRD – P07 Beamline, Petra III

## Slide 15: “Doping” Sample
Nitrogen doping @900°C
  Large grain Nb(100)
    Outgassing at 900°C/2 hours (1.0x10-5 mbar)
    Nitrogen supplied for 20 min (0.04 mbar - 30mTorr)
    Further 30 min anneal without Nitrogen
At Nb coordinates 1.1 0 0.74 (HKL)
Epitaxial β-Nb2N and NbO
SEM
GIXRD – Cu Kα

## Slide 16: XRR
X-Ray Reflectivity

## Slide 17: XPS results – Infused Sample
Red: Before HPR
Green: After HPR