## Slide 1: Degradation and recovery of ISAC-II cavities
Tobi Junginger, Arthur Chen, Bob Laxdal, Doug Storey, Zhongyuan Yao and Vladimir Zvyagintsev

## Slide 2: ISAC-II accelerator magnetic environment
5 low beta cryomodules with 4 QWRs each
3 high beta cryomodules with 2x6 and 1x8 QWRs
Each module contains a solenoid for focusing
Minimalist’s shielding strategy
  non magnetic materials where possible
  no shielding between cavity and solenoid – use procedures
Cavities should be insensitive to quench degradation since they have a reactor grade niobium jacket which acts as a Meissner shield
However the top and bottom plate of the cavity are single walled

## Slide 3: ISAC-II accelerator magnetic environment
Focusing in the SC Linac is provided by superconducting solenoids (B9T)
End fringe fields controlled with active `bucking’ coils (Bcavity30mT)
Cavity
Prototype Solenoid at Accel

## Slide 4: Observation of cavity degradation
During operation cavities sometimes trip
In a few cases the cavity will have a largely reduced Q0, multipacting or lower quench level afterwards
Our assumption is that the cavity has quenched and flux from the solenoid has been trapped
If Q0 is strongly reduced the cavity cannot be operated anymore at the same gradient. It needs to be recovered or the linac needs to be retuned (downtime up to 8h depending on operator´s experience and number of cavities following the degraded one)
In general recovering a cavity could either be done by
  quenching with solenoid off (1h downtime) or
  warming up the cryomodule above Tc (4h downtime)

## Slide 5: Weak degradation
Cavities are nominally operated -25° off crest
  We are using only cos(25°) ≈ 90% of the full voltage
This means that by decreasing the cavity phase, the voltage gain through the cavity can be increased.
Real life example:
  A cavity tripped during operation.
  We were unable to recover the initial voltage. Cavity quenched reproducibly at a voltage about 1-2% below its nominal value
  Reduced the cavity voltage by 3% and compensated this by changing the phase from -25° off crest, to -21°, so = 4°.
 Operators and RF support had a quiet night!

## Slide 6: Severe degradation
Chart: Ea, MV/m
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
Q0 at 7W | 8569539.4423 | 34278157.7691 | 77125854.9806 | 137112631.0766 | 214238486.0571 | 308503419.9223 | 419907432.672 | 548450524.3063 | 694132694.8251 | 856953944.2286 | 1036914272.5166 | 1234013679.6891
Initial | 589973305.3932 | 502889581.8713 | 425246345.1252 | 351153559.2289 | 291319384.5535
Before Thermal Cycle | 111432037.763 | 230517634.9008 | 103406121.1543 | 94852043.0937 | 89795104.0672 | 89279766.9435 | 85679404.3847 | 83564853.5741 | 80484778.9957
Quench with solenoid off does not recover Q0
Sudden degradation during operation
SCB5-2

## Slide 7: Turn off solenoid and warm cavity up
Chart: Ea, MV/m
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
Q0 at 7W | 8569539.4423 | 34278157.7691 | 77125854.9806 | 137112631.0766 | 214238486.0571 | 308503419.9223 | 419907432.672 | 548450524.3063 | 694132694.8251 | 856953944.2286 | 1036914272.5166 | 1234013679.6891
Initial | 589973305.3932 | 502889581.8713 | 425246345.1252 | 351153559.2289 | 291319384.5535
Before Thermal Cycle | 111432037.763 | 230517634.9008 | 103406121.1543 | 94852043.0937 | 89795104.0672 | 89279766.9435 | 85679404.3847 | 83564853.5741 | 80484778.9957
After thermal cycle | 1045684781.9692 | 931629201.2777 | 627060794.2889 | 455293074.8655 | 206879090.7557 | 153429558.1205 | 334684790.9846 | 824804619.5398 | 1151500845.2287 | 1280814800.7574 | 1657470700.6377
Quench with solenoid off did not recover Q0
Warm up above Tc with solenoid off recovers Q0
Sudden degradation during operation
Full recovery by thermal cycling
SCB5-2

## Slide 8: Undegraded cavities: Quench cavity with solenoid on/off
Chart: Ea, MV/m
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
Q0 at 7W | 8569539.4423 | 34278157.7691 | 77125854.9806 | 137112631.0766 | 214238486.0571 | 308503419.9223 | 419907432.672 | 548450524.3063 | 694132694.8251 | 856953944.2286 | 1036914272.5166 | 1234013679.6891
Initial test | 581344824.0405 | 605956095.4484 | 625917068.6045 | 692710260.5116 | 746285353.4864 | 782533577.0799 | 839418028.3663 | 921188955.0244 | 1193795440.9296 | 580220692.4968 | 563333940.1164 | 534838727.7473 | 515403484.7833 | 483062068.1853 | 401878966.4154 | 286599855.8221 | 164970015.4463 | 191769654.3863 | 266371188.5983 | 89019787.1541
After Quench solenoid off | 561620620.1334 | 642850914.3513 | 499925808.6183 | 403793917.3462 | 259202427.9314 | 201343162.6061 | 130368871.4678
After quench solenoid on | 115410201.762 | 196775989.6038 | 365225982.9493 | 497635669.6203 | 562031765.5124 | 626221243.2136
Chart: Ea, MV/m
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
Q0 at 7W | 8569539.4423 | 34278157.7691 | 77125854.9806 | 137112631.0766 | 214238486.0571 | 308503419.9223 | 419907432.672 | 548450524.3063 | 694132694.8251 | 856953944.2286 | 1036914272.5166 | 1234013679.6891
Initial | 832424562.875 | 970144146.1395 | 1282508834.1095 | 473935203.5282 | 610599497.8233 | 710256694.2306 | 783987758.9293 | 391695729.405 | 335235366.3545
After quench solenoid off | 867918121.0901 | 408751871.3854 | 652973607.1199 | 775107932.236 | 989278671.6089
After quench solenoid on | 464059599.896 | 671328247.925 | 870656263.3474 | 782451583.6381 | 897535027.4172
SCB2-3
SCB5-1
Distant from solenoid
Close to solenoid
Quenching the cavity with RF does not yield a degradation

## Slide 9: Undegraded cavities: Effect of thermal cycling
Chart: Ea, MV/m
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
Q0 at 7W | 8569539.4423 | 34278157.7691 | 77125854.9806 | 137112631.0766 | 214238486.0571 | 308503419.9223 | 419907432.672 | 548450524.3063 | 694132694.8251 | 856953944.2286 | 1036914272.5166 | 1234013679.6891
Initial test | 581344824.0405 | 605956095.4484 | 625917068.6045 | 692710260.5116 | 746285353.4864 | 782533577.0799 | 839418028.3663 | 921188955.0244 | 1193795440.9296 | 580220692.4968 | 563333940.1164 | 534838727.7473 | 515403484.7833 | 483062068.1853 | 401878966.4154 | 286599855.8221 | 164970015.4463 | 191769654.3863 | 266371188.5983 | 89019787.1541
After Quench solenoid off | 561620620.1334 | 642850914.3513 | 499925808.6183 | 403793917.3462 | 259202427.9314 | 201343162.6061 | 130368871.4678
After quench solenoid on | 115410201.762 | 196775989.6038 | 365225982.9493 | 497635669.6203 | 562031765.5124 | 626221243.2136
After thermal cycle | 604615388.3564 | 653532392.5088 | 729819845.5354 | 871375462.7166 | 566623383.3334 | 503499485.7547 | 381223367.7668 | 188342815.6922 | 0 | 0 | 0
Thermal cycling has no effect on undegraded cavities
SCB5-1
3 hours
T [K]
T [K]
Top
Top
Bottom
Bottom
Inner Conductor
Inner Conductor
20 K cycle
Initial
cooldown
Different cooldown dynamics
20
60
40
80
10
15
20
0
5

## Slide 10: Why do cavities degrade during operation ?
Assumption: Cavity quenches and traps flux from solenoid while the Meissner shield remains effective
Three possible points of flux entry
  Top plate  Field from solenoid below 1µT
  Beam port  Field from solenoid below 1µT
  Bottom plate

## Slide 11: Simulation of flux from solenoid on the cavity surface

## Slide 12: Why do cavities degrade during operation ?
Assumption: Bottom plate quenches and cavity traps flux from solenoid
Field from the solenoid is about 30mT
Assuming that all field is trapped we can estimate the surface area which needs to trap flux in order to account for the Q decrease
  Calculate RN at at 10K assuming normal skin effect
  Derive additional RS assuming full trapping of 30mT
  Comparison with the experimentally observed ΔQ allows to calculate the ratio
  Comparison with an RF simulation gives the area which needs to quench to explain the observed degradation

## Slide 13: RF simulation
|B|
Area which needs to trap 30mT to explain
Q decrease

## Slide 14: Summary
Degraded cavities
  Cavity voltage drop can be compensated by rephrasing (to some extent)
  Could not be restored by quenching using RF (1/1 case)
  Can be restored by thermal cycling (4/4 cases)
  If the cavity is at the end of the linac retuning might be faster than thermal cycling
 A case by case decision is necessary!
Undegraded cavities
  Do not degrade if quenched by RF (5/5 cases)
  Are insensitive to thermal cycling (7/7 cases)
Flux trapping from the solenoid would be a straight forward interpretation for the degradation, however
  Also cavities which are not next to the solenoid degrade (not presented)
  Substantial amounts of flux can only enter through the bottom plate, where the RF magnetic field is small and a large area would need to quench to explain the observed Q degradation