## Slide 1: First LCLS-II Production Cavity Results with N-Doping
Dan Gonnella
2017 TTC Workshop
February 21, 2017

## Slide 2: Outline
Introduction to LCLS-II
Cavity Preparation Method
Transfer of N-Doping to Production
RF Results from First Cavities
Summary

## Slide 3: Outline
Introduction to LCLS-II
Cavity Preparation Method
Transfer of N-Doping to Production
RF Results from First Cavities
Summary

## Slide 4: Introduction to LCLS-II
The SRF linac is closely based on the XFEL/ILC/TESLA Design
It consists of 35 cryomodules each with 8 cavities – total of 280 cavities
The 280 1.3 GHz 9-cell cavities have a very ambitious Q specification:
Additionally, cavity must reach 19 MV/m
2.7 x 1010 at 16 MV/m and 2 K
2.5 x 1010 at 16 MV/m and 2 K
Q specification lowered in VT due to addition of stainless steel blank on short side of cavity – adds ~0.8 nΩ of Rres

## Slide 5: Outline
Introduction to LCLS-II
Cavity Preparation Method
Transfer of N-Doping to Production
RF Results from First Cavities
Summary

## Slide 6: Cavity Fabrication
Two vendors were chosen to build the SRF cavities
  RI Research Instruments GmbH
  E. Zanon S.p.a.
Niobium sheet was procured from two vendors
  Tokyo Denkai
  OTIC Ningxia
For the remainder of this talk, vendor names will not be used in order to protect confidentiality

## Slide 7: Cavity Preparation Method
In order to achieve the ambitious Q specification, all 9-cell cavities for LCLS-II are prepared with nitrogen-doping
Original recipe:
  140 μm bulk EP
  800oC degas for 3 hours in vacuum
  2 minutes at 800oC in 20-30 mTorr of N2
  6 minutes at 800oC in vacuum
  5-7 μm light EP

## Slide 8: Issues with Original Recipe
Material from both vendors showed worse flux expulsion when treated at 800oC in single-cell cavity tests than material used during the prototyping and R&D stage
This means that magnetic field specifications would need to be tighter in order to minimize the need for efficient flux expulsion
Ambient magnetic field will be below the spec of 5 mG in the cryomodule with the current magnetic shielding design, therefore much improvement on this would be difficult
Worse flux expulsion is an independent phenomena from N-Doping – It impacts all cavity preparation methods

## Slide 9: Initial Cavity Results
Some Great Cavities
Some Good Cavities
All these cavities tested in very low (0-1 mG) magnetic fields

## Slide 10: Residual Resistance
Rres significantly higher than in R&D Cavities

## Slide 11: Cavity Preparation Method
In order to achieve the ambitious Q specification, all 9-cell cavities for LCLS-II are prepared with nitrogen-doping
Updated recipe:
  200 μm bulk EP
  900oC degas for 3 hours in vacuum
  2 minutes at 800oC in 20-30 mTorr of N2
  6 minutes at 800oC in vacuum
  5-7 μm light EP
For more information on flux expulsion and the change in recipe see Ari Palczewski’s Talk

## Slide 12: Residual Resistance

## Slide 13: Residual Resistance
Lower Rres due to more bulk EP and better flux expulsion

## Slide 14: Initial Cavity Results

## Slide 15: Cavity Results after Recipe Change

## Slide 16: Outline
Introduction to LCLS-II
Cavity Preparation Method
Transfer of N-Doping to Production
RF Results from First Cavities
Summary

## Slide 17: BCS Resistance in Production Cavities
RBCS is a good measurement of the doping
Doping is unaffected by recipe change
RBCS obtained in production cavities is similar to that obtained during the R&D phase
Doping protocols successfully transferred to vendors for production
Small Representative Subset of Cavities

## Slide 18: Outline
Introduction to LCLS-II
Cavity Preparation Method
Transfer of N-Doping to Production
RF Results from First Cavities
Summary

## Slide 19: Vendor Statistics
22 Cavities from Vendor A have been tested, a mix of Material 1 and 2
  8 received original recipe
  Remaining 14 received new recipe
44 Cavities from Vendor B have been tested, all from Material 1
  16 received original recipe
  Remaining 28 received new recipe

## Slide 20: Vendor B Results
Majority of Cavities Now above 3x1010
Magnetic field in VT Dewars no longer actively compensated – most of these tests in >5 mG
Subset of Vendor B Cavities after Recipe Change
All Material 1
Almost all Vendor B Cavities Quench above 22 MV/m

## Slide 21: Vendor A Results
All Material 2
Spread in Q Due to Change in Recipe
Large Q Slope present in some cavities leading to quench below the spec of 19 MV/m
Related to material?

## Slide 22: Vendor A Results
Gradient limitation not related to material type
All Material 1

## Slide 23: Vendor A – Surface Roughness
EP at Vendor A was producing a very rough surface
Roughness was as high as 15 μm
It was found that EP temperature was leading to the EP no longer being in the “polishing regime” but in the “etching regime”
This Issue was Fixed
Image courtesy of Y. Trenikhina

## Slide 24: Vendor A – Improved EP
Q Slope and gradient limitation still present

## Slide 25: Vendor A – Increased Removal
Q slope and quench unchanged after 20 more micron removal

## Slide 26: Vendor A Path Forward
We are currently working with Vendor A to improve cavity fabrication methods
Specific care is being taken to ensure that foreign media is not introduced during fabrication
In parallel, 2 cavities with poor performance are being reset to “XFEL preparation” to check if performance is improved

## Slide 27: Outline
Introduction to LCLS-II
Cavity Preparation Method
Transfer of N-Doping to Production
RF Results from First Cavities
Summary

## Slide 28: Summary
Nitrogen-doping has been successfully transferred to industry for production in LCLS-II
Due to flux expulsion limitation with material used, a recipe change was required mid-production
Vendor produced nitrogen-doped cavities show similar RBCS as cavities from the R&D phase
Vendor B now produces cavities with Q’s on the order of 3-4 x 1010
Vendor A produces cavities with good Q at low fields but with strong Q slope leading to an early quench at or below the gradient specification
  This performance is independent of material used
Work is ongoing to improve performance of Vendor A cavities

## Slide 29
Questions or Comments?