## Slide 1: On Trapped Flux Losses: Expulsion and dissipation mechanisms description
Mattia Checchin
TTC Meeting, MSU, East Lansing
22-Feb-2017

## Slide 2: Trapped flux surface resistance
⇒ temperature-dependent part of the surface resistance
⇒ intrinsic residual resistance
⇒ trapped magnetic flux surface resistance:
If pinned, vortices may survive in the Meissner state introducing dissipation
—flux trapping efficiency
—trapped flux sensitivity
—external magnetic field
H. F. Hess et al., Phys. Rev. Lett. 62, 214 (1989)
Cooldown
Vortex
Vortex lattice

## Slide 3: What is a pinning site?
Pinning sites are material imperfections or defects:
  Normal-conducting and dielectric inclusions
  Grain boundaries
  Dislocations
  Local disorder
Pinning minimization of the system energy
  Vortex = loss in condensation energy
  Defect = weak or not superconducting site
An efficient pinning center has dimension at least comparable to the coherence length
  For niobium
  is the characteristic variation length of the order parameter in the superconductor
Pinning Strength
Vortex
Pinning
center

## Slide 4
Flux Trapping Efficiency—

## Slide 5: Magnetic flux expulsion
Thermal gradient,
Pinning points
Trapped vortices
The strongest pinning point will trap the vortex no matter whether it is on the surface or in the bulk
is a bulk property!

## Slide 6: Thermodynamic force during cooldown (possible explanation)
We can define the thermodynamic force acting on the vortex as:
The Gibbs free energy density defines the stability of vortices in the SC:
Meissner State
Mixed State
Meissner State
Mixed
State

## Slide 7: Critical thermal gradient (possible explanation)
The minimum thermal gradient needed to expel vortices is the critical thermal gradient :
The pinning force acting against the expulsion is defined in terms of critical current density :
Meissner State
Mixed State
Pinning point

## Slide 8: Statistical definition of the trapping efficiency
The probability of expelling vortices with the thermal gradient is
The trapping efficiency is function of :
The trapped field is then:

## Slide 9: Double-peaked probability density function
Double distribution of pinning centers (e.g. dislocations + grain boundaries)
finite probability that vortices are not pinned
First plateau defined by the ratio of the two peaks’ area
Complete flux expulsion reached when is larger enough so that

## Slide 10: Comparison with experimental data
Cavity name | 
CBMM | 0.3
ACC002 | 1.6
Cavity name | 
CBMM | 0.3
ACC002 | 1.6
Magnetization measurements1,2 of niobium and niobium films close to show .
The model returns in agreement with the literature ones:
exp. data: S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
1 G. Park, C. E. Cunningham and B. Cabrera, Phys. Rev. Lett. 68, 12 (1992)
2 L. H. Allen and J. H. Claassen, Phys. Rev. B 39, 4 (1989)

## Slide 11
Trapped Flux Sensitivity—

## Slide 12: Sensitivity vs mean-free-path
Pinning
regime
Flux-flow
regime
  M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)
  exp. data: M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)
Small – pinning regime :
  increases with and , decreases with the increasing of
Large – flux-flow regime :
  decreases with , independent on and

## Slide 13: From pinning to flux-flow regime
1
2
3
4
5
In the pinning regime vortices are constrained by the pinning centers
In the flux-flow regime the vortex oscillation is counteracted by the material viscosity
Pinning
Flux-flow
  M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)

## Slide 14: Sensitivity as a function of pinning point position
1
2
3
4
5
sensitivity is the lowest
constant sensitivity—bulk pinning does not affect the vortex oscillation!
  M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)
is a near-surface property!

## Slide 15
Conclusions

## Slide 16: Conclusions
Trapping Efficiency——bulk property:
  Defined by the opposite action of pinning and Gibbs free energy gradient at the interface between Meissner and mixed states
  Well described by a statistical argumentation
  The higher the thermal gradient, the better the expulsion
  Several types of pinning-effective defect may be involved
Trapped Flux Sensitivity——near-surface property:
  Two regimes of dissipation:
    Small : pinning regime
      vortices are constrained by the pinning centers
      — increases if , and
    Large : flux-flow regime
      the vortex oscillation is counteracted by the material viscosity
      — decreases if , but independent on and
Thank you for the attention