## Slide 1: In-house electrospinning set up for fabricating and designing candidate future high power target material micro-structure
Sujit Bidhar
TSD topical meeting
22 Sep., 2016

## Slide 2: Outline
Background
Objectives
Motivation
Electrospinning process
Setting up electrospinning unit
Candidate target material and microstructure
Summary & Schedule

## Slide 3: Background- Target material
Demand of multi-MW high performance particle production targets
  LBNE 2.3MW proton beam, 1.6X1014 p/pulse
Structural integrity over time
  High temperature, thermal stresses, dynamic stresses
Withstand radiation damage
  Hydrogen embrittlement, radiation corrosion, swelling

## Slide 4: Current Target
ANU/NOvA, 700KWGraphite bars
Proton beam
Beam spot size<<target dimension
Solid continuum high local temperature gradient, thermal stress wave
Water cooling
Water cooling
Can it perform satisfactory at higher energy??

## Slide 5: HPT Issues
Stress waves, thermal shocks
Heat removal
Radiation damage, gas production
Radiation assisted corrosion

## Slide 6: Stress wave
40mm
Radial temperature distribution at end of pulse
Gaussian beam
Sigma 4mm
Prone to fatigue failure (Mode II)
Reduce amplitude, decrease wave speed

## Slide 7: Stress wave (1-D)
ΔL
L
Temperature distribution at end of pulse
Material compression
ΔL=LαΔT
ΔT temp. rise
α Coeff. Thermal expansion
Δt beam pulse duration(heating time)
u displacement
Equilibrium equation
Elastic wave speed
Impulse- Momentum equation
Particle velocity
Initial stress wave amplitude
Design material to have minimize local temp. gradient
High thermal diffusivity/conductivity

## Slide 8: HPT Target material design feature
Material properties
  High thermal conductivity to minimize cyclic loading due to thermal stress wave
  Low Z
  High strength
  Low Young’s Modulus
  High density
Target geometry
  Rotating ,Fluidized, liquid target (Water hammer, thermal stress wave)
  Exfoliated, foam
Alloying elements to mitigate radiation damage, corrosion

## Slide 9: Candidate material- Electrospun nanofiber
Design Microstructure to mitigate issues
Electrospun nano-fiberSinuous target
Electrospun Zirconia nanofiber

## Slide 10: Objective
Fabricate ceramic/metal, composite material nano-fiber with high strength, high density and alloying elements to reduce radiation damage.
  Set up in-house electrospun unit
  Fabricate polymer nanofiber to gain confidence
  Fabricate ceramic composites nanofiber by combining different materials
  Micro-mechanic study single fiber mechanical characterization
  Simulation for fiber damage and thermal-structural analysis

## Slide 11: Advantages & limitations
Advantages:
Discrete continuum at micro scale (broken target) but continuous at meso-scale
  Local damage of single fiber won’t affect target structural integrity as a whole
Reduced thermal stress wave
  Reduced temp. gradient, limited to fiber axis only
  High surface area & gaps  effective local heat removal by passing He gas
Customize material properties by mixing different materials
Limitations:
Widely used for polymer nanofibers
Limited research in ceramics/metal nanofiber
Low density (long target)

## Slide 12: Motivation
Cost: Commercially available set up are expensive (~US$ 50,000 or more)
  Suitable for mass producing nanofiber
  Too much sophistication/automation
Have to depend on supplier for customizing individual part for unconventional electrospinning
Goal is to build electrospin unit under US$7,500
Flexibility of customizing individual parts in house as per need

## Slide 13: Basic electrospinning Set up
10-30 cm
5-10 cm
Process carried out at room temp. and atm. pressure
Collector
Fixed type
Rotating drum type
10-30 KV DC

## Slide 14: Electrospinning Principle
Flat needle
Taylor cone
Slow acceleration
Rapid acceleration
Ohmic flow
Convective flow
+/- KV
Collector plate
Transition liquid to solid
Flow direction
Solid
Liquid
Electrostatic repulsion> surface tension
Droplet is stretched
Jet elongated by whipping action

## Slide 15: Parameters
Molecular weight of polymer
Solution properties (Viscosity, conductivity, surface tension)
Concentration, electrical potential, flow rate
Distance between needle and collector
Needle gage
Ambient temperature, humidity, air flow

## Slide 16: Raw material for electrospinning solution
Polymer
Asphaltene
Nylon
Polyacrylonitrile
(PAN)
Polyvinylepyrrolidone
(PVP)
Solvent
Toluene
Formic acid
N-N,dimethyle-
formamide
Ethanol
Inorganic precursor
Ceramics
TiO2
WO3
Zirconia
Precursors
Titanium(IV) propoxide
Ammonium Metatungstate Hydrate
Zirconium Carbonate
Salt additives
(surfactants)
Fiber diameter
Stable jet length
Morphology

## Slide 17: Ceramics nanofiber fabrication
Inorganic precursor(ceramic+precursor solution)
Polymer solution(polymer+solvent)
Salt additives (surfactants)
Solution for electrospinningpolymer-ceramic nanofiber
Calcination (Heat treatment)
Vaporize polymer
Promotes crystal growth
Bonding
Representative heating profile

## Slide 18
High Voltage Supply: 60 KV, 120 Watt
Programmable syringe pump
Syringes, blunt needles, accessories
Intended electrospinning set up
Syringe pump
Collector plate
High Voltage supply
Needle
Electrospun nano-Fiber Production Set-Up
$ 3600
$ 780
$ 500
Exhaust Fan to duct
Enclosure $ 750
Approx. $ 6000
Space requirement 2’ x 2’ x 2’
Location: MI8

## Slide 19
Electrospun nano-fiber Material Pre-Post Processing set Up
Chemical solution handling set up
Lab Hot Plate with Magnetic Stirrer
Sonicator (Ultrasonic bath)
Beakers, pipets, storing bottles
Gloves, goggles, safety items etc.
Raw materials for nano-fiber
Material specific polymer solution.
Ceramic /material precursor solution.
Post processing- Heat treatment set up
Tube furnace (1500 C) programmable
Thermal gloves, accessories etc.
$ 150
$ 2000
$ 4500
$ 500

## Slide 20: Safety requirements
Electrical Safety
  30KV DC power supply comes with safety features to prevent short circuit, arcing etc.
  Additional safety clearance from ES&H (??)
Raw material storage & handling
  Some chemicals are flammable, corrosive Special cabinet
  Others are in powder /crystal form  general cabinet
  Poisonous if taken orally, may be skin irritant  gloves, apron, goggles
  Magnetic/ultrasonic stirring with some volatile chemicals  Fume hood
Disposal of left over chemicals & processed nanofibers
  Containers
Duct work for exhaust from electrospinning unit
Additional precaution for furnace

## Slide 21: Problems
Beading
Ribbons
Porous globe
Aligned fiber
Troubleshoot
Increase flow rate
Increase polymer concentration or solvent with high evaporation
Salt additives (Surfactant)
Adjust distance between needle and collector
Porosityevaporative characteristic of solvent

## Slide 22: Candidate electrospin nanofiber
Polymer (for Starter)
Nylon 6
Metal/Ceramic
Alumina
Zirconia
WO3
Titania
Graphite
Carbon-nanotube Composite(Ultimate)
CNT-Alumina
CNT-Zirconium

## Slide 23: CNT-ceramics nanofiber composites-advantage
SWNT
1-3 nm
µm-mm
Excellent mechanical properties
E : 1~5 Tpa
Tensile strength : 15-50 Gpa
Elongation % : 16%
High thermal conductivity (axial), insulator lateral
MIT-research
Protects Aluminum metal against
radiation damage
1-D transport network for He to escape
1~2 Vol% CNT
Bulk not nanofiber!!

## Slide 24: CNT-Zirconia/Alumina proposed nanofiber
Ceramic(Zirconia) will have high Z value
Increase bulk density of nanofiber target than pure CNTs
CNT will enhance mechanical strength, provide protection against radiation damage
SWNT
Surfactant
Sonification
deionized water
Add Alumina
+ve charged alumina
Nano-particle
Add polymer
Solution
Electrospin
Calcination/
Heat treatment
CNT filled ceramic nanofiber

## Slide 25: Mechanical characterization
Macro testing electrospun nanofiber mat
Micro testing single fiber
AFM tip
nanofiber
Substrate channel
10-15µm

## Slide 26
Nano-fiber representative Network
microscopic material properties
Mathematical Homogenization through periodic boundary condition
Macroscopic response
Validate model against testing
Change fiber network/material in electrospinning
Thermal stress simulation
Damage model
Check for damage ,i,e. fiber breakage, extent of local plastic deformation
Dynamic stress
Sinuous target material- Mechanical simulation framework

## Slide 27: Summary and Schedule
Detail planning and procurement of a low cost electrospinning set up has been done (~US$6000)
Expected to produce different ceramics, metallic and CNT composites nanofiber
  Methods to fabricate ceramics-CNT composite is in place
Optimize nanofiber parameters to get better material properties
  Macro/micro mechanical characterization and simulations
Schedule