## Slide 1: Study cavity wall material
Conductivity theory predicts the anomalous skin effect
  Copper is the simplest conductor to demonstrate the effect
  How about Aluminum?
    The prediction is made for the BCS theory and it is more complicate than Cu (e.g. anisotropy of the scattering of conducting electrons)
  Presently, high-purity Aluminum is one of the most popular materials to make a quantum computer (QC)
The test used a 11.442 GHz Al Cavity
Purity: 99.999 %
Critical temperature of Al: 1.2 K
Q = 3 108 in Super Conducting RF (SRF)
Q = 105 in Normal Conducting RF (NRF)
Dashed curve is a prediction
Is Al better than Cu
for ADMX?
M. Reagor et al., arXiv:1302.4408v2 (2013)

## Slide 2: Work progress
Made several high purity Aluminum cavities
  99.99% (4N), 99.999% (5N), and 99.9999% (6N)
  Sumitomo Material provided a sample
Collaborate with the QC group at U of Chicago
  UC is interested in a high-Q SRF
    Observe a Q-factor for various SRF materials
    Utilize Fermilab SRF facility to prepare an SRF cavity
    Study a surface roughness vs a Q-factor
    First 4N Al cavity reaches 1.7 108 (Preliminary)
  ADMX is interested in a high-Q NRF
    Measure the Q-factor of a high-purity Al cavity
    in a multi-Tesla magnetic field
    Find a fridge + a multi-tesla magnet
Looking for more collaborator and funding support
  Task is halted because of short money
Clamp
Resonator
Microscopic picture of
the first FNAL Al cavity