## Slide 1
Vikas Jain
DOE Independent Project Review of PIP-II
15 November 2016
HB650 Status

## Slide 2: Vikas Jain
  Bachelor in Mechanical engineer- 1992
  Ph.D. in 2011 from Indian Institute of Technology, Bombay, Mumbai.
  Joined Institute for Plasma Research, Gandhinagar, 1994 (Tokamak research)
  Joined RRCAT, Indore -2001 (Accelerator research);
  Worked for LHC 2002-2005
  Associated with IIFC since 2009

## Slide 3: Outline
HB650 SRF program for PIP-II
HB650 cavities
    RF Simulations
    Coupled Simulations
      LFD, df/dp dependence of cavity on tuner stiffness
    Mechanical Simulations
Fabrication methodology of the SRF cavity
HB650 Tuner Design
HB650 Coupler design
IIFC and FNAL progress
Schedule for HB650 Cavity Dressing
HB 650 Cryomodule status & Schedule
Summary

## Slide 4
b = 0.9
b = 0.9
b = 0.9
b = 0.92
b = 0.92
b = 0.92
Protoype HB 650 Cryomodule will have 3 Fermilab & 3 RRCAT cavities
HB650 R&D Plan

## Slide 5: 650 MHz Design Methodology Adopted
RF Dimension 
Cavity Parameters | HB650
βG | 0.92
bopt | 0.97
R/Q(βG), Ohms | 576
Esurf/E(βG) | 2.1
Bsurf/E(βG), mT/MV/m | 3.94
G, Ohms | 260
Energy gain per cavity MeV | 19.9
HB650 b=0.92  500 MeV to 800 MeV

E-Mag Data

## Slide 6: Coupled Analysis (HB650) for Mechanical Design
2D
3D
RF Domain
Cavity domain

## Slide 7
E Field
H Field
Cavity boundary (mm)
(Pa)
Radiation pressure
Coupled Analysis (HB650) for LFD
Effect of tuner stiffness on
df/dp, LFD and Mech. modes
LFD Analysis
Modal Analysis
Longitudinal Mode #1
T.N. Khabiboulline, et al “Mechanical Optimization of High Beta 650 MHz Cavity for Pulse and CW Operation of PIP-II Project”, THPB014, SRF-2015

## Slide 8
HB650 Loads Cases for
Stress Analysis as per ASME
SCLs
Different loads applicable to cavity
Gravity
Liquid helium pressure head
P2 = 2 bar at room temp. p1=p3=0
Cool-down shrinkage to 2K
P2 = 4 bar at room temp. p1=p3=0
Tuner extension and
Cavity vacuum failure loads p3=1bar
Results
5 load cases with different combination were qualified.
All applicable stress categories have been evaluated at the stress classification lines.
It was found that in all cases the stresses are below the allowable values.
V. Jain, et al “650 MHz Elliptical Cavities for PIP-II Project”, WEB3C003, NAPAC-2016

## Slide 9: Dressed cavity fabrication
Bare Cavity Fabrication & qualification
    The development of bare cavity
    Qualifications consists of leak tests, inspection, and RF QC tests.
    Processing BCP, EP, HPR  VTS testing
Cavity Dressing
    Fabrication of helium vessel, bellow and end transition ring.
    The following tools/fixtures are used for cavity dressing:-
        a. Insertion device (medium bertha) for preparing cavity for dressing.
        b. Rotating fixture to revolve cavity during welding.
        c. Globe box for welding 5-cell 650 cavities in inert atm.
    During the entire fabrication process the dressed cavity RF frequency is monitored and kept within the specified limit.

## Slide 10: Dressed cavity preparation by tack welding
Dressing the Bare Cavity
Titanium Helium Tank
Titanium Transition Ring
Insertion device (medium bertha) for cavity dressing
CAVITY DRESSING STEPS

## Slide 11
Glovebox TIG Welding
TIG Weld #1
TIG Weld #2
TIG Weld #3
Cavity Dressing

## Slide 12
HB 650 MHz Dressed Cavity
Long Cylinder
Transition ring MC end
Transition ring FP end
Bellow assembly
Support lugs
Helium inlet
2-phase pipe assembly
Tuner Support
Lifting lugs
Components of Dressed Cavity same/ similar to LB650 are
MC & FP End groups
Helium vessel (item 1 to 10)
Tuner
Coupler
Magnetic shield
Dressed Cavity in Strong-back
of CM

## Slide 13: Tuner for 650MHz SCRF cavity
Analysis of tuner
Tuning ratio for motor ~ 20
Tuning ratio for piezo ~ 2
Tuner Stiffness ~ 68 kN/mm
Equivalent spring model
Half model of tuner with boundary conditions
Common tuner for LB & HB cavities
*Y.M. Pischalnikov, B. Evgeni, V. Jain, et al,“Testing of the Prototype Tuner for 650MHz SRF Cavities for PIP II Project”, 28th International Linear Accelerator Conference, 25-30 September 2016, East Lansing, MI, USA

## Slide 14: Coupler for HB 650 MHz design
The RF coupler for LB650 and HB650 cavities is same.
Coupler has a single room temperature coaxial ceramic window.
The window diameter is 4’’. Central conductor of the coupler is cooled by air.
S. Kazakov et al., “Design of Main Coupler for 650 MHz SC Cavities of PIP-II Project”, MOPOB24, NAPAC 2016
Current status:
  Electrical, thermal designs are done.
  Mechanical design is done.
  Review is scheduled at the end of November.
  Test stand will be design by Q2 CY17
Main Coupler Port

## Slide 15
650 MHz b = 0.9 Bare cavity work at FNAL
Total 5 bare cavities at FNAL (4 from AES+1 PAVAC)

## Slide 16: HB650 Cavity performance testing at FNAL
*A. M. Rowe, et al , CAVITY PROCESSING AND PREPARATION OF 650 MHz ELLIPTICAL CELL CAVITIES FOR PIP-II, LINAC 2016

## Slide 17: IIFC Progress: 1-cell HB650 (RRCAT)
RRCAT/IUAC Fabricated one Nb HB650 650 MHz single-cell cavity (July 2013).
  Processed & tested at FNAL/ANL
  The cavity achieved Eacc 19.3 MV/m with Q > 4E10 at 2K.
FNAL—Grassellino, Menlnychuk, Sergatskov, et al.
RRCAT -- Puntambekar, et al.

## Slide 18: IIFC Progress: 5-cell HB650 Cavity work at RRCAT
The drawings for 5-cell bare HB650 cavity fabrication were released by Fermilab on 10 February 2016
The drawings for dressed HB650 cavity fabrication and prototype tuners were released by Fermilab on 30 June 2016
Based on these drawings, RRCAT has initiated work on 5-cell HB650 cavity fabrication.
  Prototype mid and end half cells have been formed.
  Components for end group are under machining
  First prototype dumb-bell is fabricated.
HB650 B=0.92 End Group Components
Formed Half cells
1st Dumb-bell B=0.92

## Slide 19: Schedule for 1st HB650 Cavity Dressing at FNAL and at RRCAT

## Slide 20: HB 650 Prototype Cryomodule Status

## Slide 21: Summary
Development of 650 MHz elliptical cavities has been initiated for PIP-II project.
Multi-cell cavity results to date meet current performance specifications, but gap exists with 1-cell performance. Improvements likely with additional processing and testing R&D
FNAL is working on dressing of b=0.9 650 MHz cavity. HB650 B=0.9 Dressed cavity #1 processing and VTS Complete by Sept 17.
RRCAT is working for the development of b=0.92 650 MHz cavity. HB650 B=0.92 Dressed cavity #1 processing and VTS Complete by Sept 18.
Cryomodule for HB650 is being developed jointly.
1st or Prototype HB650 CM will have three b=0.92 650 MHz cavities & three b=0.9 650 MHz cavities.
Fabrication of HB650 CM is to be complete by Q1 of CY2020.
THANKS FOR YOUR KIND ATTENTION

## Slide 22
Backup slides

## Slide 23: Elliptical cavities for PIP-II
HB650 b=0.92  500 MeV to 800 MeV

## Slide 24
Mechanical Analysis
Bottom supported cavity in CM
Maximum shrinkage of cavity due to cool-down to 2K
  1.9 mm at tuner end and
  0.455mm at coupler end.

## Slide 25
BARE CAVITY FABRICATION STEPS