## Slide 1: pCM Comparison
1.3 GHz Production Readiness Review - JLab
Andrew Burrill
Jan 10, 2017

## Slide 2: Outline
Background
Assembly Facilities
Assembly Techniques
Testing Infrastructure
Test Plans

## Slide 3: Background
LCLS-II project goal is to have JLab and FNAL use their unique SRF expertise to deliver equivalent performance cryomodules
Each lab has unique infrastructure and assembly practices that have been developed over the past 15+ years.
It is not practical or cost-effective to try to implement identical facilities and processes for a project of this size.
One of the goals of the pCM testing is to validate the assembly choices and practices at each lab by looking at overall CM performance and if it meets our requirements.

## Slide 4: pCM Minimum Acceptance Test Criteria

## Slide 5: Cavity Vertical Testing
JLab
  Continuous pumping during vertical test – standard at Jlab
  Dedicated dewars (7&8) for LCLS II
  Single cavity per dewar
    Low magnetic field, controlled with compensation coils
    4 dedicated test inserts (identical configuration) equipped with pump systems
    Cavities mounted and demounted in the cleanroom
FNAL
  Active pumping up to right angle valve.
  cavity under static vacuum
  3 dewars available
    Active compensation coils mounted locally around cavity
  2 dewars capable of testing 3 cavities simultaneously
      ~ 5 mG ambient field in this configuration

## Slide 6: Cavity and String Facility Comparison
JLab
Workcenters all under 1 roof
Multiple parallel assembly workstations
Cavity Vertical Testing and CM Testing in same building
FNAL
Workcenters spread over several buildings @ FNAL
  2 buildings for CM Assembly
  1 building for Vertical Testing
  CMTS in separate facility
  HPR and Chemistry facilities at both FNAL and ANL

## Slide 7: JLab Layout for LCLS-II CM Production
Clean Room String Assembly
Phase I CM Assembly (2X)
Phase II CM Assembly (2X)
Vacuum Vessel Installation
Final Assembly / Prep for Testing
CM Testing

## Slide 8: Qualified Cavities Staged for String Assembly
Cavities will be isolated, left under vacuum and installed on the clean room storage rack until all eight are available for assembly of a string. Assembly takes about 1 week.
Each cavity has an HPR prior to mounting on the rail
No N2 purge used during string assembly
Couplers are installed as part of string assembly
Entire string is pumped down for leak check at the end of string assembly
String is left under vacuum

## Slide 9: Cavity String Assembly in Clean Room
Component assembly tooling same as FNAL
“Lollipop” supports for each cavity and BPM subassembly
Lollipops mounted to mobile rail system
Use mobile rail system rather than rail-in-floor used at DESY, CEA/Saclay and FNAL
Transfer to CM assembly rails for cold mass assembly

## Slide 10: JLab Cavity String Assembly – Berry Bolts
Restraint that enables pump down and keep cavity string under vacuum using “Berry” Bolts
Installed outside of clean room during cryomodule assembly phase I

## Slide 11: FNAL – String Assembly
Cavities are mounted with high power coupler and individually leak checked.
Once 4 cavities are mounted with couplers they are assembled into ½ of the string and leak checked.
Positive N2 purge is used during assembly
Once second ½ is ready they are assembled together and leak checked again.
String is back-filled with N2 prior to leaving the cleanroom.

## Slide 12: FNAL LCLS-II Production – CAF-MP9
WS1
WS2
WS0
Staging Area
for WS2

## Slide 13: CAF-ICB during LCLS-II Production
Sick CM
repair area
WS4
WS3
WS5
WS6

## Slide 14: Cryomodule Testing Infrastructure

## Slide 15: JLab CM Testing Infrastructure
JLab has an existing Test cave that has been modified for testing LCLS-II CMs.
  New valve box for connection to CMs
  New Feed cap and End caps fabricated
  8 New SSAs being installed and commisioned
  New RF waveguides installed

## Slide 16: FNAL CM Testing Infrastructure
New CMTS at FNAL has been built and commissioned.
  8 new SSAs have been installed and commissioned
  Installation of all new RF and control cables
  New Feed and End Caps

## Slide 17: CM Testing Differences
FNAL
New Facility with redundancy
  Cold compressor system
  Kinney pump system
Dedicated Cryogenic System
  > 30 g/s capability for cooldown
  Facilitates cooldown studies
Previous experience Testing 1.3 GHz CMs
JLab
Existing Facility
Cryogenic System shared with vertical testing dewars
  8 g/s capacity for cooldown
  Slow and slower cooldown study
Previous experience testing cryomodules for CEBAF, SNS and others.

## Slide 18: Test Plan – collaborative working document ( JLab, FNAL & SLAC)
Includes a laundry list of items.
Each lab has their own approach to satisfy these requirements
  Demagnetization of cryomodule is done at both labs prior to testing
    In the cave at FNAL - Before entering the cave at JLab
Warm RF Measurements
Cooldown to 2K
  Optimize “Fast” cooldown from 45K (FNAL)
  Verify flux expulsion
  Test active magnetic field compensation
Low Power Cold Testing
High Power RF Testing
Thermal equilibrium / Cryogenic load studies
High Q conservation

## Slide 19: pCM in-depth Validation Testing – FNAL ( Genfa Wu)
FNAL has developed a detailed validation test for the pCM that should answer the following questions.
How does the cavity performance vary as a function of cool-down procedure?
  Key to understanding impact of Nitrogen doped cavities and possible trapped magnetic field
Do we need to demagnetize the vacuum vessel and use active magnetic compensation?
How well does the magnetic shielding perform, and was the magnetic hygiene program successful?
How well does the thermal anchoring for the FPC perform?
What is the microphonics spectrum for the LCLS-II CM?

## Slide 20: Transportation Testing

## Slide 21: CM Transportation
All 35 CMs will be assembled, tested at JLab and FNAL and then shipped to SLAC.
They will not be operated at SLAC until all CM are installed in the tunnel.
A single transportation validation test has been developed by to mitigate risk of damage to CM during transport – FNAL design, JLab leading transport test plan.
A new CM transport frame has been designed for the LCLS-II CMs.
Goal to keep vertical shock below 1.5 G and transverse below 0.6 G
  XFEL believes there is a link to field emission and shock load on the CM
  LCLS-II dark current spec is very tight – so this could be important.

## Slide 22: CM transport design – FNAL (McGee)
Images from Mike McGee

## Slide 23: Proposed Shipping Test – under development
Test JLab pCM
  establish performance baseline
Load pCM onto shipping frame, transport given route
  Measure shock, beamline vacuum, etc.
Return to JLab & retest.
If CM performance does not deteriorate shipping test is complete and CMs can begin shipping to SLAC.
If problems are noted remedies and remediation will be developed.
Image from Mike McGee

## Slide 24: Summary
SLAC needs CMs that meet the minimum acceptance criteria
  We care about results.
  The exact method in which they are produced is not as important.
Difference in processes that have delivered the pCMs are well understood. - no show stoppers.
We hope to learn from one another moving forward so we can all benefit.
Excellent communication between labs on all aspects of the project.
  Cavity testing
  Cleanroom practices
  CM Assembly
  CM Testing