## Slide 1: Plans and Advancement in SRF Development for ILC
Akira Yamamoto
on behalf of Shin Michizono
(KEK/LCC)
To be presented at GARD-SRF, Fermilab, Feb. 9., 2017

## Slide 2: Outline
Introduction
Technical Design and Advancement (~ 2016)
Plans toward Realization of the ILC (2017 ~)
Summary
AY-170209

## Slide 3: ILC GDE to LCC
Technical Design Phase
ILC-GDE
2006
‘07
‘08
‘12
‘09
‘10
‘11
‘13
Higgs
discovered
126 GeV
Selection of
SC Technology
TDP 2
Ref. Design (RDR)
LCC
LHC
2004
TDR
1980’ ~ Basic Study
2013.6.12
2012.12.15
TDR publication
‘14
‘15
‘16
‘17

## Slide 4: Global Plan for SCRF R&D
Year | 07 | 2008 |  | 2009 |  | 2010 |  | 2011 | 2012
Phase | TDP-1 |  |  |  |  |  | TDP-2 |  | 
Cavity Gradient in v. test to reach 35 MV/m |  Yield 50% |  |  |  |  |  |  Yield 90% |  | 
Cavity-string to reach 31.5 MV/m, with one-cryomodule |  | Global effort for string assembly and test (DESY, FNAL, INFN, KEK) |  |  |  |  |  |  | 
System Test with beam acceleration |  |  | FLASH (DESY) , NML/ASTA (FNAL) QB, STF2 (KEK) |  |  |  |  |  | 
Preparation for Industrialization |  |  |  |  | Production Technology R&D |  |  |  | 
Communication with industry: | 1st Visit Vendors (2009), Organize Workshop (2010) 2nd visit and communication, Organize 2nd workshop (2011) 3rd communication and study contracted with selected vendors (2011-2012) |  |  |  |  |  |  |  | 
We are here

## Slide 5: Cavity Gradient: Production Yield Progress
- Systematic statistics by C. Ginsburg.
- 2nd pass statistics for 2008 ~ 2012 period:
Production yield: 94 % at > 28 MV/m,
Average gradient: 37.1 MV/m
- Statistics first shown by H. Padamsee, 2008
- Integrated statistics since 2006 ~ 2012
in 2nd pass yield
- Max. gradient achieved: > 45 MV/m

## Slide 6: ILC Acc. Design Overview (TDR)
e- Source
e+ Main Liinac
e+ Source
e- Main Linac
Item | Parameters
C.M. Energy | 500 GeV
Length | 31 km
Luminosity | 1.8 x1034 cm-2s-1
Repetition | 5 Hz
Beam Pulse Period | 0.73 ms
Beam Current | 5.8 mA
Beam size (y) at FF | 5.9 nm
SRF Cavity G. Q0 | 31.5 MV/m Q0 = 1x10 10
Nano-beam Technology
SRF Accelerating Technology
Key Technologies
Physics Detectors
Damping Ring

## Slide 7: ILC Parameters, demonstrated, by 2016
Characteristics | Parameter (Unit) | Demonstrated
Nano-bam: |  | 
ILC-FF beam size (y) KEK-ATF-FF equiv. beam size (y) | 5.9 nm 37 (reaching 41 ) nm | ATF-Collab., KEK-ATF hosted
SRF: |  | 
Average accelerating gradient | 31.5 (±20%) MV/m | DESY, FNAL, JLab, Cornell, KEK,
Cavity Q0 | 1010 | 
(Cavity qualification gradient | 35 (±20%) MV/m) | 
Beam current | 5.8 mA | DESY-FLASH (9 mA Project), KEK-QB, KEK-STF
Number of bunches per pulse | 1312 | DESY
Charge per bunch | 3.2 nC | 
Bunch spacing | 554 ns | 
Beam pulse length | 0.73 ms | DESY, KEK
RF pulse length (incl. fill time) | 1.65 ms | DESY, KEK, FNAL
Efficiency (RFbeam) | 0.44 | 
Pulse repetition rate | 5Hz | DESY, KEK

## Slide 8
Global SRF Collaboration
Europian Collab.
Asian Collab.
America(s) Collab.
FNAL/ANL
Cornell
JLAB
KEK
DESY, INFN
SLAC, LCLS-II
CEA-Saclay, LAL-Orsay
IHEP, PKU
IUAC, RRCAT
TRIUMF

## Slide 9: Advancement in ILC Acc. Technologies, by 2016
Two Key Technologies matured for the project realization !
Nano-beam Technology：
    KEK-ATF2: FF beam size (v): 41 nm at 1.3 GeV (to go 37nm, equiv. to 6 nm at ILC）
SRF Technology ：
    European XFEL: SRF Cavity completion, 100% (800) reaching <G> = ~ 30 MV/m.
      Cryomodule (CM), 100% (100) reaching <G> =~28 MV/m
      Installation into acc. Tunnel completed, and cool-down just started,
    Fermilab： CM (8 cavity string) reaching ILC gradient: <G> > 31.5MV/m
      New Surface process “N2 Infusion” demonstrated for High-Q and High-G
    SLAC, Fermilab, JLab: LCLS-II SRF CM prototypes completed/tested
    KEK: CM (8-cavity string) reaching : <G> > 31 MV/m
    US-Japan: Cost Reduction R&Ds started, reflecting recent technical advances
  Issue and Prospect:
  Cost-reduction efforts, and the ILC energy staging at CE 250 GeV

## Slide 10: European XFEL: SRF Completed
1.3 GHz / 23.6 MV/m
800+4 SRF acc. Cavities
100+3 Cryo-Modules (CM)
Progress:
2013: Construction started
2015: SRF cav. (100%) completed
CM (70%) progressed
Further Plan:
2016: E- XFEL acc. completion
2016/E: E-XFEL beam to start
Acc. : ~ 1/10 scale to ILC-ML
SRF system: ~ 1/20 scale to ILC-SRF
XFEL
DESY
XFEL site
DESY
Media.xfel.au, Dec. 2015
1 km SRF Linac
10
Nick will present the stepping-stone progress

## Slide 11: E-XFEL: SRF Cavity Performance (as received)
SRF cavity production/test ；
# RI Cavities, 373 (as of Sept. 2015)
    Final process: 40 mm EP.
      w/ same recipe to ILC-SRF’s
    Tested at DESY-AMTF
Notes:：
    “Ultra-pure water rinsing as the 2nd process improving the gradient performance (> ~10%) for lower-performed cavities (not shown here).
N. Walker, D. Reschke, SRF’15
G-max
G-usable
 | G-usable (Q0> 1010 ) | G-max | (ILC)
<G> MV/m | 29.4 | 33 | (35)
Yield at 28MV/m | 66% | 86% | (90%)
Nick will present the stepping-stone progress

## Slide 12
No degradation, after ~ XM54
O. Napoly, TTC2016

## Slide 13
Fermilab：CM2 reached <31.5 MV/m >
Cryomodule test at Fermilab reached < 31。5 > MV/m, exceeding ILC specification
E. Harms, TTC2014
ILC Milestone
31.5 MV/m

## Slide 14: New Surface Process recently demonstrated at Fermilab, “N2 Infusion at 120 C”
N2 infusion at 120 C directly after heat treatment at 800 C,
Same cavity, sequentially processed, no EP in b/w
Achieved: 45.6 MV/m Q at ~ 35 MV/m : ~ 2.3e10
A. Grassellino, S. Aderhold, TTC-2016

## Slide 15: KEK-STF: Cavity/CM Performance, and RF and Beam Test Preparation
FY14: CM1+CM2a (8+4) assembly
FY15: Cavity individually tested in CM
RF power system in preparation
FY16: 8-cavity string to be RF tested
FY17: Beam Acceleration expected
（to reach > 250 MeV )
SRF cavity Gradient (MV/m) before/after CM Assembly |  |  |  |  |  |  |  |  |  |  |  | 
Module | CM1a |  |  |  | CM1b |  |  |  | CM2a |  |  | 
Cav. # | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12
V. Test (CW) | 37 | 36 | 38 | 36 | 37 | 35 | 39 | 36 | 12 | 36 | 32 | 32
in CM (pulse) | 39 | 37 | 35 | 36 | 26 | 16 | 26 | 32 | 18 | 34 | 33 | 32
 | Gradient stable |  |  |  | Degraded |  |  |  | Gradient stable |  |  | 
*<G> ： 30 MV /m (12 Cav.) , 35 MV/m (best 8)
Y. Yamamoto, E. Kako, H. Hayano

## Slide 16
8 Cavities tuned on resonance by piezo with
vector-sum operation at 31MV/m.
8 Cavities Operation by Vector-Sum @31MV/m (2016)

## Slide 17: KEK 9-Cell Cavity (KEK-01/02)reached 36/38 MV/m
KEK-01 (Rolled, FG, 2014): Reached 36 MV/m
KEK-02 (Ingot-sliced, LG, 2016): Reached 38 MV/m
Chart: Eacc[MV/m]
| 1.01 | 1.98 | 3.01 | 4.04 | 5.04 | 6.34 | 7.07 | 8.08 | 9.08 | 10.01 | 11.03 | 12.03 | 13.05 | 14.01 | 15.04 | 16.02 | 17.03 | 18.05 | 19.05 | 20.02 | 21.19 | 22.04 | 23.03 | 24.04 | 25.0 | 26.13 | 27.0 | 28.0 | 29.01 | 30.04 | 31.02 | 31.99 | 32.99 | 34.01 | 35.01 | 35.98 | 36.91 | 37.77
KEK-2(1.5~1.95K) | 25500000000 | 31000000000 | 34400000000 | 36100000000 | 37100000000 | 37500000000 | 37600000000 | 37500000000 | 37200000000 | 36800000000 | 36100000000 | 35200000000 | 34400000000 | 33400000000 | 32400000000 | 31300000000 | 29300000000 | 28300000000 | 27300000000 | 26300000000 | 25200000000 | 24400000000 | 23500000000 | 22400000000 | 21500000000 | 19800000000 | 19000000000 | 18100000000 | 17200000000 | 16600000000 | 15200000000 | 14500000000 | 13700000000 | 12900000000 | 12200000000 | 10900000000 | 9980000000 | 8940000000
KEK-1(1.6-1.8K) | 15900000000 | 17300000000 | 17700000000 | 17900000000 | 17900000000 | 17700000000 | 17600000000 | 17300000000 | 17000000000 | 16600000000 | 16100000000 | 15500000000 | 15100000000 | 14800000000 | 14300000000 | 14000000000 | 13800000000 | 13500000000 | 13300000000 | 13000000000 | 12700000000 | 12400000000 | 12000000000 | 11600000000 | 11200000000 | 10900000000 | 10500000000 | 10200000000 | 9680000000 | 9250000000 | 8840000000 | 8700000000 | 8480000000 | 7960000000 | 7630000000 | 7460000000 | 7050000000 | 6640000000 | 6170000000 | 5950000000

## Slide 18: Outline
Introduction
Technical Design and Advancement (~ 2016)
Plans toward Realization of the ILC (2017 ~)
Summary
AY-170209

## Slide 20: KEK-ILC Action Plan Issued, in Jan. 2016 https://www.kek.jp/en/NewsRoom/Release/20160106140000/
 | Pre-Preparation Stage | Main Preparation Stage |  |  | 
 | present (we are here) | P1 | P2 | P3 | P4
ADI | Establish main parameters | Verify parameters w/ simulations |  |  | 
SRF | Beam acc. with SRF cavity string, Cost Reduction R&D | Demonstrate mass-production technology, stability, hub-lab functioning, and global sharing |  |  | 
Nano-beam | Achieve the ILC beam-size goal | Demonstrate the nanobeam size and stabilize the beam position |  |  | 
e+ | Demonstrate technological feasibility | Demonstrate both the undulator and e-driven e+ sources |  |  | 
CFS | Pre-survey and basic design | Geology survey, engineering design, specification, and drawings |  |  | 

## Slide 21: Fraction of SCRF Cavity and CMs
Cavity and CM :
35 %
Cryogenics:
8 %
HLRF
10 %

## Slide 22: SRF Mini-Workshop, 6 Dec. 2016 Motivation In view of the worldwide interest and the limited resources available for R&D on SCRF and its associated technologies, it is important to have a clear view of the priorities in each of the laboratories participating in SCRF R&D on a timescale of the next 2-3 years.
Introduction L. Evans
Plans at:
Fermilab N. Solyak
JLab B. Rimmer
DESY W-D. Moeller
INFN-LASA C. Pagani
CEA-CNRS O. Napoly
KEK S. Michizono
IHEP J. Zhai
CERN E. Jensen
TRIUMF B. Laxdal
(Cornell) (F. Furuta)
Plans for Associated Systems:
Input-coupler R&D Y. Yamamoto
Tuner R&D M. Yamanaka
(Y. Psichalnikov)
Crab-cavity R&D Y. Yamamoto
Marx-Modulator R&D M. Akemoto
Klystron R&D (I. Syratchev/
E. Jensen)
Discussions: All

## Slide 23: World-wide R&D Plans in a few years Discussed in Mini-WS. LCWS2016, Morioka
 | Project | SRF Cavity | Assoc. | CM | RF
Fermilab | LCLS-II | N2-infusion (HQ-HG) | Coupler |  | 
JLab | LCLS-II | Nb-LG/FG (sliced/rolled) , N2-infusion |  |  | 
DESY | EXFEL | N2-infusion Nano-Lab study |  | High-perform. CM | 
INFN-LASA | ESS | Nb-LG/FG study for ESS |  |  | 
CEA CNRS-LAL | IFMIF ESS, SARAF | Vertical EP (VEP), N2-Infusion | Mag.shield Coupler | Assembly robotizing | 
KEK | STF | Nb-LG/FG N2-infusion | Coupler, Tuner, C C. |  | Marx M.
IHEP | ADS | N2-infusion, In dustrialization |  | Industrial. | Marx M. h.e. Klystron
CERN | HL-LHC Hi-Isolde | Thin-film (Nb on Cu) | Coupler |  | h.e. Klystron
TRIUMF | ISAS-II, ARIEL | VEP, muSR |  |  | 
(Cornell) |  | N2-infusion, VEP |  |  | 

## Slide 24: A plan for ILC Cost-Reduction R&D in Japan and US focusing on SRF Technology, in 2~3 years
Based on recent advances in technologies;
  A1: Nb material preparation (2~3%)
  - w/ optimum RRR and clean surface
  A2: SRF cavity fabrication for high-Q /G (8~9%)
  -w/ a new baking recipe provided by Fermilab
  A3: Power input coupler fabrication (~1.5%)
  - w/ new (low SEE) ceramic without coating
  A4: Cavity chemical process (~1.5%)
  - w/ vertical EP and new chemical (non HF) solution
  Others (Tuner Optimization to be discussed, …)
S. Michizono, S. Belomestnykh

## Slide 25: Cost Reduction Estimate w/ Nb and High-Q&G (at KEK)
Cost Fraction | Cavity-CM (reduced to 90%) | CFS-tunnel (reduced to 90%) | HLRF (~ const.) | Cryog. (see note) | Fraction to ILC total Cost
Cost Reduction Fraction Nb-Material: Surface Process |  |  |  |  | 2 ~ 3 % 8 ~ 9 %-a
TDR : E= 31.5 MVm Q = 1.0e10 - w/ 2nd-EP | 0.38 | 0.16 | 0.10 | 0.07 *1 | 0.71 (
Hi-G, Hi-Q : E= 35.0 MVm Q = 1.6e10 ( 2 x 0.8e10) - w/o 2nd-EP | 0.34 - ( 0.01 ~0.015) | 0.14 | 0.10 + a | 0.057 *2 | (0.637) 0.627 ~ 0.622+a
Note: *1: ML Cryogenics fraction is 0.08 – 0.01 = 0.07 (0.01 for for other cryogenics of Sources, DR, BDS etc). *2: Cryo: cost reduction; Effective saving of the cryogenics capacity down to 1/1.6 with improving Q for dynamic loss  0.625 Breakdown: static (constat) 0.07 x ~ 0.2 = 0.014 dynamic (reduced) 0.07 x ~ 0.8 x 0.625 = 0.035 ---------------------------------------------------------------------- sum: = 0.049 Relative cryogenic power ratio: 0.049 / 0.07 = 0.7 ( Cryogenics power to be reduced to 70 %). Conversion to the Cryogenics cost (following power-index of (^0.6)  0.7^0.6 = 0.81 ( Cryogenics cost to be reduced to 81 %) Cryogenics cost fraction in Hi-G, Hi-Q  0.07x 0.81 = 0.057 ( caving fraction: 0.013) |  |  |  |  | 
ILC Cost Reduction Proposal 160711b

## Slide 26: ILC cost reduction – proposed SRF R&D at FNAL
Working groups at FNAL and KEK identified several important R&D pathways for the ILC cost reduction, and grouped them under short (3 years), medium (5 years) and long (10 years) term efforts.
The table below presents the proposed R&D timeline for cost reduction on which FNAL will focus, while KEK will focus on cost reduction of cavity material, fabrication and chemical processing as well as on synergetic with FNAL efforts on improving cavity high Q / high gradient and input couplers.

## Slide 27: A1: Niobium material preparation
~ 50% off
Ingot
Sheeting / tubing
(forging, rolling, slicing, tube forming)
Ingot
(RRR optimization
Slicing.
Motivation
Niobium material cost for fabricating SRF cavity cell and end-groups is relatively high.
If the ingot purity and manufacturing method for each part is optimized precisely as well as satisfying the ILC specification shown in the TDR, the cost will be reduced significantly.
Approach
Optimize the ingot purity with a lower residual resistivity ratio (RRR) with accepting specific residual content.
Simplify the manufacturing method such as forging, rolling, slicing and tube forming with
small loss.

## Slide 28: FG-Nb rolled or LG-Nb sliced from Ingot
Cleanness highly secured
Courtesy: G. Myneni
50 mm

## Slide 29: A1: R&D plan for Nb materialCavity
JFY2017:
Production of total 4 three-cell cavities
  High Ta medium RRR（100〜200）material
  High Ta high RRR（200〜300）material
Evaluation of these cavities from the view points of material cost, chemical cost, etc.
Selection of the material JFY2018,2019:
Production of 8 nine-cell cavities (satisfying the high pressure regulation)
Material optimization of end-group (including HOM coupler)
Chemical processing, vertical test
20
Schedule
2016
2017
2018
2019
KEK
Masashi
Yamanaka
Feasibility study using 4x3-cell cavities (ongoing)
Preparing materials
Shin MICHIZONO, ACFA, Jan.19 2017
Evaluation
Manufacture
8x9-cell cavities(Vertical&Horizontal tests)

## Slide 30: A2: R&D plan for High-Q High-G
LCWS2016 SRF Shin MICHI
ZONO
18
2016:
Single-cell KEK-cavity processing at FNAL
Q-measurement (with residual magnetic field dependence) at FNAL
Q measurement at KEK (to confirm the measurement system configuration)
2017:
New single-cell cavity production
Processing at small vacuum furnace
Procurement of new vacuum furnace for 9-cell cavity
2018:
High-Q High-G processing to 3 nine-cell cavity
Production of 8 nine-cell cavities 2019：
Performance test
Preparation of the installation to STF-2
2016 2017 2018 2019
KEK
Hitoshi HAYANO
8 - 9cell cavities fabrication
3-9cell performance
Preparation of vacuum furnace
1 cell processing
FNAL process
Performace test
Performaｎce test
Preparation for cyromodule

## Slide 31: A-3. Power input coupler fabrication
Schedule
2016
2017
2018
2019
KEK
Design
Evauation of ceramic
(on going)
Manufacturing
High power test
#2 Manufacturing
High power test
Manufacturing For cyromodule
Collaboration with FNAL
By innovating the ceramic window material, we will try to make the coupler without additional surface treatment on the ceramic leading to the cost reduction.
Material cost (including Cu plating) in cavity input coupler is rather high. We will review the
materials and Cu plating procedure.

## Slide 32: Coupler Development with low-SEE coefficient ceramic window
TTF-III/E-XFEL Coupler
New, KEK-STF Coupler
 | STF-40-A | STF-40-B*
Cold end-flange | 40 mm | 40 mm
Ceramic window | A479 | AH100A
SEE coefficient | 11.2 | 4.6
Coating | yes | no
Conditioning time | 86 hrs | In progress
Plug-compatible,
cold-interface
w/ bellows
w/o
bellows
40 φ
40 φ
* CERN-KEK Cooperation

## Slide 33: A-4. Cavity chemical treatment
The change of the SC-cavity chemical treatment, from horizontal EP and sulfuric acid + HF
(TDR) to vertical EP (VEP) + non-HF solution + bipolar EP.
VEP
with wing-cathode
Bipolar EP
using non-HF solution

## Slide 34: Tuner: LCLS II SRF Tuner developed by FNAL
DESIGN OPTIMIZATION (compatible to ILC tuner)
Mechanical size limitations must fit on the “short-short” cavity (DESY tuner can fit only on “short-long” ).
Location of the piezo. Piezo stroke translate directly to the cavity (At DESY design only ½ of piezo stroke going to cavity). Piezo preloaded inside encapsulation.
Robust/Low cost tuner frame design.
Features that must prevent loosening of the tuner part during 20 years operation (20 thermo-cycles).
Design elements that allow to replace active elements of tuner without dis-assembly tuner.
NEW ACTIVE COMPONENTS:
  Electromechanical actuator (stepper/gear/spindle) designed by Phytron per FNAL specs (LVA 52-LCLS II-UHVC-X1)
  Piezo tuner- encapsulated piezo-stack designed by PI per FNAL specs (PI-885.51)
Y. Pischalnikov et al., “Design and Test of Compact Tuner for Narrow Bandwidth SRF Cavities.” In Proc. IPAC2015, Richmond, VA, USA.
Y. Pischalnikov et al., “LCLS II Tuner Assembly for the Prototype Cryomodule at FNAL.” In Proc. NAPAC2016, Chicago, IL, USA.
Y. Pischalnikov

## Slide 35
Saclay (lever) tuner for TESLA/EXFEL cavity
KEK 早野さんのスライドより

## Slide 36: Cost reduction R&D Plan at KEK
 | 2018 | 2019
A-1： Nb material | 4 3-cell cavity Vertical test | 8 9-cell cavity VT
A-2： HighQ,HighG | 5 single cell cavity 3 9-cell cavity VT | 8 9-cell cavity VT
A-3： Input coupler | Coupler design | Evaluation
A-4： Vertical EP | Single cell cavity test | 9-cell cavity test
Assumption）
R&D budget expected to be available from JFY2018 (April, 2018~)
R&D starts from JFY2017 within the KEK-LC budget (by reducing outsourcing )

## Slide 37
Coupler: Cost reduction by no-coating ceramics
Tuner: Cost reduction by revised lever-arm tuner
Crab cavity: Concern item in Nomura-report
MARX modulator:
Concern item in Nomura-report
KEK plans for components study

## Slide 38: ILC Staging to be studied
 | Unit | ILC |  | 
CoM. Energy | GeV | 250 | 500 | 1,000
Site Length | km | ~21 | 31 | 50
Luminosity | 1034 cm-2s-1 | 0.82 | 1.8 | 3.6
Acc. Gradient | MV/m | 31.5 | 31.5 | 31.5/45
Res. Frequency | GHz | 1.3 | 1.3 | 1.3
Repetition rate | Hz | 5 | 5 | 4
IR, v. beam-size | nm | 7.7 | 5.9 | 2.7
Beam Power | MW | 2 x 2.9 | 2 x 5.2 | 2 x 13.6
AC Power | MW | 129 | 163 | 300
Value Cost in TDR | BILC | TBD | 7.98 | TBD

## Slide 39: ILC Staging Options
TDR: 500 GeV
Staging: 250 GeV
Option F
(Case 2)
Option E
(Case 2)
Option D
Option C
(Case 1)

## Slide 40: Options for Staging at 2x125 GeV
 | ACC. [GeV] | Tunnel [GeV] | Feature
TDR | 2 x 250 | 2 x 250 | TDR-2013
TDR - updated | 2 x 250 | 2 x 250 | ML tunnel width 11  9.5 m, & center-wall 3.5  1.5 m Detector hall access w/ vertical shafts No ML-tunnel extension (of 1.4 km), respecting G-upgrade
Opt. F (Case 2) | 2 x 125 | 2 x 250 | ML distributed + Full (air-conditioned) tunnel  Beam transport line cost (to be added)
Opt. E (Case 2) | 2 x 125 | 2 x 250 | ML upstream + Full (air-conditioned) tunnel  Beam transport line cost (to be added)
Opt. D | 2 x 125 | 2 x 250 | Simple (no air-conditioned empty tunnel + ML downstream  RTML, Circular/U-turn Tunnel duplicated
Opt. C (Case 1) | 2 x 125 | 2 x 125 | Min. 2 x 125 GeV w/ no add. tunnel for H.E. extension Minor additional tunnel (~ 500 m) included for future energy-upgrade work, to be possible in parallel to the continuous 250 GeV run.

## Slide 41: Summary
ILC prepared for an e+e- collider, CE 500 GeV, extendable to 1 TeV.
Nano-Beam technology demonstrated at ATF hosted at KEK
SRF Technology advanced, and, particularly, demonstrated at E- XFEL for mass-production, and at Fermilab for High-Q and High-G.
Cryogenics & Civil Eng/ works advanced, reflecting CERN-LHC exp.
Cost Reduction R&D work required for SRF technologies, reflecting recent technology progress,
    Short term (2~3 years) : Cavity and associated components R&D for 10 ~ 15 % reduction
    Long term (5~6 years): RF power system Efficiency to be improved
Study of the energy staging, at C.E. 250 GeV, to be studied for the project sooner.
    > 1/3 cost reduction for the project starting to be anticipated.

## Slide 42: backup

## Slide 43: US-Japan cost reduction R&D

## Slide 44: SRF Cavity and Cryomodule Fabrication Process
Purchasing Material/Sub-component
Manufacturing Cavity
Processing Surface
Assembling LHe-Tank
Qualifying Cavity
Cryomodule Assembly
Cavity String Assembly
Qualifying CMs
16,024 x 1.1
1,855

## Slide 45: Standard Procedure Established
 | Standard Fabrication/Process
Fabrication | Nb-sheet purchasing
 | Component Fabrication
 | Cavity assembly with EBW
Process | EP-1 (~150um)
 | Ultrasonic degreasing with detergent, or ethanol rinse
 | High-pressure pure-water rinsing
 | Hydrogen degassing at > 800 C
 | Field flatness tuning
 | EP-2 (~20um)
 | Ultrasonic degreasing or ethanol (or EP 5 um with fresh acid)
 | High-pressure pure-water rinsing
 | Antenna Assembly
 | Baking at 120 C
Cold Test (vertical test) | Performance Test with temperature and mode measurement
Key Process
Fabrication
Material
EBW
Shape
Process
Electro-Polishing
Ethanol Rinsing or
Ultra sonic. + Detergent Rins.
High Pr. Pure Water cleaning

## Slide 46: Standard Procedure Established
 | Standard Fabrication/Process
Fabrication | Nb-sheet purchasing
 | Component Fabrication
 | Cavity assembly with EBW
Process | EP-1 (~150um)
 | Ultrasonic degreasing with detergent, or ethanol rinse
 | High-pressure pure-water rinsing
 | Hydrogen degassing at > 800 C
 | Field flatness tuning
 | EP-2 (~20um)
 | Ultrasonic degreasing or ethanol (or EP 5 um with fresh acid)
 | High-pressure pure-water rinsing
 | Antenna Assembly
 | Baking at 120 C
Cold Test (vertical test) | Performance Test with temperature and mode measurement
Key Process
Fabrication
Material
EBW
Shape
Process
Electro-Polishing
Ethanol Rinsing or
Ultra sonic. + Detergent Rins.
High Pr. Pure Water cleaning
N2 infusion at 120 C directly after heat treatment at 800 C

## Slide 47: Cryogenics Layout with Further Safety and Conserving He Resource