## Slide 1
Cost Reduction of Cavity Processing
  HF- free electropolish
    “Pulse-reverse,” “cathodic polishing”, “bi-polar polishing”
    Faraday Technology, Inc. patents (model SBIR effort)
      5% sulfuric acid – demonstrated high performance single-cell and multicell success
      Sodium hydroxide
      …
  JLab collaborations with Faraday Technology & KEK/Nomura Plating
    Small sample R&D – parameter analysis
    Translating to single and multi-cell cavities
      VEP chem cabinet and pulse power supply now commissioned within our cleanroom suite (switching kiloamps)
      Effort presently funding limited
C. Reece & H. Tian
Objective: Lower the cost of industrial processing of Nb cavities
  Safer, greener chemistry - eases industrialization
  “Vertical” processing – reduced touch labor, amenable to automation