## Slide 1: Cut Cavity Materials and Cavity Fabrication Costs
New cavity materials
  Nb-Cu composite
New fabrication methods
  Hydroforming
  Spinning

## Slide 2: Cavity Material-Cost Reduction
Cost of bulk niobium is a major factor for SRF accelerators
  especially for low frequency (<650 MHz)
  the required Nb per cell scales as 1/f2.
Propose Cavity cost reduction via Nb-Cu Composites
  Nb 1 mm/Cu 4 mm,
  X5 reduction over Nb
  Material can be made by explosion bonding Cu with high RRR Nb
1-cell and 3-cell cavities made by DESY, KEK
  Proof of principle to 40 MV/m established

## Slide 3: Cavity Fabrication-Cost Reduction via Seamless Techniques with Nb-Cu Composites
Eliminate expensive e-beam welding and trim machining of parts
High quality surface preparation possible
  as with bulk Nb cavities that show high performance
Rapid production rate
Hydroformed and Spun 1-cell cavities already proven
  Hydroformed 3-cells Nb proved to > 35 MV/m
  Spun single cell Nb proved to 40 MV/m
  Spun 3-cell Nb under test at FNAL
Collaboration with INFN, DESY, and KEK, US industry

## Slide 4: Principles of Hydroforming and Spinning

## Slide 5: Proof of Principle 1-cell Nb-Cu Composite Hydroformed Reaches 40 MV/m

## Slide 6: 2-cell Nb-Cu Hydroformed

## Slide 7: 500 MHz Single Cell Spun from Nb-Cu Sheet

## Slide 8: 9-cell Nb Cavity Made by Spinning

## Slide 9: Proof of Principle for Spinning 1.3 GHz Single Cell Nb Spun Cavity – 40 MV/m

## Slide 10: 3-cell Cavity Made From Nb Tube By Spinning At INFN
T=2K
Test at FNAL
Eacc 34 MV/m

## Slide 11: Hydroformed 3-cells Welded into 9-cells 30 – 35 MV/m Proved

## Slide 12: 1300 MHz Nb-Cu Composite Cavities Reach 40 MV/m

## Slide 13: Scenario of cost reduction Cost evaluation of Nb/Cu clad seamless cavity The present cost considering effect of mass production is still higher than expected level
KEK Existing
Relative cost
ILC Mass production
Nb/Cu Clad
seamless
Nb/Cu Clad Seamless
Nb bulk Cavity
By T.Fujino Ph.D Thesis 2003

## Slide 14: Nb-Cu Composite Cavity Material & Seamless Fabrication Cost Reduction Plans
Short term
  Fabricate, process, and test 1-cell 650 MHz Nb-Cu composite cavities via spinning
  Thinning/delamination at beam tubes controlled by die selection and larger area for starting material
Medium term
  Fabricate and test multicell composite cavities
Long term
  Involve industry for mass-production
  Apply High Q treatment to Nb-Cu composite cavities
    Lower temperature of N-doping