## Slide 1: Expected impact for improved EP technique, such as Vertical EP or HF free EP
Fumio Furuta, Matthias Liepe, Cornell

## Slide 2: Expected impact for improved EP technique, such as Vertical EP or HF free EP
Potential/impact:
  VEP:
    Simplified integration with other processing steps
    Simplified infrastructure (reduced facility costs)
  HF-free
    Reduced environmental impact
    Lower risk (no HF)
    Higher performance ?

## Slide 3: Expected impact for improved EP technique, such as Vertical EP or HF free EP
Current status:
  9-cell VEP high Q, high gradient demonstration at Cornell
  HF-free EP single cell high gradient performance demonstration (Faraday, FNAL)
  Ongoing R&D programs at Cornell, Faraday, JLAB, KEK
    Faraday/Cornell: first 9-cell scale HF-free, bi-polar VEP done

## Slide 5: Expected impact for improved EP technique, such as Vertical EP or HF free EP
Next steps / suggested development program :
  R&D program on pulse-reversed (bi-polar) vertical polishing
    Explore HF-free electrolyte (e.g. 5-10 wt% H2SO4 in H2O) and acid-free salt-based electrolyte.
      Study surface chemistry
      Optimize process
    Transfer to 9-cell cavities and study high-field, high Q performance
      Demonstrate reproducibility and high yield on 9-cell cavities