## Slide 1: Introduction to Cost Reduction Session
Goal of session
  Pathways for future cost reduction
Context for cost reduction
  Impact to HEP accelerators at the energy and intensity frontiers
  Near term (5-10 year), Medium term (10 - 15 year) , Long term (20 + year).
Energy Frontier e+e-
  ILC 250 GeV – 1 TeV,
  FCC (90 GeV - 350 GeV e+e-), CEPC (240 GeV)
Energy Frontier hh
  FCC (100 TeV), CEPC (50 – 70 TeV)
Intensity Frontier: Neutrinos
  PIP-II (0.8 GeV, 1.2 MW)
  PIP-III (0.8 – 3 GeV, 3 – 8 GeV, 2. 5 MW+)
  3 – 8 GeV mostly ILC-like 1.3 GHz

## Slide 2: Promising Paths, Present Status Short & Mid-Term, Gradient, Q,
High Gradient, High Q, Niobium
  Prospect for cost reduction @ 35 MV/m, Q = 2x1010, 10% below TDR-ILC
  Prospect for cost reduction @ 40 MV/m, Q = 2-3x1010, 15%
  N-infusion
    Proof-of-Principle: 45 MV/m, Q = 2x 1010 , Single Cells, Nb
    Multicells next
  Advanced shapes: Low-Loss (Ichiro), Low-Surface-Field (LSF), Re-entrant
    Proof-of-Principle: 50 – 55 MV/m, Q = 1010 , Single Cells, Nb
    Multicell
      Low-Loss, Jlab upgrade cavity) 43 MV/m, limited by FE
      Ichiro 9-cell limited to 40 MV/m, limited by FE
Field Emission Reduction
  High gradient=> High Epk
  FE increases exponentially with Epk
  Need improved surface treatments?
    Improved HPR, Plasma processing?, High Power Pulsed RF processing (HPP)
    Proof of Principle HPP 10 => 25 MV/m
  Recovery in cryomodules
    HPP regularly used with available beam power to condition modules
    Improvement needs to be cataloged

## Slide 3: Potential ILC cost reduction
A cost model based on the ILC TDR and new progress in the SRF technology on cavity achievable efficiency (Q) and acceleration (Eacc), showing potential cost reduction up to 20%.

## Slide 4: Component Cost Reduction
Material Cost Reduction
  Large Grain Nb
    Savings Prospects 30 - 50% x sheet material cost
    Proof-of-Principle, 9-cell @ 45 MV/m , Q= 1010
    Many 9-cells, 7 in Cryomodule tested in FLASH
  Niobium-Copper composite material, plus spinning or hydrforming
    Savings prospects: Nb cavity cost reduced by x 3
    Proof-of-Principle: Single cells, 40 MV/m, Q= 1010
  Niobium Films on Copper
    Proof of principle 15 – 20 MV/m, Q-slope
Fabrication Cost Reduction
  Seamless cavities via Hydroforming, Spinning, Hydroforming/welding
  Proof of principle, 3 cell Nb, 9-cell (3x3-cell), 35 MV/m

## Slide 5: Component Cost Reduction (Con’t)
Simplify Chemical treatment
  Prospects 30% reduction
  Vertical EP
    Proof of Principle 30 – 35 MV/m for 9-cells
  HF-Free EP
    Proof of principle 30 – 40 MV/m for single cell
Reduce cost of auxiliary components
  Input coupler
    Prospect 30% reduction
    Separate Working Group
  Cryomodule

## Slide 6: Summary of Overall Potential ILC cost reduction (relative to TDR value)
Gradient & Q: 10 - 15%
Material Large Grain: 2-3 %
(Material Nb-Cu: 3 - 4%)
Chemical Processing: 1.5%
Coupler 1.5%
Total 15 – 22%

## Slide 7: Promising Paths, Long-Term
Nb3Sn
  Prospects: 80 MV/m
  Proof of Principle: 18 MV/m
Multi-Layers
Other Transformational SRF R&D
  Separate WG