## Slide 1
The next technologies
Dirty high Hc superconductor ()
eg., Nb3Sn
Clean Nb
The fourfold benefit of the layered structure will improve the maximum Eacc and Q0 : (1) the reduction of gap is small in the dirty layer
(2) suppress the surface current and enhance the theoretical field limit
(3) prevent the vortex penetration by the additional barrier . SIS structure is thought to provide with a further robust barrier and reduce vortex dissipation.
(4) In addition, dissipation decreases and Q increases because a part of current flows on the low loss surface (eg, Nb3Sn).
Dirty Nb ()
Clean Nb
Clean Nb
insulator
(Present technology)
Dirty Nb on clean Nb
(Next technology) SS structure
SIS structure

## Slide 2
F. P-J. Lin and A. Gurevich, Phys. Rev. B 85, 054513 (2012)
A. Gurevich, Rev. Accel. Sci. Technol. 5, 119 (2012)
Gap under a current (narrow!)
clean
dirty
Gap under a current
(wider than clean case!)
①
Since excited quasiparticles increase and contribute to the surface resistance as the gap decreases, a larger gap is desired. The gap in the dirty layer is rather well behaved at a high field!
→ cure the high field Q drop
Note here Bc1 is a bulk property and given by the bulk clean SC:
Bc1～170mT remains after layered.
Becomes gapless before arriving at
the superheating field!

## Slide 3
②
The surface current is suppressed.
The current suppression means an enhancement of the field limit, because the theoretical field limit is determined by the current density.
The gap reduction due to the current is further prevented.
λ1 (> λ2)
λ2
SS case:
T. Kubo, in Proceedings of LINAC2014, p. 1026, THPP074.
SIS case:
T. Kubo et al., Appl. Phys. Lett. 104, 032603 (2014).
A. Gurevich, AIP Advance 5, 017112 (2015).
S. Posen et al., Phys. Rev. Applied 4,044019 (2015).
This slope corresponds to the current density.
The surface current is suppressed!
Bs of Nb3Sn
Bs of Nb
This is SIS case.
SS case is similar.
Figures from T. Kubo, Supercond. Sci. Technol. 30, 023001 (2017)

## Slide 4
superconductor side
Bean-Livingston
barrier
Vacuum side
In SS case, vortices are expelled by the boundary if λ(layer)> λ(bulk). (left figure)
T. Kubo, in Proceedings of LINAC2014, p. 1026, THPP074.
M. Checchin et al., in Proceedings of IPAC2016, p. 2254, WEPMR002
In SIS case, vortices disappear at the insulator.
A. Gurevich, AIP Advance 5, 017112 (2015).
③
See also T. Kubo, Supercond. Sci. Technol. 30, 023001 (2017)

## Slide 5
If the surface layer has a lower surface resistance than the bulk, the total surface resistance decreases, because the screening current flows on both the surface layer and bulk.
④
Rs
A. Gurevich, AIP Advance 5, 017112 (2015)
T. Kubo, Supercond. Sci. Technol. 30, 023001 (2017)
QNb3Sn=1×1011
λNb3Sn=120nm
QNb=2×1010
λNb=40nm
are assumed
2(K)
Q improve
Thin Nb3Sn on Nb substrate