## Slide 1: New SRF research opportunities
Theory: Residual resistance and BCS surface resistance at strong fields, nonequilibrium effects. Enhancement of extended Q(H) by impurities and multilayers. RF dissipation of vortices at very strong RF drive and generation of vortices upon cooling through Tc
Nb3Sn, NbN, pnictides are more temperamental than Nb, have current-blocking grain boundaries, and suffer from local nonstoichiometry and low Hc1. To what extent can these materials features be ameliorated by surface nanostructuring and impurity management?
Is N, Ar or Ti-doping the only way to reverse the Q-slope? Any other possibilities? – Ag, Si, Ge, … Deposition of N-doped thin films and multilayers on Nb cavities can capitalize on the Q(H) rise and reverse the reduction of breakdown fields. Can it be done on Nb3Sn?
?
?
A. Romanenko et al, APL 105, 234103 (2014)
Single cell, TESLA @1.5 K
How far can Q(H) and Eacc be increased?
How far can the extended Q(H) rise
be extended?
New SRF materials (Nb3Sn, pnictides)
Surface nanostructuring and multilayers
New imaging and SRF characterization
tools (STM coupled with microscopy
and Q(H) measurements)
Theory development
A. Gurevich, FNAL, Feb. 9-10, 2017

## Slide 2: Broadening of gap peaks in N(ε) reduces Rs
Idealized
BCS model
Low-frequency surface resistance at 1-2 GHz, hf/kT ≈ 10-2
Broadened gap
peak and subgap
states in the
Dynes model
Density of states with broadened gap peaks:
The log. term in Rs results from the singularity
in the BCS density of states (γ = 0) at ε = Δ
Broadening of gap peaks
in N(ε) can reduce Rs
by 4-5 times
Rs can be reduced by:
electron-phonon inelastic
scattering
proximity-coupled
metallic suboxides
Dilute magnetic impurities
Optimal inhomogeneities
A. Gurevich, FNAL, Feb. 9-10, 2017

## Slide 3: Tuning BCS residual surface resistance
Residual resistance is a part of BCS
surface resistance taking into account
realistic broadening of gap peaks in N(E)
Ri increases with but Rs(T) at higher T
is decreased by moderate broadening
Ri = 10 nohm at 1.5 GHz and nm
corresponds to
Generalized Mattis-Bardeen:
A. Gurevich, SUST 30, 034004 (2017)
A. Gurevich, FNAL, Feb. 9-10, 2017

## Slide 4: RF current broadening of N(E) and Q(H) rise
Mattis-Bardeen Rs was derived for weak RF fields (few mT):
At high fields current broadening of N(E) takes over
No stimulated superconductivity at
dirty
clean
Dirty layer preserves the quasiparticle gap up to
the superheating field .
In the clean limit the gap closes at H < Hs.
A. Gurevich, PRL 113, 087001 (2014).
Theory of nonlinear Rs(H) based on nonequilibrium BCS
Good agreement with
JLab and FNAL data
RF field suppression of Rs
Requires sharp gap peaks
in N(E) at H = 0
STM in parallel field can
reveal how N or Ti
doping affects N(E)
A. Gurevich, FNAL, Feb. 9-10, 2017

## Slide 5: Tuning Rs for weak rf field with parallel dc field
Superimposed parallel strong dc and weak rf fields probe the rf suppression of Rs(H) under equilibrium conditions
Different ratios of hν/Δ at
Rs(f,H0) tuned by dc field
A.Gurevich, PRL 113, 087001 (2014).
Rs measurements on striplines
combined with STM in parallel field
can reveal mechanisms of nonlinearity
of Rs(H) and the extended Q(H) rise.
A. Gurevich, FNAL, Feb. 9-10, 2017

## Slide 6: Extending the extended Q(H) rise in N-doped Nb cavities above the superheating field of Nb
A. Grasselino et al, SUST 26, 102001 (2013)
Hs, Hc1?
Alloyed Nb
film of optimum
thickness
Cavity grade
bulk Nb
A few nm thick
Al2O3 spacer
To capitalize on the extended Q(B) rise
and reverse the reduction of Hc1 and Hs
Use an optimized Nb bilayer to push
the breakdown field above both
superheating fields up to 250-300 mT
A few μm thick dirty layer at the surface
Increases the GL parameter κ = λ/ξ, and
decreases both Hs and Hc1:
before
after
A. Gurevich, AIP Advances, 5, 017112 (2015)
Optimized dirty N-doped layer
A. Gurevich, FNAL, Feb. 9-10, 2017

## Slide 7: Path to 60-120 MV/m
Maximum screening field Hm at optimal thickness
Dirty Nb layer: Hc = 200 mT, Hs = 170 mT, l = 2 nm, and λ =λ(ξ0 /l)1/2 = 180 nm
Hm = 288 mT, Eacc = 70 MV/m dm = 0.44λ = 79 nm.
20% gain as compared to Hs = 240 mT of clean Nb
Nb3Sn: Hs = 0.84Hc = 454 mT and λ = 120 nm (moderately dirty):
Hm = 507 mT, Eacc = 120 MV/m, dm = 1.1λ = 132 nm
doubles the superheating field of clean Nb
A. Gurevich, FNAL, Feb. 9-10, 2017

## Slide 8: Why are dielectric barrier essential?
dirty 1-2 µm
diffusion layer
Smooth decrease of imp concentration,
reduction of Hs and Hc1 at the surface
No protection against penetration
of vortices at surface defects
Interdiffusion cannot be avoided
Intercept penetrating vortices and arrest
thermomagnetic avalanches
Great reduction of vortex dissipation
Increase Hs and Hc1
Stop interdiffusion of impurities
Artificial I layers (Al2O3, etc) in ML structures
Natural oxide interfaces which do not dissolve
during deposition of S layers
Direct deposition of S (dirty Nb, Nb3Sn, etc) onto Nb
A. Gurevich, FNAL, Feb. 9-10, 2017