## Slide 1
Sam Posen
GARD-SRF Worksbop
Fermilab
9-10 February 2017
Breakthrough Ideas, Materials, Surface Structures to Pursue to Reach Revolutionary Gradients and Quality Factors

## Slide 2: Nb3Sn at 50-80 MV/m
High power pulsed testing of Nb3Sn cavities shows:
  High T: maximum field that extrapolates far above 50 MV/m
  Low T: indicative of defects, similar drop-off to Nb not optimized for high field operation
No sign of fundamental limit in Nb3Sn yet
S. Posen, N. Valles, and M. Liepe, Phys. Rev. Lett., 115, 047001 (2015).
High T behavior trends towards
Eacc ~ 95 MV/m
Low T drop-off indicative of surface defects
CW quench

## Slide 3: Increasing Eacc in Nb3Sn Cavities
Substantial recent improvement in maximum Eacc with high Q0
Several promising paths forward for continued progress including:
  Smooth sharp-edged surfaced
  Reduce low tin content regions
20-40% increase: 22-25 MV/m
R. Porter, D. L. Hall, M. Liepe, J. T. Maniscalco, Proc. Linac Conference 2016, MOPRC027 (2016).
Cornell: AFM scan of Nb3Sn sample
Field enhancement factor >1.5
S. Posen, Ph.D. Thesis, Cornell University (2015).
Y. Trenikhina, S. Posen, D. Hall, and M. Liepe, Proc. SRF Conference 2015, TUPB056, 2015
4 μm
Several promising paths forward for continued progress in Eacc (previous presentation)
Single cells are great tools: rapid feedback on recipes, ability to dissect and look at quench spots
With progress in CW mode, use pulsed measurements to continue to probe ultimate potential

## Slide 4: Survey of Materials Other than Nb and Nb3Sn
Nb3Sn will provide experience working with small-ξ materials
Experimental and theoretical work will help identify promising materials (and geometries) to pursue
Some beneficial properties in accelerator applications for potential SRF materials:
  High Q0 at higher T, where cooling is more efficient
  High maximum field
MgB2?
NbN/NbTiN?
Pnictides?