## Slide 1
MgB2 for SRF?
High Tc
Low residual resistivity (~ 0.1 μΩcm)
High Hc, high Hsh
Low Hc1 – can be enhanced by reducing film thickness
Effect of two energy gaps – can be manipulated by impurities
Polycrystalline vs. single crystalline – properties not much affected
On metal substrates - OK
Field emission?
Degradation in water – cleaning?
Liarte et al., SUST 30, 033002 (2017)
40
6.9
5.8
0.34 (exp.)
(Hc2/κ=0.85)
0.33
(0.83)
0.051

## Slide 2
Hc1 vs. Film Thickness; Hvp with Film Coating
Hc1 increases as film thickness decreases.
Thin film coating on Nb ellipsoids: > 400 Oe Hvp enhancement observed.
Tan et al., APL Materials 3, 041101 (2015)
Tan et al., Scientific Rep. 6, 35879 (2016)
Nb0
Nb200

## Slide 3
2” MgB2 Films on Cu Grown by HPCVD
Deposition temperature ~ 470°C, much lower than HPCVD on other substrates.
Eutectic Mg–Cu liquid promote growth of MgB2 at low temperature. Mg2Cu alloy acts as a source of Mg for the growth of MgB2.
Tc = 37 K
Au et al., J. Mater. Chem. A1, 9983 (2013)
Cu cavity, 11.4 GHz
(Paul Welander, SLAC)

## Slide 4
Coating of 3 GHz SRF Cavity by HPCVD
B2H6 and Mg vapor are introduced to the interior of the cavity while it is being rotated and slowly moved along its central axis.
Films on substrates mounted on a 3.9 GHz mock cavity show Tc = 39 K
18.5 GHz Dielectric Resonator

## Slide 5
Thin Films vs. Real Cavity
Thin films:
  necessary for studies of fundamental properties
  may not predict cavity coating performance
Cavity coating
  ultimate demonstration of viability
  needs new facilities