## Slide 1
Sam Posen
GARD-SRF Worksbop
Fermilab
9-10 February 2017
Next Steps and Validating Milestones for high Q CW Machines – Nb3Sn and Flux

## Slide 2: Nb3Sn Films: Advantage of Higher Tc
Nb3Sn bulk films currently by far has the most promising SRF results of non-Nb superconductor implementations
Recent progress: reliable achievement of fields ~15 MV/m and higher with Q0~1x1010 at 4.2 K and 1.3 GHz (Cornell)
D. Hall, M. Liepe, S. Posen, Cornell University
Bulk films: Cornell, JLab, Fermilab
  (Nb3Sn/Cu: CERN)
Some obvious next steps for development within the next 4-5 years:
  Maximum Eacc
  Rres
  Muticell Cavities
Niobium Surface
After Nb3Sn Coating

## Slide 3: Increasing Eacc in Nb3Sn Cavities
Substantial recent improvement in maximum Eacc with high Q0
Several promising paths forward for continued progress including:
  Smooth sharp-edged surfaced
  Reduce low tin content regions
20-40% increase: 22-25 MV/m
R. Porter, D. L. Hall, M. Liepe, J. T. Maniscalco, Proc. Linac Conference 2016, MOPRC027 (2016).
Cornell: AFM scan of Nb3Sn sample
Field enhancement factor >1.5
S. Posen, Ph.D. Thesis, Cornell University (2015).
Y. Trenikhina, S. Posen, D. Hall, and M. Liepe, Proc. SRF Conference 2015, TUPB056, 2015
4 μm

## Slide 4: Reducing Rres in Nb3Sn Cavities by ~50%
Significant Rres in Nb3Sn connected to trapped flux, thermocurrents
Concentrated effort on reducing Rres could significantly increase Q0
2.0 K: Rres dominant
4.5 K: less expensive cryogenics
More uniform cooldown: Rs 2x smaller
Notes: 2 K and 4.2 K

## Slide 5: High Performance Multicell Cavities
Fermilab and JLab each work towards multicell coatings
Challenges: uniformity, endgroups, NbTi flanges
Should investigate other frequencies (both higher & lower)
Important to develop practical aspects – microphonics, cooldown, optimal operating temperature
Horizontal test stand tests will be informative
JLab - Designed for up to 5-cell 1.5 GHz with waveguides
Fermilab - Designed for up to 5-cell 650 MHz
Recipe development for uniform coatings of cavities with large surface area: multicell & low frequency – higher vapor pressure, longer annealing?

## Slide 6: Specifications to Minimize Flux Trapping
S. Posen, M. Checchin, A. C. Crawford, A. Grassellino, M. Martinello, O. S. Melnychuk, A. Romanenko, D. A. Sergatskov, and Y. Trenikhina, Jour. App. Phys, 119(21), 213903.
Flux expulsion R&D at Fermilab:
  Few mG trapped flux causes significant Q0 degradation
  As received material from vendors varies in expulsion behavior
  Heat treatment improves expulsion, but may require >900 C
Wah Chang
Tokyo Denkai
Complete Expulsion
Complete Trapping
1000 C 4 h vastly improves expulsion

## Slide 7: Specifications to Minimize Flux Trapping
Experience with LCLS-II cavities: same observations
  Few mG trapped flux causes significant Q0 degradation
  As received material from vendors varies in expulsion behavior
  Heat treatment improves expulsion, but may require >900 C

## Slide 8: Specifications to Minimize Flux Trapping
It is clear that expulsion is a bulk property
  Grain boundaries?
  Dislocations?
Every large grain cavity that we have measured has had strong expulsion
  Fewer grain boundaries?
  Less work – fewer dislocations?
Endeavor to develop understanding of physical mechanism so we can update material specifications to provide strong expulsion (1-2 years)