## Slide 1: Field Emission its Understanding and Control
Rong-Li Geng
Jefferson Lab
GARD-SRF Roadmap Workshop
Fermilab, February 9-10, 2017

## Slide 2: Question from Organizer
What are the state of the art and the new ideas to pursue abatement of field emission in vertical test and cryomodules? (Wu, Kelly, Geng, Padamsee, Martinello)

## Slide 3: Outline
Review of state of the art in FE control
Ideas in further raising FE onset
Examples of on-going work in understanding and control of FE at JLab
Conclusion

## Slide 4: State of the Art in Single-Cell Cavity Testing
F. Furuta, K. Saito et al., SRF2007, TUP10
Theory: Remove embed NbxSy that can not be removed by USC or HPR alone
ILC baseline surface processing + additional fresh EP

## Slide 5: State of the Art in Full-Scale 9-Cell Cavity Vertical Testing
IPAC2011, MOPC111
ILC baseline surface processing

## Slide 6: State of the Art in Full-Scale 9-Cell Cavity Horizontal Testing
A. Hocker et al., IPAC2012, WEPPC049
HTS @ FNAL
VTA @ JLAB
FE measurements site dependent!
Be careful when comparing apples to pears

## Slide 7: State of the Art in Full-Scale Cryomodule Testing
E. Harms et al., SRF2015, FRAA03

## Slide 8: FNAL CM2 Q0, FE, Dark Current
E. Harms et al., SRF2025, FRAA03
FE X-ray onset ≥ 19 MV/m
Dark Current at 31.5 MV/m
4 out of 8: No detectable
2 out of 8: ~ 1nA
1 out of 8: ~ 10 nA
1 out of 8: ~ 100 nA

## Slide 9: Summary of State of the Art High G
50-60 MV/m, Best 1-cells, alternative shape
40-45 MV/m, best 9-cells, TESLA shape
36 MV/m one 9-cell without beam
  57hours
31.5 MV/m, 7 9-cell without beam
  unknown hours
> 30 MV/m, several 9-cells with beam
  15 hours at 3 mA
  Several hours close to 9 mA
RG, TTC @ Saclay, France, July 5-8, 2016
Vertical test
Cryomodule test
without beam
Cryomodule test
with beam

## Slide 10: Field Emission
Continuous progress has been made over decades in raising FE onset at all levels of cavity testing.
  “FE-free” vertical testing demonstrated in single-cell up to 50 MV/m and full-scale 9-cell up to 40 MV/m.
Presently there is lot of enthusiasm in advancing SRF cavity gradient to 60-80 MV/m via new material and in raising Q0 at 30-40 MV/m in niobium cavities.
While achievement of low surface resistance is an important goal, one must not forget to fight FE.
FE in SRF accelerator operation remains a challenge.
Extrapolating the state of the art, due to its exponential nature, we foresee FE a bottle neck in SRF cavity operation at > 40 MV/m without or with beam.
FE study and control should be a high priority in high gradient SRF portfolio within GARD program.

## Slide 11: New (and not so New) Ideas in Raising FE Onset
Micro-EP (more later)
  Derived from “Fresh EP” idea of Saito & Furuta demonstrated in 2007.
  A Vertical EP machine a perfect tool for this task
End-group cleaning
  End-group brushing, steam cleaning, dry-ice cleaning
Low-particulate assembly
Low-particulate beamline components
  Ion pumps, gate valves…
In-situ processing
  Helium processing
    A useful tool for CEBAF upgrade cavity FE improvement at JLab
On top of everything, understanding is needed regarding the nature of actual field emitters at all stages of cavity surface preparation, string assembly, and beam operation.
  origin, mechanism of transportation into cavity…
  FE mapping
  “Forensic” studies of post-operation cavities

## Slide 12: Demonstration of Field Emission Free @ Epk>100 MV/m
Re-HPR only
+ µEP + ER + USC + HPR
Field emission free
Epk 104 MV/m
Achieved by using standard ILC EP processing at JLab horizontal EP machine
This result encourages µEP effort based on vertical EP machine at Cornell (see F. Furuta, 2nd LCC/ILC Cavity Group Meeting, Nov. 6, 2013)
Next step is to test even less removal down to 1 µm

## Slide 13: Understanding and Reduction of FE – FE Mapping
Joint testing/comparison of Kyoto/KEK sX-mapping & JLab diode ring X-Mapping Vertical Test Area, Jefferson Lab SRF Institute, Oct. 9 – 15, 2016

## Slide 14
Direct Evidence of Particulate Transportation
DI (noble)
Ion pump (Ti/Ta)
Conventional
Ion pump (Ti)
Pilot study with module FEL2 of identical design, previously operated with beam
IPAC2016, THOBB03

## Slide 15: FE Detection Around 12 GeV Upgrade Cryomodules in CEBAF Tunnel
On-going testing with JLAB-SLAC cooperation

## Slide 16: Conclusion
FE is foreseen a bottle neck in SRF cavity operation at > 40 MV/m without or with beam. Carry out R&D now.
FE control is needed at all levels from SRF cavity surface prep to cavity beam operation. New progress will benefit all DOE SRF accelerators.
Low FE operation of SRF accelerators a defining goal. Use DOE SRF accelerators, ASTA, CEBAF, LCLs-II, as test bed for FE studies.
FE diagnostics hold key toward a deeper understanding and raising FE onset to next level. Increase level of effort in FE diagnostics, exploit on-going SRF production project such as LCLS-II.
FE study and control should be a high priority in high gradient SRF portfolio within GARD program. An annual investment of $1M for next five years is recommended.