## Slide 1: SPX Cavity Layout

## Slide 2: Damper Overview
Power density spectrum in LOM damper
Damper assembly: bottom
Temperature distribution
Power handling is 900 W for LOM and 150 W for HOM loads.
Loads are affixed with high temperature S-bond solder
Resists particulation due to its high density, temperature strength, and wear resistance.
Thermal conductivity ~100 W/ (oK m).

## Slide 3: Damper: Mechanical Tests
Pull force for various bonding methods
S-bond solder
Vacuum residual gas analysis
Re-melting measurements

## Slide 4: Damper: Electrical Tests
Permittivity of SiC (Real & Imaginary)
Variation of permittivity among homogenous material
Return loss of HOM damper
Return loss of prototype damper
(a) Real
(b) Loss tan