## Slide 1: Short spool F10041117 #1003 (rejected)
Before cleaning
After cleaning

## Slide 2: Long Spool F10052775 #1006 (rejected)
After cleaning

## Slide 3: Long Bellows F10041075 #1020 (rejected)
Dark spot has a black color raised blemish in the center

## Slide 4: Long Bellows F10041075 #1027 (rejected)
Dark spot has a black color raised blemish in the center + bottom of the convolutions are not copper plated + lots of pits and dents
Before Cleaning
After Cleaning

## Slide 5: Standard UHV cleaning at CAF
20 mins Simple green with ultrasonic on
Rinse
15 mins Micro90 with ultrasonic on
Rinse
Alcohol
Dry with filtered Nitrogen
Leave under Class 10/100 hood for a few days
Bring into main Cleanroom
Total 35 minutes in ultrasonic compared to 10 minutes during the QC at SLAC