## Slide 1
Martina Martinello
P2MAC
11th April 2017
SRF Research

## Slide 2: PIP-II SRF LINAC

## Slide 3: PIP-II: SC LINAC
HWR b=0.112
SSR1 b=0.222
SSR2 b=0.475
LB650 b=0.647
HB650 b=0.97
To booster
To experiments
at 800 MeV
2.1 MeV
10.3 MeV
35 MeV
185 MeV
500 MeV
800 MeV
CM type |  |  | f0 (MHz) | Q at 2K | Eacc (MV/m)
HWR | 0.094 | 0.112 | 162.5 |  | 11.6
SSR1 | 0.186 | 0.222 | 325 |  | 11.9
SSR2 | 0.398 | 0.475 | 325 |  | 13.6
LB650 | 0.61 | 0.647 | 650 |  | 17
HB650 | 0.92 | 0.971 | 650 |  | 18.8
CM type |  |  | f0 (MHz) | Q at 2K | Eacc (MV/m)
HWR | 0.094 | 0.112 | 162.5 |  | 11.6
SSR1 | 0.186 | 0.222 | 325 |  | 11.9
SSR2 | 0.398 | 0.475 | 325 |  | 13.6
LB650 | 0.61 | 0.647 | 650 |  | 17
HB650 | 0.92 | 0.971 | 650 |  | 18.8
In this presentation Eacc is defined calculating the effective cavity length using while the CDR uses Therefore, the values of Eacc shown here are ~ 5 % larger than the values in the CDR.

## Slide 4: PIP-II: SC LINAC
Advantages of low frequencies cavities:
  Decrease number of cells per cavity (for a fixed cavity length)
  → increase acceleration efficiency
  Lower power dissipation ()
Disadvantages of low frequencies cavities:
  Increase difficulties to suppress microphonics
  Large cost due to more niobium utilization

## Slide 5: SRF Research on high-b 1.3 GHz cavities

## Slide 6: Standard SRF cavity surface treatments
High field
Q-slope
Medium field
Q-slope
Conventional Nb Cavities Surface Treatment (main steps):
Treatment proposed for the ILC
EP cavities
120C bake
cavities
Cavity after welding
EP 140 μm
3 h at 800 C UHV baking
48 h at 120 C baking
EP 40 μm

## Slide 7: The discovery of N-doping
Q-factor improvement after N-doping – up to 4 times higher Q than standard Nb cavities
Typical Q vs Eacc curve obtained with 120C bake (standard ILC treatment)
Average Q at 16MV/m:
Standard ILC treatment:
N-doping:
Anti-Q-slope
A. Grassellino et al., Supercond. Sci. Technol. 26, 102001 (2013) – Rapid Communications

## Slide 8: N-doping treatment
800 C (3 hours)
25 mTorr (2 minutes)
Example of a N-doping process (2/6 recipe):
Nb bulk EP cavity annealed for 3 hours in vacuum (UHV furnace) at 800C
Nitrogen injected (25 mTorr) at 800C for 2 minutes
Cavity stays for another 6 minutes at 800C in vacuum
Cooling in vacuum
5 um electro-polishing (EP)
Cavity after welding
EP 140 μm
3 h at 800C UHV baking
48 h at 120C baking
N2 injection 800C
EP 5 μm

## Slide 9: N-doping treatment (2/6 recipe)
N
Nb
N Interstitial
Only Nb from TEM/NED spectra:
N must be interstitial
Final RF Surface
Y. Trenikhina et Al, Proc. of SRF 2015
Cavity after welding
EP 140 μm
3 h at 800C UHV baking
48 h at 120C baking
3 h at 800 C UHV baking
EP 5 μm

## Slide 10: Origin of the anti-Q-slope
Anti-Q-slope emerges from the BCS surface resistance decreasing with field
Anti-Q-slope
A. Grassellino et al, Supercond. Sci. Technol. 26 102001 (2013) - Rapid Communications
A. Romanenko and A. Grassellino, Appl. Phys. Lett. 102, 252603 (2013)

## Slide 11: Effects of the nitrogen doping
LE-mSR measurements (Ba=25mT)
N-doping modify the mean free path
→Mean free path close to theoretical minimum of RBCS
N-doping seems to increase the reduced energy gap D/kTc at medium field
~15 nm - no screening
N-doped: mfp~40 nm
EP: mfp > 400 nm
A. Romanenko et al, Appl. Phys. Lett. 104, 072601 (2014)
A. Grassellino et al, Proc. of SRF2015
120C bake: mfp~2-16 nm
M. Martinello et al, Appl. Phys. Lett. 109, 062601 (2016)

## Slide 12: Trapped flux surface resistance
⇒ temperature-dependent part of the surface resistance
⇒ intrinsic residual resistance
⇒ trapped magnetic flux surface resistance:
If pinned, vortices may survive in the Meissner state introducing dissipation
—flux trapping efficiency
—trapped flux sensitivity
—external magnetic field
H. F. Hess et al., Phys. Rev. Lett. 62, 214 (1989)
Cooldown
Vortex
Vortex lattice

## Slide 13: Trapped flux surface resistance
These losses can be reduced by minimizing these contributions:
𝐵
Magnetic shielding/hygiene improvement
𝜂_𝑡
Fast Cooling
Material Optimization
S
Optimizing mean free path
Magnetic shielding/hygiene improvement
Fast Cooling
Material Optimization
S
Optimizing mean free path

## Slide 14: Trapped flux surface resistance
These losses can be reduced by minimizing these contributions:
𝐵
Magnetic shielding/hygiene improvement
𝜂_𝑡
Fast Cooling
Material Optimization
S
Optimizing mean free path
Magnetic shielding/hygiene improvement
Fast Cooling
Material Optimization
S
Optimizing mean free path
External magnetic field

## Slide 15: Minimization of remnant field in the cryomodule
Demagnetization
Empty vacuum vessel
Assembled Cryomodule
Coils for magnetic field demagnetization
Demagnetization

## Slide 16: Trapped flux surface resistance
These losses can be reduced by minimizing these contributions:
𝐵
Magnetic shielding/hygiene improvement
𝜂_𝑡
Fast Cooling
Material Optimization
S
Optimizing mean free path
Magnetic shielding/hygiene improvement
Fast Cooling
Material Optimization
S
Optimizing mean free path
Flux Trapping Efficiency

## Slide 17: Fast cooldown helps flux expulsion
Fast cool-down lead to large thermal gradients efficient flux expulsion
Slow cool-down lead to small thermal gradients poor flux expulsion
A. Romanenko et al., Appl. Phys. Lett. 105, 234103 (2014)
A. Romanenko et al., J. Appl. Phys. 115, 184903 (2014)
D. Gonnella et al, J. Appl. Phys. 117, 023908 (2015)
M. Martinello et al., J. Appl. Phys. 118, 044505 (2015)
S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
S. Huang, Phys. Rev. Accel. Beams 19, 082001 (2016)
T1
T2
All flux trapped
Efficient flux expulsion
Bsc/Bnc=1.74 after complete Meissner effect
Bsc/Bnc=1 after full flux trapping
Bsc/Bnc
Q0

## Slide 18: High T baking for flux expulsion improvement
Not all materials show good flux expulsion even with large thermal gradient
High T treatments are capable to improve materials flux expulsion properties
S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
Full trapping
Full expulsion
Full expulsion
Full trapping

## Slide 19: High T baking for flux expulsion improvement
S. Posen et al., J. Appl. Phys. 119, 213903 (2016)
After 900C
Full trapping
Full expulsion
After 1000C
Full expulsion
Full trapping
Not all materials show good flux expulsion even with large thermal gradient
High T treatments are capable to improve materials flux expulsion properties

## Slide 20: Trapped flux surface resistance
These losses can be reduced by minimizing these contributions:
𝐵
Magnetic shielding/hygiene improvement
𝜂_𝑡
Fast Cooling
Material Optimization
S
Optimizing mean free path
Magnetic shielding/hygiene improvement
Fast Cooling
Material Optimization
S
Optimizing mean free path
Trapped Flux Sensitivity

## Slide 21: Light doping to minimize trapped flux sensitivity
Trapped flux sensitivity:
Bell-shaped trend of as a function of mean free path
N-doping cavities present higher sensitivity than standard treated cavities
Light doping is needed to minimize trapped flux sensitivity
M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)

## Slide 22: Minimizing at 16 MV/m
Very low values of RBCS
Acceptable values of sensitivity
Low residual resistance
The best surface treatment minimizes both and contributions:
Light doping was chosen for LCLS-II:
M. Martinello et al., App. Phys. Lett. 109, 062601 (2016)
M. Checchin et al., Supercond. Sci. Technol. 30, 034003 (2017)

## Slide 23: N-doping from R&D to production
FNAL single cell cavities
Bare 9-cell cavities with 2/6 doping recipe
Many recipes were studied on single-cell cavities: light doping seemed the best in terms of both Q-factor and quench field
2/6 recipe:
Best recipe transferred to 9-cell cavities and measured before and after He vessel. Some measured also in HTS (fully dressed and assembled).

## Slide 24: N-infusion Performance
The N-infusion performance can be tuned by acting on time and temperature:
Shorter treatment and lower T → 120 C baking like behavior
Longer treatment and/or higher T → N-doping like behavior
A. Grassellino et al., arXiv:1305.2182

## Slide 25: Status of SRF Technology for PIP-II

## Slide 26: 162.5 MHz Half-Wave Resonators
*HWR technology developed at ANL via ANL/FNAL PIP-II Collaboration.
Z. Conway, A. Barcikowski, S. Gerbik, C. Hopper, M.P. Kelly, M. Kedzie, S. Kim, P. Ostroumov, T. Reid.
Bulk and light EP of jacketed HWR @ ANL
Bare HWR before jacketing
Surface treatments:
Light BCP
Deep EP
Baking at for 10 hours in UHV furnace
Light EP

## Slide 27: HWR 2 K Test Results
PIP-II specs
Curtesy of A. Lunin and Z. Conway

## Slide 28: SSR1: 325 MHz Single Spoke Resonators
Surface treatments:
Bulk BCP
Baking at for 10 hours in UHV furnace
Light BCP
Low T baking at for 48 hours
particularly favorable to process MP
L. Ristori, M.H. Awida ,P. Berrutti, T.N. Khabiboulline, M. Merio, D. Passarelli, A. Rowe, D.A. Sergatskov, A.I. Sukhanov,
Proc. of IPAC 2013, Shangai, China

## Slide 29: SSR1 VTS Test Result
PIP-II
specs
Curtesy of A. Sukanov

## Slide 30: Fully-Integrated Tests in STC
Prototype coupler
Prototype tuner
First jacketed cavities tested in the Spoke Test Cryostat (STC)
2 cavities tested with unit coupling → successful test, no degradation between VTS and STC
3 cavities tested with prototype coupler → 2 showed high level of FE, cavities will be re-HPR, re-assembled in ANL clean-room and re-tested
A. Sukhanov et al., Proceedings of LINAC2014, Geneva, Switzerland
PIP-II
specs

## Slide 31: HB650 Single-cell Test Results
PIP-II
specs
120C baked cavities not always meet specs
N-doping capable to double the Q-factor at medium field
World record Q-factor of 7e10 at 2K,17 MV/m and 650 MHz with N-doping

## Slide 32: HB650 5-cells Tests Results (all N-doped)
PIP-II
specs
B9A-AES-010
B9A-AES-009
B9A-AES-008
Light N-doping applied to 650 MHz cavities
3 N-doped 5-cells 650 MHz cavities meet PIP-II specification
Optimal doping may increase Q-factor even more

## Slide 33: Expected Q-factor from 1.3 GHz scaling
The Q extrapolated at 2 K for 650 MHz from 1.3 GHz is really promising
The results obtained so far for 650 MHz N-doped cavities are encouraging but do not meet the Q extrapolated from 1.3 GHz, meaning that optimal doping for 650 MHz cavities has not been found yet

## Slide 34: Conclusion and Future plan
HWR and SSR1 cavities meet PIP-II specs with standard treatments
It is established that N-doping can provide high Q-factors at medium field at 650 MHz
Optimal doping recipe for 650 MHz cavities to be investigated
Trapped flux sensitivity and flux expulsion to be studied to set specification of magnetic field shielding
Soon N-infused 650 MHz cavity will be tested, potentially good for both high-Q and high gradient

## Slide 35: Thank you for your attention

## Slide 36: N-infusion Thermal Process
Bulk EP
High T furnace with caps to avoid furnace contamination:
  3h @ 800C in HV
  48h @ 120-160 C with N2 (25 mTorr)
  Optional annealing 48h @ 120-160 C
NO chemistry post furnace
A. Grassellino et al., arXiv:1305.2182
Protective caps and foils are BCP’d prior to every furnace cycle and assembled in clean room, prior to transporting the cavity to furnace area
120 C
25 mTorr
800 C
Pressure (Torr)
Temperature (⁰C)