## Slide 1: MQXFA1 (QXFP coils) measurements at SG locations LBNL
Heng Pan, Dan Cheng
03/23/2017

## Slide 2: Outline
MQXFA1 Coils Cross section Measurements

## Slide 3: CMM Measurements
All LBNL data was taken using a Zeiss Accura for CMM
Calypso software post-processed data
  All surfaces were “best-fit” to reference geometry with equal weighting
  However, the alignment was not included in the MQXFA1 coils measurements (therefore, no asymmetry data)

## Slide 4: Dummy Coil Cross Section Measurements
Data was only processed at a subset (SG locations) of all the cross section measurements available:
  740 mm
  1940 mm
  3140 mm
740 mm
1940 mm
3140 mm
CMM Model Standard:
Inner Radius: 74.75 mm
Outer Radius: 113.376 mm
Midplane offset: 0.125 mm

## Slide 5: Post-processing at 740 mm from LE
Profile: ± 2 mil
Radial: -0.001”
Midplane: -0.004”
Radial: -0.001”
Midplane: -0.002”
Radial: 0”
Midplane: -0.0015”
Radial: -0.001”
Midplane: -0.002”

## Slide 6: Post-processing at 1940 mm from LE
Profile: ± 2 mil
Radial: -0.0015”
Midplane: -0.004”
Radial: -0.001”
Midplane: -0.002”
Radial: -0.0005”
Midplane: -0.0015”
Radial: -0.0015”
Midplane: -0.003”

## Slide 7: Post-processing at 3140 mm from LE
Profile: ± 2 mil
Radial: -0.0015”
Midplane: -0.004”
Radial: -0.0005”
Midplane: -0.001”
Radial: 0”
Midplane: -0.001”
Radial: -0.001”
Midplane: -0.002”

## Slide 8: Effective coil OR (mm)
 | Coil #2 | Coil #3 | Coil #4 | Coil #5
740 mm | 113.318 | 113.334 | 113.334 | 113.36
1940 mm | 113.306 | 113.347 | 113.326 | 113.355
3140 mm | 113.318 | 113.355 | 113.334 | 113.368
Avg. | 113.331 | 113.345 | 113.331 | 113.361
Nominal OR: 113.376 mm
Chart: Dev. (mil)
| 740 mm | 1940 mm | 3140 mm
Coil 2 | -2.2835 | -2.7559 | -2.2835
Coil 3 | -1.6535 | -1.1417 | -0.82677
Coil 4 | -1.6535 | -1.9685 | -1.6535
Coil 5 | -0.62992 | -0.82677 | -0.31496
Coil OR Dev. from Nominal

## Slide 9
Sector 1
Sector 4
Sector 3
Sector 2
Sec1 Out (+)
Sec1 In
Sec4 Out
Sec4 In
Sec3 Out
Sec3 In (-)
Sec2 Out
Sec2 In
Sec2-Sec4 Splice
Sec3-Sec2 Splice
Sec1-Sec4 Splice
Splice Order: (+) o1i – i4o – i2o – o3i (-)

## Slide 10: Coil Order Constraints
Bring all coils to same collar arc length
Splice order
  changed quadrants in 10/2016 to match CERN’s naming conventions
  Sectors 4 and 2 are the only options for QXFP03
5
3
2
4
Shifted due Undersized
Add shim to match OR larger coils
8 x dmidplane = 2 p x dROR
Shifted due Undersized
Add midplane shim to match effective arc length
Add shim to match OR larger coils
Add midplane shim to match effective arc length

## Slide 11: Backup Slides
From MQXFA1 Coils and Conductor Readiness Review
  https://indico.fnal.gov/conferenceDisplay.py?confId=14087

## Slide 12: Coil Azimuthal Size (L + R)

## Slide 13: Measured Coil Radius

## Slide 14: QXFP02 & 04
Coil Size: