## Slide 1: MQXFA-1 Readiness Review Conductor
Lance Cooley (representing also Arup Ghosh)
LARP L3-Strand

## Slide 2: Content
Coil | Cable | Strand | Spec.
MQXFP1 | P33OL1059 | 0.85 mm 108/127* | LARP 8002.F (2011)
MQXFP2 | P35OL1060 | 0.85 mm 132/169 | LARP 8004.B (2013)
MQXFP3 | P47OL1064 | 0.85 mm 144/169 | LARP 8004.C (2014)
MQXFP4 | P45OL1069 | 0.85 mm 132/169 | LARP 8004.B (2013)
MQXFP5 | P43OL1070 | 0.85 mm 108/127 | LARP 8004.D / HiLumi (2015)
* Most of the virgin strand data is for 0.78 mm diameter
PxxOLnnnn is the cable ID:
  “xx” is the project and strand type
    30 series = QXF gen 1 with annealed strands; 40 series = QXF gen 2 with annealed strands;
    Odd = cored cable; x3, x5, x7 determines strand type
  “nnnn” is the cable map number

## Slide 3: Timeline
Strands for coils QXFP1 thru P3 were purchased by BNL; strands for P4 and P5 were purchased by FNAL
Coils P1, P2, & P3 were reacted prior to retirement of Arup Ghosh; P4 and P5 were reacted afterward
  Witness samples for P1 and P2 were tested at BNL
  Witness samples for P3 were reacted at FNAL on BNL-style HT barrels and were supposed to be tested at BNL, but were never delivered due to retirement. Urgent testing is planned.
  Witness samples for P4 and P5 were tested at FNAL
    The number of samples was reduced in anticipation of the new holder for witness samples at the coil end

## Slide 4: LARP and CDP Ti-alloyed RRP Nb3Sn over the past decade
83 km of RRP 108/127
  0.778 mm, Cu:NC = 1.2,“Std. Sn” at 3.4:1 Nb:Sn ratio
  Some lengths 0.85 mm “-5% Sn” at 3.6:1  MQXFP1
64 km of RRP 132/169
  10 km 0.85 mm, 1.2, “Std. Sn”, “type 2 Nb” 54 km 0.85 mm, 1.2, “-5% Sn” at 3.6:1  MQXFP2 & P4
38 km of 144/169
  0.85 mm, 1.1, “-2.5% Sn” at 3.5:1  MQXFP3
167 km of 108/127 (HL-LHC)
  0.85 mm, 1.2; -5% Sn  MQXFP5

## Slide 5: Reduced tin was meant to facilitate higher temp HT
50-75 h @ 665 ºC
48 or 50 h @ 650 ºC
LARP 8004.D & HL-LHC
LARP 8002 &
LARP 8004.A-C

## Slide 6: Round wire
Chart: Ic (4.2 K, 15 T) (A)
| 389.13138295411738 | 403.45523754138554 | 408.22985573714158 | 0 | 417.77909212865364 | 0 | 383.16311020942237 | 377.1948374647273 | 386.74407385623937 | 381.96945566048333 | 385.55041930730039 | 405.84254663926356 | 390.32503750305642 | 373.6138738179103 | 436.87756491167784 | 404.64889209032452
108/127, 0.78 mm | 289 | 192 | 46 | 52 | 297 | 302 | 192 | 166 | 283 | 227 | 174 | 143 | 69 | 66
132/169, Std. Sn | 176 | 132 | 151 | 105 | 206 | 103 | 150 | 87
132/169, –5% Sn | 369 | 279 | 326 | 328 | 349 | 266 | 318 | 290 | 305 | 339 | 338 | 291 | 342 | 323 | 356 | 296 | 291 | 257 | 381 | 357
144/169, –2.5% Sn | 214 | 235 | 237 | 282 | 272 | 257 | 277 | 197 | 201 | 260 | 259 | 274 | 280
HiLumi 108/127 | 291 | 275 | 354 | 348 | 313 | 321 | 350 | 345 | 303 | 303 | 363 | 361 | 274 | 296 | 294 | 292 | 297 | 303 | 334 | 382 | 309 | 294 | 328 | 363
QXFP1
QXFP2,4
QXFP5
QXFP3
RRR – all specs
Ic – 8004.D & HiLumi
Ic – 8002.F & 8004.B,C
Data shown for 108/127 0.78 mm has been scaled by (0.85/0.78)2 to allow comparison with other strands.
3.4:1 Nb:Sn
Not used in coil

## Slide 7: Heat treatment
Coil | HT actual
QXFP1 | 25 / 210 / 74 + 50 / 401 / 49 + 50 / 641 / 48
QXFP2 | 25 / 210 / 72 + 50 / 400 / 48 + 50 / 650 / 48
QXFP3 | 25 / 210 / 72 + 50 / 400 / 48 + 50 / 650 / 48
QXFP4 | 25 / 210 / 72 + 50 / 400 / 48 + 50 / 649 / 48
QXFP5 | 25 / 210 / 72 + 50 / 400 / 48 + 50 / 665 / 50
Nomenclature: Ramp °C per hour / soak °C / soak duration in hours
HT Schedule for most coils: 25/210/72 + 50/400/48 + 50/650/48
Coil QXFP5: final stage 50/665/50
Early 108/127 had 3.4:1 Nb:Sn and used 640/48, but this didn’t go into P1
108/127 0.78 mm strand at 3.6:1 and 144/169 at 3.5:1: final stage 650/50
132/169 at 3.6:1: final stage 665/50
Hi-Lumi 108/127 at 3.6:1: final stage 665/75

## Slide 8: Coil QXFP1, cable 1059 – Witness samples
Billet | # Respools | RRR | Ic(11T) | Ic(12T) | Ic(13T) | Ic(14T) | Ic(15T)
14793 | 10 of 40 | 299 307 | 860 852 | 713 706 | 581 576 | 468 462 | 368 362
14794 | 9 of 40 | 284 295 | 856 839 | 706 694 | 573 566 | 459 452 | 359 354
14795 | 7 of 40 | 327 | 848 | 700 | 570 | 458 | 359
14943 | 10 of 40 | 304 206 | 878 878 | 726 727 | 591 592 | 474 474 | 370 370
15291 | 4 of 40 | 341 | 862 | 713 | 580 | 465 | 363
14793 | Round | 352 |  |  |  | 472 | 370
14794 | Round | 249 | 888 | 734 | 601 | 484 | 381
14795 | Round | 279 | 895 | 745 | 609 | 491 | 387
14943 | Round | 216 | 915 | 756 | 619 | 497 | 391
Cable degradation 4.7%

## Slide 9: Coil QXFP1, Cable 1059 – SSL information
1.9 K SSL intercept 15.06 T, 22.1 kA
16.5 kA Operating point at 74.7% SSL
SSL crosses 11.4 T, 16.5 kA @ TCS = 7.24 K
TCS – TOP = 5.3 K
Cable Ic at 11.4 T = 44.2 kA
16.5 kA IOP = 37.3% Cable Ic

## Slide 10: Coil QXFP2, cable 1060 – Witness samples
Billet | # Respools | RRR | Ic(11T) | Ic(12T) | Ic(13T) | Ic(14T) | Ic(15T)
16317 | 15 of 40 | 427 330 318 | 795 793 790 | 656 653 653 | 537 536 532 | 429 428 426 | 338 337 335
16336 | 15 of 40 | 393 313 315 | 852 800 817 | 709 667 677 | 582 546 557 | 471 441 448 | 375 349 356
16342 | 6 of 40 | 219 240 | 804 808 | 669 671 | 549 552 | 442 445 | 348 353
16628 | 4 of 40 |  |  |  |  |  | 
16317 | Round | 352 |  |  |  | 472 | 370
16336 | Round | 249 | 888 | 731 | 601 | 484 | 381
16342 | Round | 279 | 895 | 745 | 609 | 491 | 387
16628 | Round | 216 | 915 | 756 | 619 | 497 | 391
Cable degradation 10.4%

## Slide 11: Coil QXFP2, Cable 1060 – SSL information
1.9 K SSL intercept 14.82 T, 21.7 kA
16.5 kA Operating point at 75.9% SSL
SSL crosses 11.4 T, 16.5 kA @ TCS = 7.0 K
TCS – TOP = 5.1 K
Cable Ic at 11.4 T = 41.0 kA
16.5 kA IOP = 40.2% Cable Ic

## Slide 12: Coil QXFP3, cable 1064 – Witness samples
Samples will be measured with high priority

## Slide 13: Coil QXFP4, cable 1069 – Witness samples
Billet | # Respools | RRR | Ic(12T) | Ic(13T) | Ic(14T) | Ic(15T) | n(15T)
16313 | 9 of 40 |  | 647 | 524 | 419 | 328 | 37
16315 | 7 of 40 |  | 693 | 568 | 457 | 362 | 39
16316 | 7 of 40 |  | 644 | 523 | 418 | 331 | 29
16338 | 6 of 40 |  | 668 | 547 | 443 | 351 | 38
16341 | 11 of 40 |  | 678 661 | 553 540 | 446 434 | 351 342 | 36 36
16341 | Witness |  | 670 | 546 | 438 | 344 | 38
16313 | As Rcvd | 369 | 680 | 563 | 461 | 367 | 31
16315 |  | 326 | 711 | 591 | 481 | 386 | 39
16316 | As Rcvd | 349 | 688 | 568 | 463 | 370 | 40
16338 | As Rcvd | 342 | 700 | 582 | 478 | 386 | 41
16341 | As Rcvd | 356 | 707 | 585 | 477 | 381 | 37
Strand HT 665/50, coil HT 650/48
Fit: cable degradation 4.5%

## Slide 14: Coil QXFP4, Cable 1069 – SSL information
1.9 K SSL intercept 14.46 T, 21.2 kA
16.5 kA Operating point at 77.7% SSL
SSL crosses 11.4 T, 16.5 kA @ TCS = 6.86 K
TCS – TOP = 4.96 K
Cable Ic at 11.4 T = 39.4 kA
16.5 kA IOP = 41.8% Cable Ic

## Slide 15: Coil QXFP5, cable 1070 – Witness samples
Billet | # Respools | RRR | Ic(12T) | Ic(13T) | Ic(14T) | Ic(15T) | n(15T)
H0003 | 15 of 40 | 251 | 701 | 581 | 474 | 385 | 46
H0007 | 18 of 40 | 285 | 732 | 608 | 499 | 403 | 47
H0008 | 7 of 40 | 248 | 691 | 577 | 467 | 384 | 41
H0003 | Witness | 323 | 717 | 595 | 491 | 394 | 38
H0003 | As Rcvd | 347 353 | 691 706 | 567 584 | 461 477 | 368 383 | 43 40
H0007 | As Rcvd | 347 349 | 756 749 | 629 621 | 515 507 | 416 407 | 43 30
H0008 | As Rcvd | 301 301 | 688 680 | 566 562 | 461 457 | 368 368 | 52 53
Strand HT 665/75, coil HT 665/50
Fit: cable degradation 2.7%

## Slide 16: Coil QXFP4, Cable 1069 – SSL information
1.9 K SSL intercept 14.94 T, 22.0 kA
16.5 kA Operating point at 75.0% SSL
SSL crosses 11.4 T, 16.5 kA @ TCS = 7.3 K
TCS – TOP = 5.4 K
Cable Ic at 11.4 T = 41.9 kA
16.5 kA IOP = 39.3% Cable Ic

## Slide 17: Summary of Data
Coil | SSL field (T) | SSL current (kA) | IOP/ISSL (%) | T margin (K) | Cable IC (kA) | IOP/IC (%)
MQXFP1 | 15.06 | 22.1 | 74.7 | 5.3 | 44.2 | 37.3
MQXFP2 | 14.82 | 21.7 | 75.9 | 5.1 | 41.0 | 40.2
MQXFP3 |  |  |  |  |  | 
MQXFP4 | 14.46 | 21.2 | 77.7 | 5.0 | 39.4 | 41.8
MQXFP5 | 14.94 | 22.0 | 75.0 | 5.4 | 41.9 | 39.3
Coils P2 and P4 may have been under-reacted.
MQXFP3 has extra sub-elements and lower Cu:NC compared with P2 and P4. The 650/48 HT should also be OK.
As received strand predicts 15.07 T, 22.2 kA at SSL