## Slide 1: MQXFA1 Coil Review Coil QXFP01 Reaction at BNL
J. Schmalzle
March 23, 2017

## Slide 2: QXFP01
Reaction Cycle:
  72 Hours at 210 C
  48 hours at 400 C
  48 hours at 640 C