## Slide 1: SRF Sector Update 2017-05-01
R&D
  Two 3.9 GHz 1-cell cavities were in processing
  One 2.6 GHz cavity tested with good performance (45 MV/m, good Q0), another one to be tested.
  5 1.3 GHz 1-cell cavities were in different stages of processing.
  Two 1.3 GHz 1-cell Cavities were tested, results pending.
LCLS-II
  Two bare cavities road tested, and showed new furnace recipe does not affect mechanical strength
  One E. Zanon cavity qualified. One needs re-HPR and expected to qualify. One is slightly below gradient spec, may be usable if needed.
  CM02 was cold during the weekend. Test starts 5/1.
  CM03 WS5 with instrumentation.
  CM04 is in WS3 stage with thermal strapping and instrumentation
  CM05 WS1 string assembly
  CM06 has 6 qualified cavities compared to last week’s 5.
    Three more to be tested this week (5/1 week)
PIP-II
  Two 650 MHz 1-cell cavity were assembled in clean room for vertical test
  One 650 MHz 1-cell cavity received light EP (8um)
  One spoke cavity horizontal test assembly is in progress at STC test cave
  Two 1-cell 650 MHz cavities were vertical tested. One reached 27.3 MV/m. One is 20.8 MV/m. Re-processing is needed for the second 1-cell cavity.

## Slide 2: Magnet sector update
LCLS II – SPQA105 completed cold testing and is being warmed for alignment and delivery to assembly.
  LARP – Two 4.2 m production-length coils are manufactured simultaneously, one in winding stage one in reaction. Short model MQXFS1c (150 mm aperture) connected to the top plate, leads spliced, final electrical checkout before cool down is expected next week. This is a short 2 m-long model for the HL LHC IR quadrupole upgrade.
AS – A remanufactured Main Ring quad, IQBB401 for MI is ready for MTF test. A MI lambertson spare has completed the bake-out and is cooling after achieving vacuum 10^-8’s.
Mu2e – Making steady progress toward testing the TS proto module in the test facility. Efforts are underway to prepare for releasing the ISA sextupole for bid - 6 magnets are needed.
PIPII – Magnetic measurements of MEBT triplet completed. Negotiating next magnet delivery from BARC.
    G-2 – The SC inflector cable is insulated. Parts are prepared for winding. the NbTi superconducting shield material has been delivered from Japan
MDP 15-16 T dipole R&D – ROXIE EM simulations and FEA models with stress management are in progress.
Infrastructure (IB1) – removing old Tevatron equipment, continuing with feeder removal from the TeV PS, cable trays, feeder cables

## Slide 3: Cryogenic Sector
Organization
  Responding to the OHEP request to update on the status of the cryogenic expertize consolidation by the end of FY17
Operations
  Extending MTA operational support
  NML is being prepared for cooldown: Expect to complete Kinney booster repair by May 10; Compressor oil is processed; Purifier has been regenerated
  LCLS-II CM2 is cold
  MDB warm helium pumping system water piping replacement complete
  Plan to cooldown fast cycling superconducting magnet LDRD late May
  VCTF is operational; VMTF – preparing for MQXFS1c; LCLS-II split quad SPQA-105 testing completed
Projects
  LCLS- II Cryogenic Distribution System
    Feed Cap 1 & 2 inspection at SLAC was success
    End Caps have been delivered to SLAC
    Bypass transferline was delivered to SLAC
  Infrastructure upgrades
  Dilution refrigerator procurement