## Slide 1
George Lewis
Supervisor: Yulia Trenikhina
PARTI/Helen Edwards Final presentation
24 August 2017
Characterisation of SRF Cavity Materials
Notes: With focus on nitrogen treated niobium

## Slide 2: Timeline of my Fermilab internship
1 2 3 4 5 6 7 8 9 10
Weeks at Fermilab
Introductions
Reading
Solo use of SIMS
Coding of data analysis software
Analysis of a temperature series of nitrogen infused samples
Analysis of samples prepared with variations on the 120 °C nitrogen infusion recipe
In-situ baking and nitrogen treatment
Analysis of previous work and ongoing experiments
Notes: Explain contents of talk and that I will explain T series in greater detail and only mention a couple of the other experiments

## Slide 3: Timeline of my Fermilab internship
1 2 3 4 5 6 7 8 9 10
Weeks at Fermilab

## Slide 4: Background – SRF cavities and nitrogen treatment
Figure 1: Bunch acceleration in an SRF cavity1
Superconducting radio frequency cavities
Efficient accelerators
1 CERN, 2014 http://cds.cern.ch/record/1709737
2 Modified from Padamsee, 2017
Figure 2: Typical Q degradation caused by various phenomena2
Nitrogen treated SRF cavities
Even more efficient accelerators
+ Less chance of voltage breakdown
+ Each bunch always sees accelerating field
+ Standing waves store large amounts of energy
+ Superconductivity reduces surface resistance
- Power is still dissipated in the cavity walls
- Costs per unit length are very high
+ Nitrogen treatment lowers surface resistance
(Provides barrier to vortex nucleation)
+ Doping and infusion offer tailored benefits + Higher Q0 means lower total costs
± We still need to know more about it!
Notes:   FAST at Fermilab (27 cells),
  LEP-II at CERN (176 cells)
  ILC, future collider (144 000 cells)
RF beats electrostatic because less limited by breakdown
Work by putting standing wave in cavity, bunch always sees a field that accelerates it.
Time varying B field induces current in surface (Faraday’s law ) so most energy is lost in the walls of the cavity – reducing resistance lowers losses.
SRF still has some loss because High frequency B field penetrates surface layer and induces oscillations in electrons not bound in Cooper pairs,
Nitrogen treatment appears to lower this resistance. Particle accelerators are used widely across science, industry, medicine and security, producing products with a net worth in excess of $500 billion [1]. Research is currently underway to produce Superconducting Radio Frequency (SRF) cavities which will enable the production of a new class of simple, compact and efficient accelerators that will find broad application throughout society [2].
The merit of an SRF cavity is measured by its average accelerating gradient and its quality factor which is a measure of the number of oscillations before the stored energy is dissipated. Typically, at medium fields, it is found that can drop a factor of two between 5 and 25 MV m−1 [3]. However, with nitrogen doped cavities, a so-called anti Q‑slope is observed, whereby is actually increased above the theoretical prediction for pure niobium over this range [4]. Research into optimising the doping process to produce high for medium fields has been successful and a recipe for building cavities has been developed which depends upon the presence of low levels of interstitial nitrogen introduced by injection of nitrogen for 2 minutes and 6 minutes of annealing all at 800 °C, followed by removal of 5 µm by Electro-Polishing (EP) to remove poorly superconducting niobium nitride phases [5].
Particle accelerators are used widely across science, industry, medicine and security, producing products with a net worth in excess of $500 billion [1]. Research is currently underway to produce Superconducting Radio Frequency (SRF) cavities which will enable the production of a new class of simple, compact and efficient accelerators that will find broad application throughout society [2].
The merit of an SRF cavity is measured by its average accelerating gradient 𝐸_𝑎𝑐𝑐 and its quality factor 𝑄_0 which is a measure of the number of oscillations before the stored energy is dissipated. Typically, at medium 𝐸_𝑎𝑐𝑐 fields, it is found that 𝑄_0 can drop a factor of two between 5 and 25 MV m−1 [3]. However, with nitrogen doped cavities, a so-called anti Q‑slope is observed, whereby 𝑄_0 is actually increased above the theoretical prediction for pure niobium over this range [4]. Research into optimising the doping process to produce high 𝑄_0 for medium fields has been successful and a recipe for building cavities has been developed which depends upon the presence of low levels of interstitial nitrogen introduced by injection of nitrogen for 2 minutes and 6 minutes of annealing all at 800 °C, followed by removal of 5 µm by Electro-Polishing (EP) to remove poorly superconducting niobium nitride phases [5].

## Slide 5: Background – Secondary ion mass spectrometry
1 SIMS animation by IONTOF
1
Primary ion beam hits sample to produce secondary ions
Fine control over the primary beam is a major benefit
Can produce depth profiles and surface maps
Exact process is complex and cannot be accurately modelled
One of the most sensitive surface analysis techniques, can detect impurities < 1 ppm
+ Detects all elements, including H
+ Extremely high sensitivity
+ Choice of primary ion beam gives many possibilities
- High degree of complexity
Notes: Explain normal mass spec: Sample is ionized, accelerated by field, deflected by magnets and detected at the end.
What is the difference? We use a primary ion beam which can be finely controlled, and so we can consequently more precisely analyse the sample.
Things like XPS can’t detect H since there are no core electrons.

## Slide 6: Data analysis
Raw data
My analysis program
Unmodified output
Modified output
Notes: 6000 lines of data
600 lines of code

## Slide 7: Experiments: Temperature series
Sample preparation
3 hour bake at 800 °C
30 minutes nitrogen infusion at 7 different temperatures
At what temperature do poorly superconducting nitride phases form?
Sample analysis
Depth profiles taken using SIMS
Surface images taken using SEM
Prediction
Temperature trend should roughly follow Fick’s laws
1st law: , where
A phase change should produce some visible difference
Figure 3: Animation of a scanning electron microscope1
1 Animation by Physics Reimagined
Notes: 1st law: flux goes from regions of high concentration to regions of low concentration
J = Diffusion flux (mol m-2 s-1)
D = Diffusion constant (m2 s-1) follows Arrhenius relation
Phi = Concentration by volume (mol m-3)
Beam scans the surface and impinging electrons eject secondary electrons, number depends on topography
Similar in principle but not destructive

## Slide 8: Experiments: Temperature series
SIMS results
At what temperature do poorly superconducting nitride phases form?

## Slide 9: Experiments: Temperature series
SEM results
At what temperature do poorly superconducting nitride phases form?
800 ˚C
300 ˚C
400 ˚C
600 ˚C
700 ˚C
500 ˚C

## Slide 10: Experiments: Temperature series
Conclusion
At what temperature do poorly superconducting nitride phases form?
600 ˚C
700 ˚C
Shape of depth profile changes from 600 to 700 ˚C
Accompanied by visual change from ‘star-shaped’ to ‘scaly’ nitrides
This possibly suggests a phase transition in the region 600 to 700 ˚C
Future XRD studies will provide further detail
Notes: Different between grains

## Slide 11: Experiments: 120 ˚C nitrogen infusion variations
What are the best parameters for a nitrogen infusion recipe?
Sample preparation
Standard = 3 hr bake at 800 ˚C, 48 hr nitrogen infusion at 120 ˚C & 25 mTorr
Variations: No 800 ˚C bake, 96 hr infusion, infusion at 760 Torr (1 atm)
Results
Regular
760 Torr
96 hr
No 800 bake
Conclusion
Specific treatments can be tailored for specific results
Notes: - Real cavities for these samples provide v. useful insight.
- Each is intelligent empirical treatment
No bake allows to look at effect of oxide on infusion since 800 bake would destroy oxide
Got 2 pieces of puzzle, need more

## Slide 12: Experiments: In-situ sample preparation
How does oxidation change the nitrogen profile?
TOF detector
Analysis gun
Sputtering gun
Prep chamber
Analysis chamber
Baking chamber
Sample preparation
In-situ preparation allows surface analysis before exposure to oxygen
Results
Conclusion
Trial run using in-situ preparation was successful, oxide layer clearly visible

## Slide 13: Conclusion
Several material characterisation experiments performed
Experience gained in SIMS, SEM, python, and being a scientist
Small contribution towards nitrogen-treated SRF cavity research
Finally, to Yulia and all the technical division staff,
the internship coordinators
and my fellow interns…

## Slide 14: Further detail – What is an SRF cavity?
Superconducting Low surface resistance, small power loss
Radio Frequency Surface resistance scales as above 3 GHz
(resonant) Cavity Ellipsoidal shape prevents multipacting
Figure 1: Bunch acceleration in an SRF cavity
(CERN, 2014 http://cds.cern.ch/record/1709737)
Provides efficient acceleration
  Model cavity as LC circuit which produces oscillating E fields
  Lorentz force
  AC resonators permit high power
Thousands installed worldwide:
  FAST at Fermilab (27 cells),
  LEP-II at CERN (176 cells)
  ILC, future collider (144 000 cells)
Notes: - Normal conducting (Super proton synchrotron CERN) 52 Mw for 315 GeV, Superconducting (HERA) 6 MW for 920 GeV beam
SRF cavities work by creating a standing wave of RF frequency
Bunches of particles are timed to arrive such that they receive maximum acceleration
LEP-II is the biggest, over 400 m of SRF

## Slide 15: Further detail: Degradation phenomena
Multipacting: Localised, resonant process where an electron avalanche occurs. Requires the time between electron impacts to be an integer number of half RF periods and occur above a threshold energy – this happens at specific Eacc.
Thermal breakdown: Small defects (scratches, welding beads etc.) give local non-superconducting regions which heat up, this eventually warms the surrounding Nb above Tcrit and the defect grows unstably, quenching the cavity. This can be avoided through taking great care in preparation and by increasing Tc.
Field emission: Micron sized particles lead to exponentially increasing electron currents which cause a rise in temperature and sharp decrease in quality factor. Advanced cleaning techniques such as HPR and the use of class 10 clean rooms. (Also possible to destroy particulates through RF manipulation).
High Field Q Slope: Q reduction around 25 MV m-1, caused by nanohydrides at penetration depth, EP followed by baking at 120 °C provides an empirical solution.
Hydrogen disease: Hydrogen dissolved in Nb can precipitate as a lossy hydride. De-gassing by baking at 800 °C and formation of protective oxide solves issue.
Notes: High pressure rinsing – 100 bar of ultra pure water
Class 10 – particles >0.3 microns totally filtered, less no more than 10 particles <0.1 microns per m^3

## Slide 16: Further detail: Quality factor
  From and for an inductor :
  Using equation for inductance of coil and magnetic induction
  we see that energy stored is
  Similar manipulations yield
  So we end up with:
Quality factors are widely used in physics to describe the selectivity of a signal, generally, Higher Q = Oscillations take longer to die out
There are several ways of defining Q:
  Where G is the geometry factor and depends strongly on cavity shape (but not size).
Notes: High pressure rinsing – 100 bar of ultra pure water
Class 10 – particles >0.3 microns totally filtered, less no more than 10 particles <0.1 microns per m^3

## Slide 17: Further detail: SRF cavities as an LC circuit
Picture two capacitive plates with a parallel inductor
  This creates a resonator with frequency
Now imagine the inductor becomes many single loops of wire, this eventually forms a pillbox cavity
Add a beam tube to allow particles to pass through
Further modify the pillbox cavity to an elliptical one for better field manipulation
=

## Slide 18: Further detail: Primary ion sources for SIMS
LMIG: Liquid Metal Ion Gun uses bismuth (traditionally Gallium but Bi offers a lower melting point)
Produces short, focused beams for analysis
DSC: Dual Sputtering Column fires cesium/oxygen to enhance yield of electro -positive/-negative atoms respectively and sputters sample fast enough to allow depth profiling

## Slide 19: Further detail: Surface resistance in SRF cavities
DC superconductors have zero resistance, but not for AC
High frequency B field penetrates surface layer and induces oscillations in electrons not bound in Cooper pairs
The motion of these electrons dissipates power
By considering the current in normal and superconducting regions of the material, it is possible to derive that
The residual resistance can be caused by impurities, trapped magnetic flux, and lattice distortions.

## Slide 20: Further detail: Challenges
Instrument issues:
  LMIG dropout
  Side emission
  Network issues
  Serious hardware failures
Quantification of data
  SIMS and SEM are by nature qualitative methods
Comparing SIMS profiles of different samples
  Ion behavior varies depending on: operating currents, exposed crystal orientation, sample holder + many more....
Assimilation of data from different sources
  Data from Q vs E curves, SIMS, SEM, XRD, TEM and more must be combined and interpreted coherently
Reduced time for data collection
Notes: J = Diffusion flux (mol m-2 s-1)
D = Diffusion constant (m2 s-1)
Phi = Concentration by volume (mol m-3)

## Slide 21: Further detail: Magnetic vortices and dirty surfaces
Vortices can be thought of as a normal conducting core with superconducting currents encircling them which screens the magnetic flux that is confined within them.
Vortices experience an attractive Lorentz force pulling them to the superconductor’s surface due to interaction with currents
There is also a repulsive Lorentz force between the vortex and the applied field which pushes it into the bulk.
Integrating these forces gives the Gibbs free energy density as a function of depth for the vortex, which shows that there is an energy barrier which in the absence of nucleation points, prevents vortices residing in the bulk
the Ginzburg-Landau parameter can be viewed as a measure of the surface cleanliness (higher if dirty due to shorter mean free electron path), so by considering the case where it varies with depth allows us to analyse the effect of a dirty layer.
It turns out that a thin dirty layer means that vortices are less stable in the bulk and require a greater field to survive. Also its presence greatly increases the energy barrier which can explain a lower RBCS.
1 Graphs from M. Checchin
1
Notes: is London penetration depth
is coherence length
𝜆 is London penetration depth
𝜉 is coherence length