## Slide 1: Prospective on ultimate gradient limitations in SRF cavities
Alex Gurevich
Department of Physics and Center for Accelerator Science,
Old Dominion University, Norfolk, VA
Supported by DOE under Grant DE-SC100387-020
TTC Meeting, FNAL, November 15-17, 2017

## Slide 2: Outline
Nb state of the art: Eacc = 45-50 MV/m and Q = (3-5)1010 @2K and 1.5-2 GHz
What are the fundamental limits of Q and Eacc at 2-4K and 1-2 GHz?
We do not really know, a theory must be developed.
Is it a dc superheating field or a dynamic superheating field?
Nonequilibrium quasiparticles but a quasi-equilibrium SC condensate. How can it affect Hs at 2K and 1-2 GHz? Clean or dirty surface?
New SRF materials (Nb3Sn, Fe-pnictides, ... ?), including alloyed Nb:
Hs = 500 mT (Nb3Sn) or Hs = 700-900 mT for FBS vs 240 mT for a clean Nb
Potentially serious grain boundary limitations of the RF breakdown field in polycrystalline materials other than Nb
Surface materials nano-structuring, multilayers, impurity management to prevent vortex dissipation.

## Slide 3: DC superheating field
Meissner state becomes unstable at H > Hs as the current density at the surface reaches
the depairing limit Jd = Hs/ at the maximum velocity of Cooper pairs, vd = Δ/pF
Hs near Tc: (Matricon and Saint-James, 1967)
Bs decreases as the surface gets dirtier
and the GL parameter κ = λ/ξ increases.
Nb
At T << Tc, only Hs(0) = 0.84Hc at κ >> 1 has been calculated in the clean limit (Galaiko 1966, Catelani and Sethna, 2008) and for an arbitrary impurity concentration (Lin and Gurevich, 2012)
Common ad-hoc extrapolation of the GL results to T << Tc underestimates Hs
Surface barrier for
vortices vanishes at H = Hs

## Slide 4: Non-equilibrium effects at 2K and 1 GHz
SRF frequencies 1-2 Gz are well below the gap frequencies = = 0.7-2 THz:
SRF is quasistatic for the SC condensate. DC pairbreaking unless quasiparticles matter.
SRF frequencies at 2K are much smaller than the temperature:
But it does not mean that quasiparticles are in equilibrium
E
k
kF
Stimulated
superconductivity:
Superfluid density
is increased
(but not the gap!)
Eliashberg, 1971
k
kF
E
Quasiparticle density:
If n(T) << n0,
quasiparticles do not
affect the dynamics
of the SC condensate,
but that may change
at H = Hs
The case of SRF cavities
Not the case of SRF cavities

## Slide 5: Current-induced broadening of N(ε) in clean limit
Rocking “tilted” electron spectrum in the
current-carrying rf state, J(t) = J0cost
Superfluid velocity vs(t) = J/nse
J. Bardeen, RMP 34, 667 (1962)
The energy gap εg =  - pF|vs| <  at vs > 0
Density of thermally-dissociated quasiparticles
increases with H. Gapless state at H = Hs.
2 - 2vpF
2 + 2vpF
Non-equilibrium quasiparticles produced by a shaking N(ε,t)
at H = Hs, so non-equilibrium
SC can affect the dynamic Hs at T << Tc

## Slide 6: Benefits of a dirty layer at the surface
dirty
clean
Effect of current on DOS (Bardeen 1964, Maki, 1963, Fulde, 1965)
Clean limit: gap closes at H < Hs
Dirty limit: gap remains finite (εg = 0.3 Δ) at H = Hs
Impurities can reduce Rs and the high-field Q slope
Moderate reduction of Hs
At H = Hs, the density of quasiparticles can be small
P-J Lin and AG, PRB 85, 054513 (2012)
For Nb @ 2K:
Impurities reduce the influence
of non-equilibrium effects
on the static Hs

## Slide 7: Grain boundaries impeding high SRF currents
H(t)
H(t)
GBs are transparent to the RF current density
GBs are partly transparent to the RF
current density
Critical current density Jc of GB is larger than
J(x) up to
Jc of GB is not large enough to transmit
J(x) above a penetration field:
For Jc = 0.1Jd, Abrikosov-Josephson vortices penetrate in and out of GBs in Nb3Sn at H > 50 mT

## Slide 8: GB problem in cuprates and pnictides
16O [001] tilt grain boundary in YBCO


J
1 nm
X. Song et al. Nature Mat. 4, 470 (2005)
Exponential decrease of Jc with the misorientation angle
GBs behave as weakly-coupled Josephson junctions
Jc = 104 -105 A/cm2 at 15-30o are more then 3 orders
of magnitude smaller than the SRF screening
current densities at Ba = 100 mT:

## Slide 9: GBs block strong currents and pin vortices in Nb3Sn
J
Durrell et al, Rep. Prog. Phys. 74, 124511 (2011)
Vortices caged in the grains and pinned by GBs
GBs transmit currents much smaller than the bulk depairing limit:
Bulk pinning force depends on the grain size d:
GB cuts currents circulating around a vortex
causing its attraction to the GB at r < L:
Gurevich and Cooley, PRB 50, 13563 (1994)

## Slide 10: Hc1 and superheating field for GB vortices
Weakly coupled GBs with
Both BJc1 and BJs are much smaller than Bc, particularly for Nb3Sn with κ = λ/ξ = 20--30
Here but the AJ superheating field can be much larger than if:
Jc is of the order of Jd for a large – κ superconductor like Nb3Sn
GBs do not have edge defects which locally reduce Jc down to
Strongly coupled GBs with
Gurevich, PRB 46, 3187 (1992)
Josephson core length of mixed AJ vortices
GBs as weakly or strongly coupled long Josephson contacts

## Slide 11: How fast can vortices penetrate and can they be stopped?
Nature Comm. 8, 85 (2017)
75 nm thick Pb film: imaging of penetrating vortices with a nanoscale SQUID on tip
Velocities of vortices can reach 10—20 km/s as J(x,y)
at the edge reaches the depairing current density,
(H = Hs in the SRF cavities)
If v = 10 km/s, a vortex penetrates over L = v/f = 10 microns
@ f = 1GHz. Since , vortices penetrate almost instantaneously across the Meissner screening layer.
Hot vortex branching trees ignite global thermal quench. No “natural” materials defects can pin such superfast vortices.

## Slide 12: Arresting penetration of vortices in a multilayer
I layer intercepts propagating vortex loops.
No propagation in the bulk if h(d) < Hc1
Great reduction of the RF vortex power q
localized in a thin S layer:
Nb3Sn: ρn = 0.2 μΩm, d/λ = 0.2, κ = 20,
λ = 100 nm, β = Hp/Hs = 1/2, f = 2GHz
For Nb3Sn, um ≈ 4 μm, and q ≈ 2 μW
Unlike thick Nb3Sn films, a thin ML only slightly (by ≈ 5%) increases the thermal impedance
of the cavity wall. No deterioration of thermal quench stability.
NbN overlayer (C Z Antoine et al, APL 102, 102603 (2013); WM Roach, et al, IEEE Trans. Appl. Supercond. 23 (2013))
NbTiN/Al2O3/Nb thin film bilayers at Jlab (A-M Valente, SUST, 2017 )
Nb3Sn and pnictide multilayers are being developed (C-B Eom,UW/ODU)
MgB2 films coating of Nb (T Tan et al, Sci. Rep. 5, 35879 (2016))
Experimental progress

## Slide 13: Penetration of vortices along GBs
Field onset of penetration for Josephson vortices
Higher Hc = 540 mT for Nb3Sn can result
in better high-field SRF performance only if
GBs are strongly coupled, Jc > 0.2Jd
Mismatch of GB structures in S coating layers and the Nb cavity: I layer intercepts AJ vortices
Penetration of AJ vortices along GBs does not go beyond the first S layer
50-60 mT
Hc1 or
GBs?
25-30 mT

## Slide 14: Maximum screening field
The maximum screening field Hm at the optimum S thickness d = dm
Hm at the optimum thickness exceeds the bulk superheating fields of both Nb and the layer material because of counterflow induced by Nb in the S layers with λ > λ0
For λ >> λ0, practically for λ > 160 nm for a S layer on the Nb cavity with λ0 = 40 nm, Hm approaches the limit
A. Gurevich, AIP Advances, 5, 017112 (2015)
T. Kubo, Y. Iwashita, T. Saeki, APL 104, 032603 (2014); T. Kubo, SUST 30, 023001 (2017)

## Slide 15: Extending the extended Q(H) rise in N-doped Nb cavities above the superheating field of Nb
FNAL, 2013
Hs, Hc1?
Alloyed Nb
film of optimum
thickness
Cavity grade
bulk Nb
A few nm thick
Al2O3 spacer
Capitalize on the extended Q(B) rise
and reverse the reduction of Hc1 and Hs
Use an optimized Nb bilayer to push
the breakdown field above both
superheating fields up to 250-300 mT
A few μm thick dirty layer at the surface
decreases both Hs and Hc1:
Optimized dirty N-doped layer
JLab, 2013
Hs, Hc1?

## Slide 16: Path to 70-120-200 MV/m
Maximum screening field Hm at optimal thickness
Dirty Nb layer on Nb:
Hc = 200 mT, Hs = 170 mT, l = 2 nm, and λ =λ(ξ0 /l)1/2 = 180 nm
Hm = 288 mT, Eacc = 70 MV/m dm = 0.44λ = 79 nm.
20% gain as compared to Hs = 240 mT of clean Nb
Nb3Sn on Nb: Hs = 0.84Hc = 454 mT and λ = 120 nm (moderately dirty):
Hm = 507 mT, Eacc = 120 MV/m, dm = 1.1λ = 132 nm
doubles the superheating field of clean Nb
GARD-RF Research Roadmap Workshop, Washington DC, March 8-9, 2017
Fe-pnictides on Nb: Hs = 0.84Hc = 840 mT and λ = 200 nm:
Hm = 872 mT, Eacc = 206 MV/m, dm = 1.78λ = 356 nm
quadruples the superheating field of clean Nb

## Slide 17: Why is the dielectric barrier important in multilayers?
Smooth decrease of imp concentration,
reduction of Hs and Hc1 at the surface
No protection against penetration
of vortices an interdiffusion
Intercept penetrating vortices and arrest
thermomagnetic avalanches
Great reduction of vortex dissipation
Increase Hs and Hc1
Stop interdiffusion of impurities
Artificial I layers (Al2O3, etc) in ML structures
Natural oxide interfaces which do not dissolve
during deposition of S layers
Direct deposition of S (dirty Nb, Nb3Sn, etc) onto Nb
dirty 1-2 µm
diffusion layer
H(t)

## Slide 18: High-gradient R&D challenges and opportunities
Understanding the fundamental limits of SRF field gradients
Theory of superheating field at low temperatures and GHz frequencies. Manifestations of nonequilibrium effects in a dynamic superheating field.
Physics of vortices driven by strong RF currents
Experimental investigations of dynamic superheating field on small samples and test cavities under controlled conditions of RF and pulsed fields
Getting more out of Nb:
Impurity engineering and surface nanostructuring to optimize 100 nm dirty layer at the surface ( reverse the Q slope and increase Hs ). Nb may still bring surprises.
Deposition of N-infused Nb thin films and SIS multilayers on Nb cavities can capitalize on the Q(H) rise and reverse the reduction of breakdown fields. Can it be done on Nb3Sn?
Beyond the bulk Nb
N-infused Nb-I-Nb ML on Nb (well-developed technology, quick progress appears likely):
Extend the Q(Eacc) rise up to 70 mV/m
Nb3Sn SIS multilayers (more challenging than Nb, current-blocking grain boundaries, low thermal and electrical conductivity, local nonstoichiometry). Higher Q up to 120 mV/m
Pnictides – next level, but a potentially big payoff. Pushing the limit beyond 200 MV/m