## Slide 2: Deposition of NbN and NbTiN thin films
Sergio Calatroni - CERN

## Slide 3: Introduction
Lot of literature on thin films of NbN, NbCN, NbTiN etc…
Several studies for devices, but fewer for SRF
Reviews:
  V. Palmieri, “New Materials For Superconducting Radiofrequency Cavities”, Proc. of SRF 2001
  A.-M. Valente-Feliciano, “Superconducting RF materials other than bulk niobium: a review”, Supercond. Sci. Technol. 29(2016)113002

## Slide 4: BCS
Iso-RBCS lines
at 4.2 K and 500 MHz
128 n
64
32
16
8
4
2
1 n
0.5
0.25
8 10 12 14 16 18
100
10
1
MoRe
NbTiN (600 °C)
NbTiN (200 °C)
NbN (600 °C)
NbN (200 °C)
Nb3Sn
V3Si
Nb

## Slide 5: The NbN phase diagram
From: R. Musenich
SC fcc phase
TC = 17.3 K
SC tetragonal phase
TC = 12÷15 K

## Slide 6: The NbTiN phase diagram at 1200 °C
Equilibrium nitride phase for any Nb,Ti ratio
Segregation of other phases for non optimal composition range
Stabilization of -phase at low temperature, associated with equilibrium segregation of TiN
(from Musenich)
Thin-film sputtering is inherently a non-equilibrium process

## Slide 7: Choosing the right Nb1-xTixN composition
SC NbTi magnets
Optimum for SRF

## Slide 8: Thin film coatings: reactive sputtering
Formation of nitrides
Sputtering yield: YTi > YTiN
Ar + N2
Problem understood and techniques devised to control instability and film composition: larger pumping speed, target to substrate surface ratio…
Sputtering rate [a.u.]

## Slide 9: NbN sputtering
T sputtering = 600 °C
Reactive sputtering transition

## Slide 10: Characterization by simple resonators (examples)
TE011 demountable cavity at 6.5 GHz, NbN
Microstrip resonator at 3.5 GHz, NbTiN
Very promising RBCS
High Rres
Little effect of external DC magnetic field
(Lot of work done for SC-RF devices in many labs)

## Slide 11: Cavity coatings: CEA-Saclay (TE011 plates at 4 GHz)
Tc = 16.0 K
Tc = 16.31 K
Tc = 16.17 K
Proc. SRF 1991
Proc. SRF 1993
Development towards 1.5 GHz stopped

## Slide 12: Cavity coatings: CERN – 500 MHz cavities
12.1979
12.1983
Nb/Cu

## Slide 13: Sputtering of 500 MHz at CERN
Tcoating ≈ 200 °C
Proc. SRF 1991

## Slide 14: Sputtering of 500 MHz at CERN
Proc. SRF 1991
Measured Tc ≈ 14.5 K
RBCS = 9 n
Rres = 18 n
Scaled LEP specs for bulk Nb @ 4.5 K

## Slide 15: Grain-boundary model
Phys.Rev.B 43 (1991) 6128

## Slide 16: Grain boundaries fit
Grain-Boundaries [µcm]
S.C. – Thesis 1990
intragrain ≈ 40÷50 µcm
G.B. ≈ 20÷30 µcm
30÷40% of total

## Slide 17: Sputtering of 1.5 GHz at CERN

## Slide 18: Sputtering of 1.5 GHz at CERN at 350 °C
M. Marino - Proc. SRF 1997
Analysis: G.B. < 20 % of the total resistivity

## Slide 19: Further developments: increase coating temperature
Massimo Marino PhD Thesis 1999
1.5 GHz
Nb/Cu
1÷3 n
150 °C
400 n

## Slide 20: Known limitations
Limit of pumping speed
Cathode temperature and surface ratio
Sputtering profile of cathode, differential adsorption
Atomic composition distribution on cavity Ti/Nb

## Slide 21: Known limitations
Limit of pumping speed and cathode surface
Cathode temperature and surface ratio
Sputtering profile of cathode, differential adsorption
Atomic composition distribution on cavity Ti/Nb
Control of instabilities problematic
New techniques: pulsed sputtering (loss of efficiency)

## Slide 22: Known limitations
Limit of pumping speed and cathode surface
Cathode temperature
Sputtering profile of cathode, differential adsorption
Atomic composition distribution on cavity Ti/Nb
Evolution of cathode composition during sputtering through N2 absorption.
Cooling of cathode

## Slide 23: Known limitations
Limit of pumping speed
Cathode temperature and surface ratio
Sputtering profile of cathode, differential adsorption
Atomic composition distribution on cavity Ti/Nb
N2 to NbTi ratio depends on position, can be problematic close to sputtering threshold.
Better designs are possible

## Slide 24: Known limitations
Limit of pumping speed
Cathode temperature and surface ratio
Sputtering profile of cathode, differential adsorption
Atomic composition distribution on cavity Ti/Nb
Non homogenous composition along cavity meridian
(Can be troublesome for Nb3Sn)
Better cathode design

## Slide 25: Conclusion and perspectives
NbTiN thin films have been sputter-coated on real SRF Cu cavities
Low-field performance at 4.2 K better than for Nb/Cu sputtered films
  Possible use for circular colliders
  (However present R&D is focused on Nb3Sn)
Roads for further improvements:
  Better control of reactive sputtering
  Increase of coating temperature
  Active cooling of the cathode

## Slide 26: 

## Slide 27: Model Nb/Cu films at 500 MHz
Phys.Rev.B 43 (1991) 6128
109
1010
RBCS
RBCS+Rresidual