## Slide 1
Atomic Layer Deposition
of superconductors:
State of the art and future opportunities
Thomas Proslier
16/11/2017
CMS
Double Chooz
HESS
Edelweiss
Herschel
ALICE
Déchiffrer les rayons de l’Univers
Topical TTC meeting 2017
Notes: Saisir les champs « Titre », « P. Nom » et « Date.
Laisser ou retirer le bandeau.

## Slide 2
Collaborations:
Theory-ANL: A. Glatz, D. Ford, M. Kharitonov
CEA: C. Antoine, C. Chapelier, P. Joyez
CERN: S. Calatroni
Jlab: A-M. Valente, G. Ciovati
FNAL: S. Posen, A. Romanenko, A. Grassellino
TRIUMPH: T. Junginger
Cornell: M. Liepe
IIT: J. Zasadzinski
ODU: A. Gurevich
Los Alamos: T. Tajima
Team:
PI: Th. Proslier
Post-doctorants: J. Klug, Nick Groll, K. Chen
Ph.D. Students: C. Cao, N. Becker, M. Weimer
Notes: Cliquez sur Insertion puis En-tête/Pied pour saisir les champs « Evènement – Date » et « Service » ; puis cliquer sur Appliquer partout.

## Slide 3
Multilayers:
A. Gurevich, APL 88, 012511
Fields in bulk Nb cavities approaching dc depairing limit for Nb, Hc(0) ≈ 200 mT
Superconductor-Insulator multilayer [Gurevich, Appl. Phys. Lett. 88, 012511 (2006)]
Increase performance
  Move beyond limits of Nb
Decrease cost
  Higher operating temperature (reduce cryogen costs)
  Replace bulk Nb with cheaper material (Cu/Al)
Coat inside Nb SRF cavity with precise, layered structure → ALD

## Slide 4
Atomic Layer Deposition
The ALD Reaction Scheme involves two separate reagents applied sequentially
  each reagent reacts saturating the surface completely
    Reactant A == Al(CH3)3
    Reactant B == H2O
  each reagent will not react with itself
Application of each AB pulse sequence
  Reforms the original surface
  Adds precisely 1 monolayer
    Defined by Reactant A coverage
    ~ 0.5 ml of Al2O3
Growth rate = Å/cy 0.2 <GR< 5 Å/cy

## Slide 5
Advantages:
Atomic-level control of thickness and composition
Smooth, continuous, pinhole-free coatings on large area substrates
No line-of-sight limits → excellent conformality over complex shaped surfaces
Limits:
Slow
New Alloys means new Chemistries
ALD: Systems

## Slide 6
Atomic layer deposition (ALD)
See: Miikulainen et al., J. Appl. Phys. 113, 021301 (2013).
Puurunen, J. Appl. Phys. 97, 121301 (2005).
Silicides
Borides

## Slide 7
W and Mo: W/MoF6 + Si2H6 -> W/Mo + SiHxFy(g) – deposition < 200°C
pure Mixture amorphous/crystalline ( TC = 3K for W). Growth rate ~ 5Ǻ/cy.
Pd/Pt/Ir: Pd(hfac)2 + HCOH -> Pd + gas reactants – deposition = 200°C
Pure, crystalline – GR ~ 0.2Ǻ/cy
Pt(MeCp)Me3 + O2 -> Pt + gas reactants – deposition = 300°C
Pure, crystalline – GR ~ 0.45 Ǻ/cy
Ir(acac)3 + O2 -> Pt + gas reactants – deposition = 350°C
Pure, crystalline – GR ~ 0.4 Ǻ/cy
Ni/Co: Ni/Co(dmamb)2 + NH3 -> Ni/Co + gas reactants – deposition = 300°C
O, crystalline – GR ~0.6 Ǻ/cy
Few examples of elementals by Atomic layer deposition (ALD)
Cu,Pt, Ir, Pd, Ni, Co: Island growth
Pure: C, O, N <~ 1%

## Slide 8
Superconductors by ALD
Goal for SRF is a material with a Tc higher than bulk Nb (9.2 K)
Niobium Carbide: NbC 1.7 K
  NbF5 + Al(CH3)3
  NbCl5 + Al(CH3)3
Niobium Carbo-Nitride: NbC1-xNx 3.8 K
  Al(CH3)3 + NbF5 + NH3
  Al(CH3)3 + NbCl5 + NH3
Niobium Silicide: NbSi 3.1 K
  NbF5 + Si2H6
  NbF5 + SiH4
Titanium Nitride: TiN 3.9 K (4 K)
- TiCl4 + NH3
Molybdenum Nitride: MoN 12 K (12-13 K)
  MoCl5 + NH3
  MoCl5 + Zn + NH3
Niobium Titanium Nitride: Nb1-xTixN 14 K (17 K)
  (NbF5, TiCl4) + NH3
  (NbCl5, TiCl4) + Zn + NH3
Superconducting alloys grown by ALD

## Slide 9
Superconductors by ALD
Goal for SRF is a material with a Tc higher than bulk Nb (9.2 K)
Niobium Carbide: NbC 1.7 K
  NbF5 + Al(CH3)3
  NbCl5 + Al(CH3)3
Niobium Carbo-Nitride: NbC1-xNx 3.8 K
  Al(CH3)3 + NbF5 + NH3
  Al(CH3)3 + NbCl5 + NH3
Niobium Silicide: NbSi 3.1 K
  NbF5 + Si2H6
  NbF5 + SiH4
Titanium Nitride: TiN 3.9 K
- TiCl4 + NH3
Molybdenum Nitride: MoN 12 K
  MoCl5 + NH3
  MoCl5 + Zn + NH3
Niobium Titanium Nitride: Nb1-xTixN 14 K
  (NbF5, TiCl4) + NH3
  (NbCl5, TiCl4) + Zn + NH3
Superconducting alloys grown by ALD

## Slide 10
Molybdenum nitride
d-MoN (P63mc)
g-Mo2N (Fm3m)
_
Crystal structures: Bull, et al., J. Solid State Chem. 177, 1488 (2004); Bull, et al., J. Solid State Chem. 179, 1762 (2006)
Tc = 12 K
Tc = 5.2 K

## Slide 11
Linear, well controlled growth with fine thickness control
Bulk-like density, roughness 25-35 Å
Growth temperature: 450 0C
MoCl5 + NH3 - AlN : AlCl3 + NH3
Molybdenum Nitride (MoN)

## Slide 12
MoNx ALD: Tc vs. thickness

## Slide 13
MoNx ALD: MoCl5 and NH3 – Epitaxy ?
Al2O3
MgO
MoN
TEM: C. Alvarez (ANL/NU)
Open questions:
Unclear why or how structure evolves during nucleation.
Can nucleation be controlled with process parameters?
DFT (D. Ford/P. Zapol, MSD) → structure and coordination in first few layers should have a strong effect.

## Slide 14
MoN (0001)
Mo2N (111)
Al2O3 (0001)
MoNx Density Functional Theory
MoN/Al2O3 Mo2N/Al2O3 MoN,int – Mo2N,int
m(N,NH3) @ 298K,0.1MPa m(N,NH3) @ 673K,0.1MPa
DFT shows that: Mo2N is more favorable on C-Plan and MoN is preferred on R-Plan
Confirm the trend seen experimentally

## Slide 15
Summary - Epitaxy
High quality epitaxial IV-VI nitrides synthesized by atomic layer deposition at modest temperatures (450°C).
Films on a-Al2O3 show superior electrical and superconducting properties compared to those grown concurrently on amorphous SiO2.
Klug, Becker, et al., Appl. Phys. Lett. 103, 211602 (2013).

## Slide 16
60 nm MoN
Klug, Becker, et al., Appl. Phys. Lett. 103, 211602 (2013).
Electrical Properties

## Slide 17
MoNx ALD: Tc vs. thickness
Tc = 9.25 K
ΔNb = 1.55 meV
15nm
18 nm
20 nm
30 nm
60 nm
Thickness > 50 nm

## Slide 18
Hc2(0) → x(0) = 5.7 ± 0.1 nm
MoNx ALD: Field dependence
Assume λ ~ 200 nm, estimate JD(0)~1×108 A/cm2; JD(2K)~8×107 A/cm2, Jc(0) ~ 107 A/cm2
For MoN (d = 60 nm) on 50 µm Cu wire, IMAX ~ 1,5 A; IMAX(2K) ~ 1,3 A
H

## Slide 19
Copper magnet
2.5 cm
Cu/MoN(1000cy)/AlN(300cy) at 450°C : 200 wires/ 50 µm diameter
Conformal Deposition
  Multilayer SIS
JC EXP ~ 10% de JD, IMAX ~ 260 A per layer at 2 K
MoNx ALD: Application - magnets ?

## Slide 20
Niobium Titanium (Nb1-xTixN) 2:1
Decrease temp:
lower density
more impurities ~ 2% Cl @ 350 0C
(NbCl5 + Zn + NH3)N + (TiCl4 + Zn + NH3)
-> ZnCl2 (> 410 0C)
N=2 (2:1 ratio)
XPS
XRR

## Slide 21
Niobium Titanium (Nb1-xTixN) 2:1
Resistivity bulk ~ 250 μΩ.cm
Tc bulk ~ 7.8 K
Resistivity bulk ~ 630 μΩ.cm
Tc bulk ~ 4.5 K
450 0C
350 0C

## Slide 22
Niobium Titanium (Nb1-xTixN) 2:1 with Zn
Resistivity bulk ~ 150 μΩ.cm
Tc bulk ~ 12.5 K
Si
NbTiN
AlN
TEM
Grain size ~ 30 nm
Cubic (200) and (111)

## Slide 23
41
Nb1-xTixN: Superconducting Tc
Achieved superconducting Tc=14 K 4:1
  40% higher than previously reported value for ALD NbN [Hiltunen et al., Thin Solid Films 166, 149 (1988)]
Δ = 2.3 meV +- 0.1
T= 1.8K

## Slide 24
(t-butylimido)tris(diethylamido) Nb(V) –TBTDEN Nb
H2 plasma-300°C – GR ~ 0.4 Ǻ/Cy – Each Cycle ~ 4 mins
Plasma enhanced ALD of NbN
M. Sowa et al. Journal of Vacuum Science and Technol. A. 35, 01B143 (2017)

## Slide 25
Controlled composition
TiCl4/NbCl5 Ratio ALD Cycles
Atomic control of Composition -> Tune Tc

## Slide 26
ALD on Nb cavity - superconductors
Deposition at temp. > 250°C for10 hr to 48 hr on Nb metal require an UHV environment
Clean room(100)
HV Oven : 10-8T a 500 0C
Automatic growth process
4 solid precuror lines HT (250°C)
1 precursor line UHT (500°C)
4 precursor lines gases/liquids
RGA analysis

## Slide 27
Eacc [MV/m]
NbTiN/AlN
ALD multilayer NbTiN(50 nm)/AlN(10 nm) 450°C – 10 hrs
ALD
ALD multilayer MoN(80 nm)/AlN(10 nm) 450°C – 10 hrs
Chart: 
| 5.1286138399136494 | 5.559042572704036 | 5.7543993733715713 | 5.7543993733715713 | 5.1286138399136494 | 4.7315125896148054 | 4.4668359215096318 | 3.6307805477010135 | 1.9724227361148534
2.0 K | 1454857147.9696 | 1201401534.5881 | 1119596357.7998 | 896887797.6797 | 1544351364.6669 | 1748124763.4927 | 1946213396.3146 | 2493970638.2896 | 1807858751.6761
2.0 K | 877902130.0759 | 1140016401.6456 | 1462766119.6586 | 1791595106.975 | 2194489281.763 | 1755730191.4596 | 914303547.1222 | 440573170.2397
3.5 K | 720892972.6904 | 892346473.6784 | 764117606.7172 | 870668762.022 | 912300977.7101 | 1030498207.8534 | 1023623231.0438 | 1052965833.8773 | 959794350.5156 | 959622223.7913 | 988853849.5968 | 848151720.9416 | 714686130.9974 | 622830539.9402 | 446054422.7316 | 383700216.5555
Eacc [MV/m]
2 K
3.5K
MoN/AlN
ALD on Nb cavity - superconductors

## Slide 28
Summary
Tune Tc and transport properties by controlling film thickness
  Tune Tc and transport properties by controlling composition: Nb1-xTixN, TiN, MoN, NbSi, NbC, NbCN ...
  Growth temperature : lower Temp for High quality nitrides
  Fundamental interest for Quasi 2D limits + applications: Bolometers, High energy physics accelerators, magnets…
  Future work:
  MgB2 (40K), FeSeTe (15K), K(FeSe)2 (31K) etc… More cavity coating/Testing
  functionalizing top surface of Nb (normal metals W, Mo…)

## Slide 29
Direction de la Recherche Fondamentale
Institut de recherche
sur les lois fondamentales de l’Univers
Commissariat à l’énergie atomique et aux énergies alternatives
Centre de Saclay | 91191 Gif-sur-Yvette Cedex
Etablissement public à caractère industriel et commercial | R.C.S Paris B 775 685 019
Service
THANKS !
Notes: Saisir le champ « Service »

## Slide 30
Synchrotron tools
Synchrotron techniques offer a suite of probes sensitive to atomic-scale structural and chemical information.
By applying synchrotron measurements in situ to study ALD processes, we can investigate the evolution of crystallinity, microstructure, morphology, and chemical composition in the crucial early stages of film growth.
ALD
ALD
Crystallinity
Microstructure
Morphology
Composition

## Slide 31
ALD “Viscous Flow” Reactor
Elam, et al., Rev. Sci. Instrum. 73, 2981 (2002).

## Slide 32
ALD on wheels
3 high vapor pressure precursor channels
2 low vapor pressure precursor channels
Computer controlled flow/pneumatic valves
7 independent PID heater channels
Remote operation, SPEC/EPICS trigger

## Slide 33
ALD Reactor Modules
X-ray scattering module
grazing-incidence XRF/XAS module
Total transmission (in & out)
Advantages of Graphite
Non-toxic
High temperature
Easy to clean
10x less expensive than Be
Klug, et al., Rev. Scientific Instrum. 86, 113905 (2015).

## Slide 34
MoNx ALD: Application ?
TiN(7.5 nm)/MoN(50nm) at 450°C
SQUID

## Slide 35
ALD on Nb cavity: Test
10 nm Al2O3 (90°C – 1 hr)
2 nm Al2O3 / 15 nm Nb2O5(250°C – 2 hr)
15 nm Al2O3(250°C – 2 hr) + 450 °C/20 hrs
Remplace Nb2O5 by another more stable oxide: l’Al2O3
Diffusion/decomposition of Nb2O5 into bulk Nb to create a
clean interface.

## Slide 36
Hall measurement
Carrier concentration
Dirty limit: ξ > l
Transition:
Strong disorder kF.l~1 to kF.l >> 1
meff = 6.4 me
MoNx ALD: Hall effect vs. Thickness

## Slide 37: Titre intercalaire

## Slide 38: Nb1-xTixN: Superconducting Tc
Achieved superconducting Tc=14 K 4:1
  40% higher than previously reported value for ALD NbN [Hiltunen et al., Thin Solid Films 166, 149 (1988)]
Δ = 2.3 meV +- 0.1
T= 1.8K
50 nm NbTiN film

## Slide 39: In situ X-ray reflectivity: ALD ZnO on Al2O3(0001)
Why ZnO?
Wide band-gap semiconductor with may uses (LEDs, TFTs, solar cells, etc.)
Epitaxial growth on a-Al2O3 is well established (even by ALD)
ALD ZnO
Well behaved, widely studied ALD chemistry
Low temperature process (<180 °C)
High volatility, liquid precursors ((C5H5)2Zn and H2O)
Previous in situ study on Si(001) (Fong APL 2010)
A good process to test a new instrument.

## Slide 40: In situ X-ray reflectivity: ALD ZnO on Al2O3(0001)
Measurement details
Beamline: 33BM-C
Energy: 15.5 keV
Detector: PILATUS 100K
Measurement goal
Observe film structure and morphology evolve during epitaxial growth

## Slide 41: In situ X-ray reflectivity: ALD ZnO on Al2O3(0001)
ALD parameters
Temperature: 150 °C
Pressure: 3 Torr
0.25s-30s-0.25s-30s (DEZn-purge-H2O-purge)
Measurements
Low angle/1 cycle
Short L-scan/5 cycles
Full L-scan/10 cycles
Klug, et al., Rev. Sci. Instrum. (submitted).

## Slide 42: ZnO/Al2O3(0001): Low angle X-ray reflectivity
Analysis of every 5th cycle
Transition at ~20 cycles
After 20 cycles:
  Linear 1.7 Å/cycle
  Density ~90% of P63mc
  Roughness ~8 Å
Before 20 cycles:
  Growth/cycle ~1 Å/cycle
  Rise in roughness (island nucleation – Fong, et al.)
Klug, et al., Rev. Sci. Instrum. (submitted).
  Non-monotonic change in density → change in either composition or structure

## Slide 43: ZnO/Al2O3(0001): Low angle X-ray reflectivity
Additional complexity
Thickness ~cZnO for #2-7
Gradual increase in density, roughness up to #6
Abrupt rise in density, roughness at #7 followed by onset of thickness change
Initial growth only on Al2O3,
Klug, et al., Rev. Sci. Instrum. (submitted).
cZnO
Notes: This behavior suggests initial ZnO growth primarily on the Al2O3 surface, with the formation and gradual densification of a single unit cell of ZnO up to a critical density, which subsequently leads to an abrupt change in film density, morphology, and structure, as well as the onset of out-of-plane film growth. I like that “multilayer roughness”

## Slide 44: ZnO/Al2O3(0001): High resolution X-ray reflectivity
Steady growth of ZnO(0002) peak, thickness fringes
Film is crystalline, oriented throughout deposition (in contrast to Si(001)/Fong, et al.)
Klug, et al., Rev. Sci. Instrum. (submitted).
  Change in lattice constant is further evidence of evolution in composition/structure.
  Need to look at in-plane structure, morphology.
Notes: The agreement between the thickness values extracted from XRR and CTR indicates that c-axis oriented, crystalline ZnO was deposited on Al2O3(0001) from the initial nucleation period onward, in
contrast to the findings of Fong et al., where no evidence of crystalline ZnO was observed within the first 45 A of deposition at 125 C on native oxide Si.

## Slide 47
Notes: Cliquez sur Insertion puis En-tête/Pied pour saisir les champs « Evènement – Date » et « Service » ; puis cliquer sur Appliquer partout.