## Slide 1
Dependence of flux trapping and flux penetration on various treatment
Shreyas Balachandran
Anatolii Polyanskii, Santosh Chetri, Mingmin Wang, Thomas R. Bieler, Pashupati Dhakal, David C. Larbalestier, Peter J. Lee

## Slide 2: Background- SRF Nb cavities with High Q
Performance of cavities is given by quality factor Q0
Residual surface resistance (Rs)
Rs = RBCS + Ri
Extrinsic Material properties (precipitates, microstructure etc) , trapped magnetic vortices
A Grassellino et al 2017 Supercond. Sci. Technol. 30 094004
N infusion
Baseline

## Slide 3: Trapped vortices increase Rs by several nΩ/mG during operation
Effects of trapped vortices can be reduced by:
Better magnetic shielding
Surface preparation, and reduction in lossy hydride precipitates (2000- present)
  Heat treatments and nitrogen doping reduce hydride precipitates.
Flux expulsion by gradient cooling through Tc (2014- present )
  Temperature gradient creates a thermal force which counteracts the pinning force of defects, and flux is expelled from the superconducting state.

## Slide 4: Flux expulsion behavior improves with 1000˚C/4h heat treatment
1000 C/4h
S. Posen; et.al Journal of Applied Physics 2016, 119,
As received
Heat treatment at 900C/3h
Heat treatment at 1000C/3h

## Slide 5: Driving questions for our research
Do grain boundaries (GB’s) pin flux, and under what conditions?
Do slip bands and substructures (dislocation networks) affect flux penetration?
Can DC magnetization measurements on coupon samples be used to characterize flux trapping?

## Slide 6: MO imaging- Qualitative understanding of flux behavior in SRF Nb
MOI Schematic and principle
Allows direct Imaging of Bz in plane above superconductor
Double Faraday effect occurs in reflective mode using Bi-doped YFe indicator film with in-plane magnetization
ZFC- Cooled in the absence of external fields to below Tc, at T< Tc visualized in an external magnetic field.
FC- Sample cooled below Tc in the presence of a magnetic field, and visualized after removing the external field
Notes: Magneto optical (MO) imaging is a remarkable tool for viewing the local and global flux penetration into a superconductor. It uses the strong Faraday Effect in bismuth doped yttrium iron garnet (B-YIG) to measure the change of vertical magnetic field component above a superconducting sample using a standard polarized light microscope. The garnet imaging film is placed directly on the Nb so as to attain the highest possible sensitivity. The technique is able to resolve fields of the order of 1 mT with ~ 5–10 μm spatial resolution. A continuous flow cryostat is able to cool a sample down to ~5 K, and two external electromagnetic solenoids can apply vertical (Hz) and in-plane (Hx) fields up to ~ 120 mT to the sample.

## Slide 7: Do grain boundaries (GB’s) pin flux, and under what conditions?

## Slide 8: Sample description (GBNX9) and procedures flow chart
As received 3mm Ningxia bi-crystal sample, cut from LG sheet from MSU
Mechanical polishing, and 10 µm BCP at FSU
MO imaging
MO1
OIM analysis
Sample was BCP’ed at JLAB
800˚C/3h + 140C/48h- 25 mTorr Nitrogen infusion
Cool down cycle
Below Nb Tc (9.2K)
MO imaging
MO2
Below Nb Tc (9.2K)
Cool down cycle

## Slide 9: Magneto Optical Image(MO-1) of as received Nb disk after MP +10µm BCP
After BCP at room temperature
GB
3 mm diameter: EDM + BCP of as-received Ningxia sample
MO image, overlaid on optical image
Flux trapped
GB
Applied field H points out of plane
Flux trapped “fork”
GB oriented parallel to the applied field causes flux penetration (Polyanskii, et.al AIP Conf. Proc. 1352, 186-202 (2011)).
The fork in the sample was unexpected

## Slide 10: MO1: DC flux trapping can occur due to low angle boundaries in SRF Nb.
GB
GB
Hydride pits
Crystal 1
Crystal 2
Crystal 3
Misorientation measurements across boundaries indicates a low-angle boundary with a misorientation of 3 °
Identifying these boundaries is a challenge
RF, T = 8.7 K, H = 0, after H =32 mT
Hydride remains indicate excess hydrogen in the sample

## Slide 11: MO2 Flux trapping at GB’s no longer visible after 800˚C/3h + 140˚C/48h-25 mTorr N2 infusion
GB
Scratch
After 800˚C/3h + 1400C/48h-25 mTorr N2
GB not distinguishable by MO after 800˚C/3h +140˚C N infusion heat treatment. No micron sized hydride pits
GB
RF, T = 6.4 K, H = 0, after H =22 mT
MO image
Crystal 1
Crystal 2
GB

## Slide 12: 800˚C/3h + 140˚C/48h-25 mTorr N2 heat treatment removes GB pinning
GB
RF, T = 6.4 K, H = 0, after H =22 mT
Summary of Observations:
GB, and LAGB are intact after 800˚C/3h + 140˚C/48h-25 mTorr N2 infusion heat treatment.
Weak pinning observed after 800˚C/3h + 140˚C/48h-25 mTorr N2 infusion heat treatment.
Questions:
Do contaminants contribute to GB pinning in SRF Nb?
Does a high temperature heat treatment lead to a cleaner GB?
  Lesser hydrogen, interstitial (O) redistribution?

## Slide 13
1. Do slip bands and substructures (dislocation networks) affect flux penetration?

## Slide 14: Example- Nb microstructure after deformation and heat treatment
Heavily deformed Nb- Total Shear Strain of 5.6.
Equivalent Rolling thickness reduction (90%)
800C/3h
600C/3h
Partial Recrystallization
Full Recrystallization

## Slide 15: Preliminary MO result on shear-deformed Nb (RRR 130) bi-crystal. Do dislocation networks influence flux penetration?
GB
Deformation features
Deformation features
Crystal 1
Crystal 2
ZFC, T=6.3K H=52 mT
Crystal 2
Crystal 1
GB
ZFC, T=6.3K H=100 mT
Crystal 1
Crystal 2
ZFC, T=6.3K H=112 mT
Crystal 1
Crystal 2
5mm

## Slide 16: Why are dislocation substructures important? Unrecovered substructure occurs in as received Nb sheets used to fabricate cavities- Example Sheet id: 342104
Through thickness scan shows regions where the substructure is unrecovered even after a recrystallization heat treatment
Cross-sectional OIM of sheet id: 342104, Vendor A for LCLS-II
~3mm

## Slide 17: Dislocation substructures are also present in as received sheet id: T11007, Vendor B for LCLS-II.
Cross-sectional OIM of sheet id: T11007
Vendor B for LCLS-II
~3mm
Unrecovered substructure
Through thickness scan shows regions with substructure on near surface layers.

## Slide 18: Can DC magnetization measurements on coupon samples be used to characterize flux trapping?

## Slide 19: Flux trapping measurements on coupon samples from cavity replica material (JLAB)- Sample description
Cavity performance
Φ1 mm
3 mm
3 mm
Coupon samples also underwent the recipes shown and the same color-scheme will identify the HT
Test | Δ/kBTc | mfp (nm) | Rres (nΩ)
Baseline (ILC) | 1.82 ± 0.02 | 164 ± 27 | 2.2 ± 0.1
+120 °C/48h* | 1.86 ± 0.02 | 26 ± 7 | 4.6 ± 0.2
+800 °C/3h+ 120 °C/48h@25 mTorr N2 | 1.84 ± 0.02 | 28 ± 5 | 1.9 ± 0.1
+10 μm EP | 1.81 ± 0.02 | 164 ± 23 | 1.2 ± 0.1
+800 °C/3h+ 160 °C/48h@25 mTorr N2 | 1.80 ± 0.02 | 54 ± 14 | 1.0 ± 0.1
+10 μm EP | 1.79 ± 0.02 | 122 ± 16 | 0.5 ± 0.1
+800 °C/3h+ 140 °C/48h@25 mTorr N2 | 1.80 ± 0.02 | 26 ± 87 | 0.9 ± 0.1
No post chemistry after each furnace treatment.
Dhakal. P, et.al,
https://arxiv.org/abs/1711.03991

## Slide 20: Coupon Flux Trapping: Magnetization measurements
M = 0
Any magnetization observed under this condition is due to the trapped flux
The samples were field cooled (1 mT) to below Tc (8.5 K) of Nb. Cooling rate: 5 K/min. Then the field was removed
1 mm diam.
3 mm long
Nb cylinders
T = 12 K >9.2 K(Tc)
Bext= 1 mT
T=8.5 K< 9.2 K(Tc)
Bext = 1 mT
T=8.5 K< 9.2 K(Tc)
Bext = 0 mT
Flux Trapping
  M ≠ 0

## Slide 21: Result: Variations observed in flux expulsion observed with different treatments
No DC flux trapping in 800 °C/3h coupon cylinder
Among N infusion samples, low flux trapping was observed in 140 °C/48h+N infused sample
800 °C/3h+N2 160 °C/48h
800˚C/3h
800°C/3h+120°C/48h
800 °C/3h+N2 140 °C/48h
800 °C/3h+N2 120 °C/48h
Warming

## Slide 22: Summary and Discussion Questions
MO imaging indicates that flux trapping behavior is enhanced after mechanical polishing and BCP. After, 800˚C/3h + N infusion heat treatment, the bulk pinning is low.
  Is contamination or normal precipitates at and around GB’s responsible for trapping behavior?
Systematic studies on recovery and recrystallization of deformed Nb bi-crystal is on-going.
  Preliminary results indicate deformation structures could influence flux penetration.
As received sheets from Vendor A, and Vendor B for LCLS-II cavities show presence of dislocation networks and substructure.
  How important are dislocation networks, substructures in final cavity material?
  Is incomplete recrystallization a symptom of residual interstitials?
  Influence of local chemistry on recovery and recrystallization needs evaluation..
Coupon studies could be an option to evaluate flux trapping behavior in SRF Nb.
What bulk properties are relevant for Nb specifications for for High Q and High Gradient material?

## Slide 23: Acknowledgements
This material is based upon work supported by the U.S. Department of Energy, Office of Science, Office of High Energy Physics under Award Numbers # DE-SC 0009960 (FSU) and DE-FG02-09ER41638 (MSU) and the State of Florida. Additional support for the National High Magnetic Field Laboratory facilities is from the NSF: NSF-DMR-1157490. We also thank Chris Compton at FRIB for providing a large grain Nb slice used for some of this work
Thank you!

## Slide 24: EXTRAS

## Slide 25: GB and flux penetration- Angular dependence with applied field (H) in SRF grade Nb
GB plane normal (n)
GB trace
GB trace
MO indicator
H
n
ZFC, T= 8.1 K, H = 80 mT,
H●n ≠ 0
ZFC , T = 6.4 K
H = 80 mT
H = 112 mT
H●n ~ 0
n
MO indicator
H

## Slide 26: Literature- Grain boundaries as pinning centers.
Distortions only exist on an atomic scale around GB’s
Image:
http://wwwhrem.msm.cam.ac.uk/gallery/pics/allarge.jpg
Zerweck (1981)- Pinning by GB takes place through the electron scattering mechanism.
Electron mean free path (m.f.p) decreases near the GB, and the coherence length (ξ) becomes shorter.
Variation in the electron mean free path with the distance from the boundary [Zerweck,1981].
Ref: Fig 6.10. T. Matsushita, Flux Pinning in Superconductors
Distance from boundary
m.f.p
Variation in the coherence length with the distance from the boundary [Zerweck,1981].
Ref: Fig 6.11, T. Matsushita, Flux Pinning in Superconductors
α- Impurity parameter
α=0.01
α=10
Distance from boundary
Crystal 1
Crystal 2

## Slide 27: Literature- Pinning force at Grain boundary
Dependence of the elementary pinning force (per unit length of the flux line) of the grain boundary on the impurity parameter (after Welch (1985)).
Boundary thickness
d = 0
d = 1.5ξ
Pinning at the GB is attributed to change in the coherence length.
  Could lead to Hc2 enhancement
Impurity parameter α, is an introduced parameter.
Impurities can be present at GB’s in Nb.
Diffusion of interstitials can occur at a faster rate along GB’s
Example: GB in SRF Nb can be easily contaminated by a nonsuperconducting phase produced during the chemical treatment.
Z.Sung et.al, IEEE Trans, 2014

## Slide 28: Background- Polycrystalline deformation structures.
10’s of nm
Common features in metals deforming where slip (multiple) is the major deformation mechanism.
Nb deforms by multiple slip
10-100 µm
mm
100-1000 nm
Adapted from Fig 2.8, Humphery, and Hatherly, Recrystallization and Related Annealing Phenomenon, Second Edition

## Slide 29: Background- Annealing of Polycrystalline deformation structures- Heat treatment effects
Deformed state
Recovery
Partial Recrystallization
Full Recrystallization
Adapted from Fig 1.1, Humphery, and Hatherly, Recrystallization and Related Annealing Phenomenon, Second Edition
New nuclei
GB
Deformation in grain
Recovered dislocation structure in grain
New GB